Copyright 2010 AIA
MasterSpec Professional
02/10

Copyright 2010 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 071353 - ELASTOMERIC SHEET WATERPROOFING
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. EPDM rubber sheet waterproofing.

2. Butyl rubber sheet waterproofing.

1.2 PREINSTALLATION MEETINGS

A. Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

1.3 ACTION SUBMITTALS

A. Product Data: For each type of product.

Retain "Shop Drawings" Paragraph below if justified by extent or complexity of waterproofing.

B. Shop Drawings: Show locations and extent of waterproofing and details of substrate joints and cracks, sheet flashings, penetrations, inside and outside corners, tie-ins with adjoining waterproofing, and other termination conditions.

1.4 INFORMATIONAL SUBMITTALS

A. Sample warranties.

1.5 QUALITY ASSURANCE

Revise "Installer Qualifications" Paragraph below to suit warranty requirements; verify with manufacturers that installers meeting this requirement are available for Project location.

A. Installer Qualifications: An entity that employs installers and supervisors who are trained and approved by waterproofing manufacturer.

1.6 WARRANTY

Waterproofing warranties for EPDM and butyl sheet waterproofing are limited to materials only.

A. Manufacturer's Warranty: Manufacturer's standard materials-only warranty in which manufacturer agrees to furnish replacement waterproofing material for waterproofing that does not comply with requirements or that fails to remain watertight within specified warranty period.

Verify available warranties and warranty periods.

1. Warranty Period: [10] [20] <Insert number> years from date of Substantial Completion.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 SHEET WATERPROOFING

A. EPDM Rubber Sheet: ASTM D 6134, Type I, 60-mil- (1.5-mm-) thick flexible sheet, unreinforced, formed from EPDM.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Carlisle Coatings & Waterproofing Inc.; Sure-Seal EPDM.

b. <Insert manufacturer's name; product name or designation>.

Revise thickness in "Butyl Rubber Sheet" Paragraph below to suit Project; 60-mil (1.5-mm) thickness is most common. Distinguish thicknesses for vertical wall and plaza-deck applications.

B. Butyl Rubber Sheet: ASTM D 6134, Type II, [60-mil- (1.5-mm-)] [90-mil- (2.3-mm-)] [120-mil- (3.0-mm-)] thick flexible sheet, unreinforced, formed from isobutylene-isoprene rubber.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Carlisle Coatings & Waterproofing Inc.; Sure-Seal Butyl.

b. <Insert manufacturer's name; product name or designation>.

2.2 AUXILIARY MATERIALS

A. General: Furnish auxiliary materials recommended by waterproofing manufacturer for intended use and compatible with sheet waterproofing.

1. Furnish liquid-type auxiliary materials that comply with VOC limits of authorities having jurisdiction.

B. Concealed Sheet Flashing: Same material, construction, and thickness as sheet waterproofing or 60-mil- (1.5-mm-) thick, uncured EPDM, as required by manufacturer.

Retain "Exposed Sheet Flashing" Paragraph below if sheet flashings are exposed.

C. Exposed Sheet Flashing: 60-mil- (1.5-mm-) thick EPDM, cured or uncured, as required by manufacturer.

Retain "Bonding Adhesives" Paragraph below for sheets fully and partially adhered and for sheet flashings.

D. Bonding Adhesives: For bonding waterproofing sheets and sheet flashings to substrates and projections.

Retain "Splicing Cement and Cleaner" Paragraph below for splicing seams in EPDM and butyl.

E. Splicing Cement and Cleaner: Single-component butyl splicing cement and solvent-based splice cleaner.

Retain "Butyl Gum Tape" Subparagraph below with "Splicing Cement and Cleaner" Paragraph above if seams require splicing cement and butyl gum tape.

1. Butyl Gum Tape: 30-mil- (0.76-mm-) thick-by-6-1/4-inch- (160-mm-) wide, uncured butyl with polyethylene release film.

F. Lap Sealant: Single-component sealant.

Retain "In-Seam Sealant" Paragraph below if seams use splicing cement without butyl gum tape.

G. In-Seam Sealant: Single-component sealant.

H. Water-Cutoff Mastic: Butyl mastic sealant.

I. Waterproofing and Sheet-Flashing Accessories: Provide sealants, pourable sealers, cone and vent flashings, inside and outside corner flashings, termination reglets, and other accessories recommended by waterproofing manufacturer for intended use.

J. Metal Termination Bars: Manufacturer's standard aluminum bars, approximately 1 inch (25 mm) wide, prepunched, with fasteners.

Retain protection course type from two "Protection Course" paragraphs below. Delete paragraphs if molded-sheet drainage panels or insulation drainage panels replace protection course.

Product in first "Protection Course" Paragraph below describes Carlisle's "Protection Board H."

K. Protection Course: Semirigid sheets of asphalt-impregnated organic mat, mineral surface, with a nominal thickness of 1/8 inch (3 mm).

Product in "Protection Course" Paragraph below describes Carlisle's "Protection Board V."

L. Protection Course: Fan folded, with a core of extruded-polystyrene board insulation, a nominal thickness of 1/4 inch (6 mm), and a compressive strength of not less than 8 psi (55 kPa).

2.3 MOLDED-SHEET DRAINAGE PANELS

Retain this article if molded-sheet drainage panels are required. Retain "Molded-Sheet Drainage Panel" Paragraph below if specifying molded-sheet drainage panels in another Section; revise to suit Project.

A. Molded-Sheet Drainage Panel: Comply with Section 334600 "Subdrainage."

Retain one or both molded-sheet drainage-panel paragraphs below if specifying molded-sheet drainage panels in this Section; revise to suit Project. If not shown on Drawings, insert thickness requirement only after coordinating required thickness with required flow rate.

Retain "Nonwoven-Geotextile-Faced, Molded-Sheet Drainage Panel" Paragraph below if required, usually for foundation walls. Option describes Carlisle's "CCW MiraDRAIN 6200" and "CCW MiraDRAIN 6200XL."

B. Nonwoven-Geotextile-Faced, Molded-Sheet Drainage Panel: Composite subsurface drainage panel consisting of a studded, nonbiodegradable, molded-plastic-sheet drainage core; with a nonwoven, needle-punched geotextile facing with an apparent opening size not exceeding No. 70 (0.21-mm) sieve laminated to one side of the core[ and a polymeric film bonded to the other side]; and with a vertical flow rate of 9 to 15 gpm per ft. (112 to 188 L/min. per m).

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1.  Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Carlisle Coatings & Waterproofing Inc.; [CCW MiraDRAIN 6000] [CCW MiraDRAIN 6000XL] [CCW MiraDRAIN 6200] [or] [CCW MiraDRAIN 6200XL].

b. <Insert manufacturer's name; product name or designation>.

Retain "Woven-Geotextile-Faced, Molded-Sheet Drainage Panel" Paragraph below if required, usually for plaza decks.

C. Woven-Geotextile-Faced, Molded-Sheet Drainage Panel: Composite subsurface drainage panels consisting of a studded, nonbiodegradable, molded-plastic-sheet drainage core; with a woven-geotextile facing with an apparent opening size not exceeding No. 40 (0.425-mm) sieve laminated to one side of the core; and with a horizontal flow rate not less than 2.8 gpm per ft. (35 L/min. per m).

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Carlisle Coatings & Waterproofing Inc.; [CCW MiraDRAIN 9000] [or] [CCW MiraDRAIN 9900].

b. <Insert manufacturer's name; product name or designation>.

2.4 INSULATION DRAINAGE PANELS

If not shown on Drawings, insert thickness requirement for insulation drainage panels.

In "Unfaced Wall-Insulation Drainage Panels" Paragraph below, DiversiFoam's "CertiFoam 25 SL Drainage Board" and Dow's "Styrofoam Perimate" are Type IV. DiversiFoam's "CertiFoam 40 (with channel edges) Drainage Board" is Type VI.

A. Unfaced Wall-Insulation Drainage Panels: Extruded-polystyrene board insulation complying with ASTM C 578, [Type IV, 25-psi (173-kPa)] [or] [Type VI, 40-psi (276-kPa)] minimum compressive strength; unfaced; fabricated with shiplap or channel edges and with one side having grooved drainage channels.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. DiversiFoam Products; [CertiFoam 25 SL] [or] [CertiFoam 40 (with channel edges)] Drainage Board.

b. Dow Chemical Company (The); Styrofoam Perimate.

c. <Insert manufacturer's name; product name or designation>.

In "Geotextile-Faced, Wall-Insulation Drainage Panels" Paragraph below, Owens Corning Insulating System's "Insul-Drain" and T. Clear's "Thermadry 750" are Type IV; T. Clear's "Thermadry 1250" is Type VI.

B. Geotextile-Faced, Wall-Insulation Drainage Panels: Extruded-polystyrene board insulation complying with ASTM C 578, [Type IV, 25-psi (173-kPa)] [or] [Type VI, 40-psi (276-kPa)] minimum compressive strength; fabricated with tongue-and-groove edges and with one side having grooved drainage channels faced with nonwoven geotextile filter fabric.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Owens Corning Insulating Systems LLC; Insul-Drain.

b. T. Clear Corporation, a subsidiary of Fin Pan Inc.; [Thermadry 750] [or] [Thermadry 1250].

c. <Insert manufacturer's name; product name or designation>.

In "Unfaced Plaza-Deck Insulation Drainage Panels" Paragraph below, Dow's "Styrofoam Ribbed Roofmate" and Owens Corning's "Foamular 404 RB" are Type VI; American Hydrotech's "Hydroguard" is also Type VI and has a cementitious surfacing for wear; DiversiFoam's "CertiFoam Plaza Deck" and Owens Corning's "Foamular 604 RB" are Type VII.

C. Unfaced Plaza-Deck Insulation Drainage Panels: Extruded-polystyrene board insulation complying with ASTM C 578, [Type VI, 40-psi (276-kPa)] [or] [Type VII, 60-psi (414-kPa)] minimum compressive strength; unfaced; fabricated with shiplapped, channel, or tongue-and-groove edges and with one side having ribbed drainage channels.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. American Hydrotech, Inc.; Hydroguard.

b. DiversiFoam Products; CertiFoam Plaza Deck.

c. Dow Chemical Company (The); Styrofoam Ribbed Roofmate.

d. Owens Corning Insulating Systems LLC; [Foamular 404 RB] [Foamular 604 RB].

e. <Insert manufacturer's name; product name or designation>.

D. Geotextile-Faced, Plaza-Deck Insulation Drainage Panels: Extruded-polystyrene board insulation complying with ASTM C 578, [Type VI, 40-psi (276-kPa)] [or] [Type VII, 60-psi (414-kPa)] minimum compressive strength; fabricated with tongue-and-groove edges and with one side having grooved drainage channels faced with manufacturer's standard, nonwoven geotextile filter fabric.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. T. Clear Corporation, a subsidiary of Fin Pan Inc.; [Thermadry 1250] [or] [Thermadry 1750].

b. <Insert manufacturer's name; product name or designation>.

PART 3 -  EXECUTION

3.1 FULLY ADHERED SHEET INSTALLATION

Retain this article for fully adhered horizontal or vertical installations.

A. Prepare surfaces and install fully adhered sheets over entire area to receive waterproofing according to manufacturer's written instructions and recommendations in ASTM D 5843.

B. Accurately align sheets and maintain uniform side and end laps of minimum dimensions required. Stagger end laps.

C. Apply bonding adhesive to substrates at required rate and allow it to partially dry.

D. Apply bonding adhesive to sheets and firmly adhere sheets to substrates. Do not apply bonding adhesive to splice area of sheet.

Retain first paragraph below if tie-ins to existing waterproofing are required.

E. Install fully adhered sheets and auxiliary materials to tie into existing waterproofing.

F. Repair tears, voids, and lapped seams in waterproofing that do not comply with requirements. Slit and flatten fishmouths and blisters. Patch with sheet waterproofing extending beyond repaired areas in all directions.

G. Horizontal Application: Apply sheets with side laps shingled with slope of deck where possible.

1. Spread sealant bed over deck drain flange at deck drains and securely seal sheet waterproofing in place with clamping ring.

3.2 PARTIALLY ADHERED SHEET INSTALLATION

Retain this article for partially adhered vertical installations.

A. Prepare surfaces and install partially adhered sheets over entire area to receive waterproofing according to manufacturer's written instructions.

B. Accurately align sheets and maintain uniform side and end laps of minimum dimensions required. Stagger end laps.

C. Apply bonding adhesive to the following areas of substrates and to each sheet at required rate and allow to partially dry:

Subparagraph below is based on Carlisle's recommendations for partially adhered EPDM and butyl sheets. Revise area to suit Project.

1. Upper 25 percent of length of each sheet and 18 inches (457 mm) around perimeter of each sheet.

D. Firmly adhere sheets to substrate. Do not apply bonding adhesive to splice area of sheet.

Retain first paragraph below if tie-ins to existing waterproofing are required.

E. Install partially adhered sheets and auxiliary materials to tie into existing waterproofing.

F. Repair tears, voids, and lapped seams in waterproofing that do not comply with requirements. Slit and flatten fishmouths and blisters. Patch with sheet waterproofing extending beyond repaired areas in all directions.

3.3 COMPARTMENTED, LOOSELY LAID SHEET INSTALLATION

Retain this article for compartmented, loosely laid, horizontal installations.

A. Prepare surfaces and install compartmented, loosely laid sheets over entire area to receive waterproofing according to manufacturer's written instructions.

B. Accurately align sheets and maintain uniform side and end laps of minimum dimensions required. Stagger end laps.

C. Apply continuous beads of water-cutoff mastic, of size recommended in writing by waterproofing manufacturer, to substrates in a 60-by-60-inch (1500-by-1500-mm) grid pattern before installing sheet.

D. Apply sheets with side laps shingled with slope of deck where possible.

E. Spread sealant bed over deck drain flange at deck drains and securely seal sheet waterproofing in place with clamping ring.

Retain first paragraph below if tie-ins to existing waterproofing are required.

F. Install compartmented, loosely laid sheets and auxiliary materials to tie into existing waterproofing.

G. Repair tears, voids, and lapped seams in waterproofing that do not comply with requirements. Slit and flatten fishmouths and blisters. Patch with sheet waterproofing extending beyond repaired areas in all directions.

3.4 SEAM INSTALLATION

Retain "Cement Splice" Paragraph below for cement splicing of EPDM or butyl sheet seams.

A. Cement Splice: Clean splice areas, apply splicing cement and in-seam sealant, and firmly roll side and end laps of overlapping sheets according to manufacturer's written instructions to produce a splice not less than 6 inches (150 mm) wide and to ensure a watertight seam installation. Apply lap sealant and seal edges of sheet terminations.

Retain "Cement and Tape Splice" Paragraph below for cement and butyl gum tape splicing of EPDM or butyl sheet seams.

B. Cement and Tape Splice: Clean splice areas, apply splicing cement and butyl gum tape, and firmly roll side and end laps of overlapping sheets according to manufacturer's written instructions to ensure a watertight seam installation. Apply lap sealant and seal edges of sheet terminations.

3.5 SHEET FLASHING INSTALLATION

A. Install sheet flashings and preformed flashing accessories and adhere to substrates according to waterproofing manufacturer's written instructions.

Retain one of first two paragraphs below; revise to suit Project.

B. Form wall flashings using exposed sheet flashing.

C. Extend deck sheet waterproofing to form wall flashings.

1. Flash penetrations and field-formed inside and outside corners with uncured sheet flashing.

2. Clean splice areas, apply splicing cement, and firmly roll side and end laps of overlapping sheets to ensure a watertight installation. Apply lap sealant and seal edges of sheet flashing terminations.

Verify with manufacturer that first paragraph below applies to Project for EPDM or butyl sheet; revise if required. Coordinate expansion-joint treatment with Section 079500 "Expansion Control." Specialty manufacturers such as Situra also produce membrane-type waterproofing expansion joints.

D. Cover expansion joints and discontinuous deck-to-wall or deck-to-deck joints by extending deck sheet waterproofing over joints.

E. Terminate and seal top of sheet flashings[ with mechanically anchored termination bars].

3.6 PROTECTION COURSE INSTALLATION

A. Install protection course over waterproofing membrane according to manufacturer's written instructions and before beginning subsequent construction operations. Minimize exposure of membrane.

Retain applicable options in subparagraph below if drainage panels are used and are permitted by waterproofing manufacturer to replace protection course.

1. [Molded-sheet drainage panels] [Insulation drainage panels] may be used in place of a separate protection course for vertical applications when approved by waterproofing manufacturer.

3.7 MOLDED-SHEET DRAINAGE-PANEL INSTALLATION

A. Place and secure molded-sheet drainage panels, with geotextile facing away from wall or deck substrate, according to manufacturer's written instructions. Use adhesives or other methods that do not penetrate waterproofing. Lap edges and ends of geotextile to maintain continuity. Protect installed molded-sheet drainage panels during subsequent construction.

Retain subparagraph below if protection course is installed before installing molded-sheet drainage panels.

1. For vertical applications, install protection course before installing drainage panels.

3.8 INSULATION DRAINAGE-PANEL INSTALLATION

A. Install insulation drainage panels over waterproofed surfaces. Cut and fit to within 3/4 inch (19 mm) of projections and penetrations.

B. Ensure that drainage channels are aligned and free of obstructions.

Retain first paragraph below if support is required during backfilling.

C. On vertical surfaces, set insulation drainage panels in adhesive or tape applied according to manufacturer's written instructions.

D. On horizontal surfaces, loosely lay insulation drainage panels according to manufacturer's written instructions. Stagger end joints and tightly abut insulation units.

3.9 PROTECTION, REPAIR, AND CLEANING

A. Do not permit foot or vehicular traffic on unprotected membrane.

B. Protect installed insulation drainage panels from damage due to UV light, harmful weather exposures, physical abuse, and other causes. Provide temporary coverings where insulation is subject to abuse and cannot be concealed and protected by permanent construction immediately after installation.

C. Correct deficiencies in or remove waterproofing that does not comply with requirements; repair substrates, reapply waterproofing, and repair sheet flashings.

D. Clean spillage and soiling from adjacent construction using cleaning agents and procedures recommended by manufacturer of affected construction.

END OF SECTION 071353

	ELASTOMERIC SHEET WATERPROOFING
	071353 - 1



