Copyright 2011 AIA
MasterSpec Professional
02/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 072500 - WEATHER BARRIERS
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

Revise subparagraphs below to suit Project.

1. Building paper.

2. Building wrap.

3. Flexible flashing.

1.2 ACTION SUBMITTALS

A. Product Data: For each type of product.

1.3 INFORMATIONAL SUBMITTALS

A. Evaluation Reports: For [water-resistive barrier] [and] [flexible flashing], from ICC-ES.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see SECTION 016000 "Product Requirements."

2.1 WATER-RESISTIVE BARRIER

Usually retain this article; a water-resistive barrier over sheathing is inexpensive and is required behind masonry veneers. Delete article if a water-resistive barrier will interfere with exterior insulation and finish systems or similar construction.

Retain one of two "Building Paper" paragraphs or "Building Wrap" Paragraph below.

A. Building Paper: ASTM D 226, Type 1 (No. 15 asphalt-saturated organic felt), unperforated.

Option in "Building Paper" Paragraph below is based on "Super Jumbo Tex 60 Minute" by Fortifiber.

B. Building Paper: Water-vapor-permeable, asphalt-saturated kraft building paper that complies with ICC-ES AC38, Grade D[; except with water-resistance rating not less than 1 hour].

Note that ASTM standard referenced in "Building Wrap" Paragraph below is for air barriers for low-rise buildings. This standard allows 15 times as much air infiltration as the limit for air barriers in the Massachusetts State Building Code.

C. Building Wrap: ASTM E 1677, Type I air barrier; with flame-spread and smoke-developed indexes of less than 25 and 450, respectively, when tested according to ASTM E 84; UV stabilized; and acceptable to authorities having jurisdiction.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Dow Chemical Company (The); Styrofoam Weathermate Plus Brand Housewrap.

b. DuPont (E. I. du Pont de Nemours and Company); Tyvek [CommercialWrap] [StuccoWrap] [HomeWrap] [HomeWrap and HeaderWrap].

c. Ludlow Coated Products; [Air Stop Housewrap] [Barricade Building Wrap] [EnergyWrap Housewrap] [R-Wrap Protective House Wrap].

d. Pactiv, Inc.; GreenGuard [Classic Wrap] [RainDrop] [Ultra Wrap] [Value Wrap].

e. Raven Industries Inc.; Fortress Pro Weather Protective Barrier.

f. Reemay, Inc.; Typar HouseWrap.

g. <Insert manufacturer's name; product name or designation>.

Coordinate permeance value retained or inserted in "Water-Vapor Permeance" Subparagraph below with products retained. Consult manufacturers' literature.

2. Water-Vapor Permeance: Not less than [50] <Insert number> g through 1 sq. m of surface in 24 hours per ASTM E 96/E 96M, Desiccant Method (Procedure A).

D. Building-Wrap Tape: Pressure-sensitive plastic tape recommended by building-wrap manufacturer for sealing joints and penetrations in building wrap.

2.2 MISCELLANEOUS MATERIALS

A. Flexible Flashing: Self-adhesive [butyl rubber] [or] [rubberized-asphalt] compound, bonded to a high-density polyethylene film, aluminum foil, or spunbonded polyolefin to produce an overall thickness of not less than 0.025 inch (0.6 mm).

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

Products in first four subparagraphs below are butyl rubber products.

a. DuPont (E. I. du Pont de Nemours and Company); DuPont Flashing Tape.

b. Grace Construction Products, a unit of W. R. Grace & Co. - Conn.; Vycor Butyl Self Adhered Flashing.

c. Protecto Wrap Company; BT-25 XL.

d. Raven Industries Inc.; Fortress Flashshield.

Products in subparagraphs below are rubberized asphalt products.

e. Advanced Building Products Inc.; Wind-o-wrap.

f. Carlisle Coatings & Waterproofing; CCW-705-TWF Thru-Wall Flashing.

g. Fiberweb, Clark Hammerbeam Corp.; Aquaflash 500.

h. Fortifiber Building Systems Group; [Fortiflash 25] [Fortiflash 40].

i. Grace Construction Products, a unit of W. R. Grace & Co. - Conn.; [Vycor Plus Self-Adhered Flashing] [Vycor V40 Self-Adhered Flashing].

j. MFM Building Products Corp.; Window Wrap.

k. Polyguard Products, Inc.; [Polyguard JT-20 Tape] [Polyguard JT-30 Tape].

l. Sandell Manufacturing Co., Inc.; Presto-Seal.

m. <Insert manufacturer's name; product name or designation>.

PART 3 -  EXECUTION

3.1 WATER-RESISTIVE BARRIER INSTALLATION

A. Cover sheathing with water-resistive barrier as follows:

1. Cut back barrier 1/2 inch (13 mm) on each side of the break in supporting members at expansion- or control-joint locations.

2. Apply barrier to cover vertical flashing with a minimum 4-inch (100-mm) overlap unless otherwise indicated.

Retain "Building Paper" or "Building Wrap" Paragraph below to correspond with products retained in Part 2.

B. Building Paper: Apply horizontally with a 2-inch (50-mm) overlap and a 6-inch (150-mm) end lap; fasten to sheathing with galvanized staples or roofing nails.

C. Building Wrap: Comply with manufacturer's written instructions.

1. Seal seams, edges, fasteners, and penetrations with tape.

2. Extend into jambs of openings and seal corners with tape.

3.2 FLEXIBLE FLASHING INSTALLATION

A. Apply flexible flashing where indicated to comply with manufacturer's written instructions.

1. Lap seams and junctures with other materials at least 4 inches (100 mm) except that at flashing flanges of other construction, laps need not exceed flange width.

2. Lap flashing over water-resistive barrier at bottom and sides of openings.

Retain subparagraph below if head flashing is used; see Evaluations.

3. Lap water-resistive barrier over flashing at heads of openings.

END OF SECTION 072500

	WEATHER BARRIERS
	072500 - 1



