Copyright 2012 AIA
MasterSpec Professional
02/12

Copyright 2012 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 092116.23 - GYPSUM BOARD SHAFT WALL ASSEMBLIES
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes: Gypsum board shaft wall assemblies.

1.2 ACTION SUBMITTALS

A. Product Data: For each component of gypsum board shaft wall assembly.

B. LEED Submittals:

1. Product Data for Credit MR 4: For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content. Include statement indicating cost for each product having recycled content.

"Product Certificates for Credit MR 5" Subparagraph below applies to LEED-NC, LEED-CS, and LEED for Schools.

2. Product Certificates for Credit MR 5: For products and materials required to comply with requirements for regional materials, certificates indicating location of material manufacturer and point of extraction, harvest, or recovery for each raw material. Include statement indicating distance to Project, cost for each regional material, and fraction by weight that is considered regional.

"Product Certificates for Credit MR 5" Subparagraph below applies to LEED-CI. Retain option for Credit MR 5, Option 2.

3. Product Certificates for Credit MR 5: For products and materials required to comply with requirements for regionally manufactured[ and regionally extracted and manufactured] materials. Include statement indicating cost for each regionally manufactured material.

First subparagraph below applies to LEED-CI Credit MR 5, Option 1 and Option 2.

a. Include statement indicating location of manufacturer and distance to Project for each regionally manufactured material.

First subparagraph below applies to LEED-CI Credit MR 5, Option 2.

b. Include statement indicating location of manufacturer and point of extraction, harvest, or recovery for each raw material used in regionally extracted and manufactured materials. Indicate distance to Project and fraction by weight of each regionally manufactured material that is regionally extracted.

"Laboratory Test Reports for Credit EQ 4" Subparagraph below applies to LEED for Schools.

4. Laboratory Test Reports for Credit EQ 4: For gypsum board shaft wall systems, documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 PERFORMANCE REQUIREMENTS

Indicate fire-resistance ratings of specific assemblies on Drawings or in "Gypsum Board Shaft Wall Assemblies" Article.

A. Fire-Resistance-Rated Assemblies: For fire-resistance-rated assemblies, provide materials and construction identical to those tested in assembly indicated according to ASTM E 119 by an independent testing agency.

Retain "STC-Rated Assemblies" Paragraph below if shaft wall is part of STC-rated assemblies. Indicate design designations of specific assemblies on Drawings.

B. STC-Rated Assemblies: Provide materials and construction identical to those of assemblies tested according to ASTM E 90 and classified according to ASTM E 413 by a testing and inspecting agency.

Retain "Low-Emitting Materials" Paragraph below if required for LEED for Schools.

C. Low-Emitting Materials: Gypsum shaft wall assemblies shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

2.2 GYPSUM BOARD SHAFT WALL ASSEMBLIES <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation. Use these designations on Drawings to identify each product.

A. Fire-Resistance Rating: [As indicated] [1 hour] [2 hours] [3 hours] [4 hours] <Insert rating>.

Retain "STC Rating" Paragraph below if required to reduce airborne sound transmission.

B. STC Rating: [As indicated] [51, minimum] <Insert rating>.

C. Studs: Manufacturer's standard profile for repetitive members, corner and end members, and fire-resistance-rated assembly indicated.

1. Depth: [As indicated] [2-1/2 inches (64 mm)] [4 inches (102 mm)] [6 inches (152 mm)].

Second option in "Minimum Base-Metal Thickness" Subparagraph below corresponds to 25 gage; third option corresponds to 20 gage.

2. Minimum Base-Metal Thickness: [As indicated] [0.018 inch (0.45 mm)] [0.033 inch (0.84 mm)] <Insert value>.

D. Runner Tracks: Manufacturer's standard J-profile track with manufacturer's standard long-leg length, but at least 2 inches (51 mm) long and matching studs in depth.

Third option in "Minimum Base-Metal Thickness" Subparagraph below corresponds to 25 gage; fourth option corresponds to 24 gage; fifth option corresponds to 20 gage.

1. Minimum Base-Metal Thickness: [As indicated] [Matching steel studs] [0.018 inch (0.45 mm)] [0.021 inch (0.53 mm)] [0.033 inch (0.84 mm)] <Insert value>.

Retain "Firestop Tracks" Paragraph below if required.

E. Firestop Tracks: Provide firestop track at head of shaft wall on each floor level.

F. Elevator Hoistway Entrances: Manufacturer's standard J-profile jamb strut with long-leg length of 3 inches (76 mm), matching studs in depth.

Retain "Room-Side Finish" and "Shaft-Side Finish" paragraphs below or delete and show room- and shaft-side finishes on Drawings.

G. Room-Side Finish: [As indicated] [Gypsum board] [Gypsum veneer plaster] [Cementitious backer units] <Insert finish>.

H. Shaft-Side Finish: [As indicated] [Gypsum shaftliner board, Type X] [Gypsum shaftliner board, moisture- and mold-resistant Type X] [As indicated by fire-resistance-rated assembly design designation] <Insert finish>.

I. Insulation: Sound attenuation blankets.

2.3 PANEL PRODUCTS

Retain "Recycled Content of Gypsum Panel Products" Paragraph below to specify recycled content if applying for LEED Credit MR 4. An alternative method of dealing with these credit requirements is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.16 "Sustainable Design Requirements - LEED for Commercial Interiors," Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development," Section 018113.23 "Sustainable Design Requirements - LEED for Schools" that gives Contractor the option and responsibility to determine how these credit requirements will be met.

A. Recycled Content of Gypsum Panel Products: Postconsumer recycled content plus one-half of preconsumer recycled content not less than <Insert number> percent by weight.

Retain first "Regional Materials" Paragraph below for LEED-NC, LEED-CS, and LEED for Schools Credit MR 5 and LEED-CI Credit MR 5, Option 2; before retaining, verify availability of materials that comply.

B. Regional Materials: Gypsum panel products shall be manufactured within 500 miles (800 km) of Project site from materials that have been extracted, harvested, or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

Retain "Regional Materials" Paragraph below for LEED-CI Credit MR 5, Option 1; before retaining, verify availability of materials that comply.

C. Regional Materials: Gypsum panel products shall be manufactured within 500 miles (800 km) of Project site.

D. Panel Size: Provide in maximum lengths and widths available that will minimize joints in each area and that correspond with support system indicated.

E. Gypsum Shaftliner Board, Type X: ASTM C 1396/C 1396M; manufacturer's proprietary fire-resistive liner panels with paper faces.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. American Gypsum; Shaft Liner.

b. CertainTeed Corp.; ProRoc Shaftliner.

c. Georgia-Pacific Gypsum LLC, Subsidiary of Georgia Pacific; ToughRock Fireguard Shaftliner.

d. Lafarge North America, Inc.; Firecheck Type X Shaftliner.

e. National Gypsum Company; Gold Bond Brand Fire-Shield Shaftliner.

f. PABCO Gypsum; Pabcore Shaftliner Type X.

g. Temple-Inland Inc.; Fire-Rated SilentGuard Gypsum Shaftliner System.

h. USG Corporation; Sheetrock Brand Gypsum Liner Panel.

i. <Insert manufacturer's name; product name or designation>.

2. Thickness: 1 inch (25.4 mm).

3. Long Edges: Double bevel.

F. Gypsum Shaftliner Board, Moisture- and Mold-Resistant Type X: ASTM C 1396/C 1396M; manufacturer's proprietary fire-resistive liner panels with moisture- and mold-resistant core and surfaces.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. CertainTeed Corp.; ProRoc Moisture and Mold Resistant Shaftliner.

b. Georgia-Pacific Gypsum LLC, Subsidiary of Georgia Pacific; Dens-Glass Ultra Shaftliner.

c. Lafarge North America, Inc.; Firecheck Moldcheck Type X Shaftliner.

d. National Gypsum Company; Gold Bond Brand Fire-Shield Shaftliner XP.

e. PABCO Gypsum; Pabcore Mold Curb Shaftliner Type X.

f. Temple-Inland Inc.; Fire-Rated SilentGuard TS Mold-Resistant Gypsum Shaftliner System.

g. USG Corporation; Sheetrock Brand Mold Tough Gypsum Liner Panel.

h. <Insert manufacturer's name; product name or designation>.

2. Thickness: 1 inch (25.4 mm).

3. Long Edges: Double bevel.

4. Mold Resistance: ASTM D 3273, score of 10 as rated according to ASTM D 3274.

Retain "Gypsum Board" Paragraph below if exposed surfaces of shaft walls or backing panels of multilayer applications are gypsum board.

G. Gypsum Board: As specified in Section 092900 "Gypsum Board."

2.4 NON-LOAD-BEARING STEEL FRAMING

Retain "Recycled Content of Steel" Paragraph below if required for LEED.

A. Recycled Content of Steel: Postconsumer recycled content plus one-half of preconsumer recycled content not less than [25] <Insert number> percent.

Steel framing complies with ASTM C 645 for material thickness; stud type and size do not apply.

B. Steel Framing Members: Comply with ASTM C 645 requirements for metal.

C. Firestop Tracks: Top runner manufactured to allow partition heads to expand and contract with movement of the structure while maintaining continuity of fire-resistance-rated assembly indicated.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Fire Trak Corp.; Fire Trak System[ attached to studs with Fire Trak Posi Klip].

b. Grace Construction Products; FlameSafe FlowTrak System.

c. Metal-Lite, Inc.; The System.

d. Steel Network Inc. (The); [VertiClip SLD] [VertiTrack VTD] Series.

e. <Insert manufacturer's name; product name or designation>.

2.5 AUXILIARY MATERIALS

A. Trim Accessories: Material and shapes as specified in [Section 092900 "Gypsum Board"] [Section 092613 "Gypsum Veneer Plastering"] that comply with gypsum board shaft wall assembly manufacturer's written recommendations for application indicated.

B. Steel Drill Screws: ASTM C 1002 unless otherwise indicated.

C. Track Fasteners: Power-driven fasteners of size and material required to withstand loading conditions.

D. Sound Attenuation Blankets: As specified in [Section 092900 "Gypsum Board."] [Section 092613 "Gypsum Veneer Plastering."]

E. Acoustical Sealant: As specified in [Section 092900 "Gypsum Board."] [Section 092613 "Gypsum Veneer Plastering."]

PART 3 -  EXECUTION

3.1 INSTALLATION

A. General: Comply with requirements of fire-resistance-rated assemblies indicated, manufacturer's written installation instructions, and ASTM C 754 other than stud-spacing requirements.

B. Examine panels before installation. Reject panels that are wet, moisture damaged, or mold damaged.

C. Sprayed Fire-Resistive Materials: Patch or replace sprayed fire-resistive materials removed or damaged during installation of shaft wall assemblies. After application, remove only to extent necessary for installation of gypsum board shaft wall assemblies.

D. Building Expansion Joints: Frame both sides of expansion joints with furring and other support.

E. Install supplementary framing around openings and as required for blocking, bracing, and support of gravity and pullout loads of fixtures, equipment, handrails, and similar items.

1. Elevator Hoistway: Provide jamb struts on each side of door frame.

F. Penetrations: Install supplementary steel framing around perimeter of penetration behind boxes containing wiring devices, elevator call buttons, elevator floor indicators, and similar items.

G. Isolate perimeter of gypsum panels from building structure, while maintaining continuity of fire-rated construction.

H. Firestop Tracks: Install to maintain continuity of fire-resistance-rated assembly indicated.

I. Control Joints: Install control joints [at locations indicated on Drawings] [according to ASTM C 840 and in specific locations approved by Architect] while maintaining fire-resistance rating of gypsum board shaft wall assemblies.

J. Sound-Rated Shaft Wall Assemblies: Seal with acoustical sealant at perimeter of each assembly and at joints and penetrations.

Delete "Cant Panels" Paragraph below if no projections or if cants are specified in Section 055000 "Metal Fabrications."

K. Cant Panels: At projections into shaft exceeding 4 inches (102 mm), install 1/2- or 5/8-inch- (13- or 16-mm-) thick gypsum board cants covering tops of projections.

L. Installation Tolerance: Install each framing member so fastening surfaces vary not more than 1/8 inch (3 mm) from the plane formed by faces of adjacent framing.

M. Remove and replace panels that are wet, moisture damaged, or mold damaged.

END OF SECTION 092116.23

	GYPSUM BOARD SHAFT WALL ASSEMBLIES
	092116.23 - 1



