Copyright 2011 AIA
MasterSpec Professional
02/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 096816 - SHEET CARPETING
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section includes [tufted] [and] [woven] <Insert carpet construction> carpet[ and carpet cushion].

1.2 PREINSTALLATION MEETINGS

A. Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

1.3 ACTION SUBMITTALS

A. Product Data: For each type of product.

B. LEED Submittals:

"Product Data for Credit EQ 4.3" Subparagraph below applies to LEED-NC, LEED-CS, or LEED-CI; coordinate with requirements selected in Part 2 for carpet, carpet cushion, and adhesives.

1. Product Data for Credit EQ 4.3:

a. For carpet, documentation indicating compliance with testing and product requirements of CRI's "Green Label Plus" program.

b. For carpet cushion, documentation indicating compliance with testing and product requirements of CRI's "Green Label" program.

c. For installation adhesive, including printed statement of VOC content.

"Laboratory Test Reports for Credit EQ 4" Subparagraph below applies to LEED for Schools.

2. Laboratory Test Reports for Credit EQ 4: For carpet[ and installation adhesives], documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

C. Shop Drawings: Show the following:

Retain, delete, or revise subparagraphs below to suit Project.

1. Columns, doorways, enclosing walls or partitions, built-in cabinets, and locations where cutouts are required in carpet.

2. Carpet type, color, and dye lot.

3. Seam locations, types, and methods.

4. Pile direction.

"Samples" Paragraph below assumes manufacturer's standard-size Samples are acceptable. Revise to suit Project.

D. Samples: For each exposed product and for each color and texture specified.

Retain "Sustainability" Paragraph below only if verification is available from manufacturer.

E. Sustainability: Provide the Statement of the Achievement Level the carpet has attained for [Bronze, 28 to 36] [Silver, 37 to 51] [Gold, 52 to 70] points, based on specific Sustainable Attribute Performance for all product stages according to ANSI/NSF 140.

1.4 INFORMATIONAL SUBMITTALS

A. Product test reports.

B. Warrant: Sample of special warranty.

1.5 CLOSEOUT SUBMITTALS

A. Maintenance data.

1.6 QUALITY ASSURANCE

A. Installer Qualifications: An experienced Installer who is certified by the International Certified Floorcovering Installers Association at the [Commercial II] [Master II] <Insert description> certification level.

B. Fire-Test-Response Ratings: Where indicated, provide carpet[ and carpet cushion] identical to those of assemblies tested for fire response per NFPA 253 by a qualified testing agency.

1.7 DELIVERY, STORAGE, AND HANDLING

A. Comply with CRI 104.

1.8 FIELD CONDITIONS

A. Comply with CRI 104 for temperature, humidity, and ventilation limitations.

1.9 WARRANTY

Revise "Special Warranty for Carpet" Paragraph below if manufacturers have separate warranties for various characteristics.

A. Special Warranty for Carpet: Manufacturer agrees to repair or replace components of carpet installation that fail in materials or workmanship within specified warranty period.

1. Warranty does not include deterioration or failure of carpet due to unusual traffic, failure of substrate, vandalism, or abuse.

2. Failures include, but are not limited to, more than 10 percent loss of face fiber, edge raveling, snags, runs, [loss of tuft bind strength,] [excess static discharge,] <Insert failure characteristic> and delamination.

Verify available warranties and warranty periods for carpet.

3. Warranty Period: [10] <Insert number> years from date of Substantial Completion.

B. Special Warranty for Carpet Cushion: Manufacturer agrees to repair or replace components of carpet cushion installation that fail in materials or workmanship within specified warranty period.

1. Warranty includes consequent removal and replacement of carpet and accessories.

2. Warranty does not include deterioration or failure of carpet cushion due to unusual traffic, failure of substrate, vandalism, or abuse.

3. Failure includes, but is not limited to, permanent indentation or compression.

Verify available warranties and warranty periods for carpet cushion.

4. Warranty Period: [10] <Insert number> years from date of Substantial Completion.

PART 2 -  PRODUCTS

2.1 TUFTED CARPET <Insert designation>

Revise article title above if fusion-bonded, needle-punched, knitted, or another carpet construction is required to suit Project.

Copy this article and re-edit for each product.

Insert number to complete drawing designation. Use these designations on Drawings to identify each product.

Retain "Products" Paragraph and add list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

A. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

For competitive bidding, copy subparagraph below and repeat requirements for each additional product.

1. <Insert manufacturer's name; product name or designation>.

Retain "Basis-of-Design Product" Paragraph and add list of manufacturers below to identify a specific product or a comparable product from manufacturers listed. Retain option and delete insert note if manufacturer's or carpet supplier's name and product name or designation are indicated on Drawings.

B. Basis-of-Design Product: Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's or carpet supplier's name; product name or designation> or comparable product by one of the following:

1. <Insert manufacturers' names>.

C. Color: [Match Architect's samples] [As selected by Architect from manufacturer's full range] <Insert color>.

D. Pattern: [Match Architect's samples] <Insert pattern>.

Retain remainder of this article unless products are limited to those listed above.

E. Fiber Content: [100 percent nylon 6, 6] [100 percent nylon 6] [100 percent polypropylene] <Insert fiber and content by percentage>.

Retain "Fiber Type" Paragraph below and insert proprietary fiber type such as Antron, Ultron, or Zeftron if required.

F. Fiber Type: <Insert proprietary fiber type>.

G. Pile Characteristic: [Level-loop] [Cut] [Cut-and-loop] [Multilevel-loop] [Level tip shear] [Random shear] [Frieze] [Sculptured] <Insert characteristic> pile.

H. Yarn Twist: <Insert twist in TPI (TPCM)>.

I. Yarn Count: <Insert yarn count>.

J. Density: <Insert oz./cu. yd. (g/cu. cm)>.

K. Pile Thickness: <Insert inches (mm)> for finished carpet[ per ASTM D 6859].

L. Stitches: <Insert stitches per inch (mm)>.

M. Gage: <Insert gage in ends per inch (mm)>.

N. Face Weight: <Insert oz./sq. yd. (g/sq. m)>.

O. Total Weight: <Insert oz./sq. yd. (g/sq. m)> for finished carpet.

Retain one or more of the first three paragraphs below if describing backing construction instead of naming a proprietary backing system.

P. Primary Backing: [Manufacturer's standard material] [Woven polypropylene] [Nonwoven, polypropylene or polyester] <Insert specific primary backing material>.

Q. Secondary Backing: [Manufacturer's standard material] [Woven polypropylene] [Nonwoven, polypropylene or polyester] [Woven jute] [Fiberglass] <Insert specific secondary backing material>.

R. Backcoating: [Manufacturer's standard material] [SBR latex] [PVC] [Thermoplastic copolymer] <Insert backcoating; consult manufacturers>.

Retain "Backing System" Paragraph below if naming a proprietary backing system, such as "ActionBac."

S. Backing System: <Insert proprietary name>.

T. Width: [12 feet (3.7 m)] [6 feet (1.8 m)] [13.5 feet (4.1 m)] [15 feet (4.6 m)] <Insert dimension>.

U. Applied Soil-Resistance Treatment: [Manufacturer's standard material] <Insert treatment>.

V. Antimicrobial Treatment: [Manufacturer's standard material] <Insert treatment>.

If specifying compliance with ANSI/NSF 140, some of the following performance characteristics are also in the appendix of the standard.

W. Performance Characteristics: As follows:

1. Appearance Retention Rating: [Moderate traffic, 2.5] [Heavy traffic, 3.0] [Severe traffic, 3.5] <Insert number> minimum per ASTM D 7330.

2. Critical Radiant Flux Classification: Not less than [0.45 W/sq. cm] [0.22 W/sq. cm].

3. Dry Breaking Strength: Not less than 100 lbf (445 N) per ASTM D 2646.

4. Tuft Bind: Not less than [3 lbf (13 N)] [5 lbf (22 N)] [6.2 lbf (28 N)] [8 lbf (36 N)] [10 lbf (45 N)] <Insert value> per ASTM D 1335.

5. Delamination: Not less than [2.5 lbf/in. (12 N/mm)] [3.5 lbf/in. (15 N/mm)] [4 lbf/in. (18 N/mm)] <Insert value> per ASTM D 3936.

6. Resistance to Insects: Comply with AATCC 24.

7. Colorfastness to Crocking: Not less than 4, wet and dry, per AATCC 165.

8. Colorfastness to Light: Not less than 4 after [40] [60] <Insert number> AFU (AATCC fading units) per AATCC 16, Option E.

9. Antimicrobial Activity: Not less than 2-mm halo of inhibition for gram-positive bacteria; not less than 1-mm halo of inhibition for gram-negative bacteria; no fungal growth; per AATCC 174.

10. Electrostatic Propensity: Less than [3.5] [2] <Insert number> kV per AATCC 134.

Retain "Emissions" Subparagraph below if required for LEED-NC, LEED-CS, or LEED-CI Credit EQ 4.3.

11. Emissions: Provide carpet that complies with testing and product requirements of CRI's "Green Label Plus" program.

Retain "Emissions" Subparagraph below if required for LEED for Schools.

12. Emissions: Provide carpet that complies with the product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

Insert other performance characteristics to suit Project, such as smoke density, texture retention, additional colorfastness characteristics, or quantification of soil-resistance treatment.

2.2 WOVEN CARPET <Insert designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation. Use these designations on Drawings to identify each product.

Retain "Products" Paragraph and add list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

A. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

For competitive bidding, copy subparagraph below and repeat requirements for each additional product.

1. <Insert manufacturer's name; product name or designation>.

Retain "Basis-of-Design Product" Paragraph and add list of manufacturers below to identify a specific product or a comparable product from manufacturers listed. Retain option and delete insert note if manufacturer's or carpet supplier's name and product name or designation are indicated on Drawings.

B. Basis-of-Design Product: Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's or carpet supplier's name; product name or designation> or comparable product by one of the following:

1. <Insert manufacturers' names>.

C. Color: [Match Architect's samples] [As selected by Architect from manufacturer's full range] <Insert color>.

D. Pattern: [Match Architect's samples] <Insert pattern>.

Retain remainder of this article unless products are limited to those listed above.

E. Fiber Content: [100 percent wool] [80 percent wool; 20 percent nylon 6, 6] [80 percent wool; 20 percent nylon 6] <Insert fiber and content by percentage>.

1. Document that [5 to 20] [85 to 100] <Insert number> percent of the material feedstock for carpet is composed of biobased or recycled materials according to ANSI/NSF 140.

F. Face Construction: [Axminster] [Wilton] [Velvet] <Insert construction>.

G. Pile Characteristic: [Level-loop] [Cut] [Cut-and-loop] pile.

H. Yarn Twist: <Insert twist in TPI (TPCM)>.

I. Yarn Count: <Insert yarn count>.

J. Density: <Insert oz./cu. yd. (g/cu. cm)>.

K. Pile Thickness: <Insert inches (mm)> for finished carpet[ per ASTM D 6859].

L. Rows: <Insert number of lengthwise tufts per inch (mm)>.

M. Pitch: <Insert number of rows in 27 inches (686 mm)>.

N. Face Weight: <Insert oz./sq. yd. (g/sq. m)>.

O. Total Weight: <Insert oz./sq. yd. (g/sq. m)> for finished carpet.

P. Backing: [Manufacturer's standard.] [As follows:]

1. Chain Warp: <Insert material>.

2. Stuffer Warp: <Insert material>.

3. Shot or Fill Weft: <Insert material>.

4. Backcoating: <Insert backcoating>.

Q. Applied Soil-Resistance Treatment: [Manufacturer's standard material] <Insert treatment>.

R. Antimicrobial Treatment: [Manufacturer's standard material] <Insert treatment>.

S. Performance Characteristics: As follows:

1. Appearance Retention Rating: [Moderate traffic, 2.5] [Heavy traffic, 3.0] [Severe traffic, 3.5] <Insert number> minimum per ASTM D 7330.

2. Critical Radiant Flux Classification: Not less than [0.45 W/sq. cm] [0.22 W/sq. cm].

3. Dry Breaking Strength: Not less than 100 lbf (445 N) per ASTM D 2646.

4. Resistance to Insects: Comply with AATCC 24.

5. Colorfastness to Crocking: Not less than 4, wet and dry, per AATCC 165.

6. Colorfastness to Light: Not less than 4 after [40] [60] <Insert number> AFU (AATCC fading units) per AATCC 16, Option E.

7. Electrostatic Propensity: Less than [3.5] [2] <Insert number> kV per AATCC 134.

Retain "Emissions" Subparagraph below if required for LEED-NC, LEED-CS, or LEED-CI Credit EQ 4.3.

8. Emissions: Provide carpet that complies with testing and product requirements of CRI's "Green Label Plus" program.

Retain "Emissions" Subparagraph below if required for LEED for Schools.

9. Emissions: Provide carpet that complies with the product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

Insert other performance characteristics to suit Project, such as smoke density, additional colorfastness characteristics, or quantification of soil-resistance treatment.

2.3 CARPET CUSHION <Insert designation>

Retain "Manufacturers" Paragraph and add list of manufacturers below to require specific products from manufacturers listed or a comparable product from other manufacturers.

A. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

Retain "Basis-of-Design Product" Paragraph and add list of manufacturers below to identify a specific product or a comparable product from manufacturers listed. Retain option and delete insert note if manufacturer's or carpet cushion supplier's name and product name or designation are indicated on Drawings.

B. Basis-of-Design Product: Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

1. <Insert manufacturers' names>.

C. Traffic Classification: CCC [Class I, moderate] [Class II, heavy] [Class III, extra-heavy] traffic.

D. Fiber Cushion: [Rubberized hair, mothproofed and sterilized] [Rubberized jute, mothproofed and sterilized] [Synthetic] [Resinated, recycled textile].

1. Weight: <Insert oz./sq. yd. (g/sq. m)>.

2. Thickness: <Insert inches (mm)> plus 5 percent maximum.

3. Density: <Insert lb/cu. ft. (kg/cu. m)>.

E. Rubber Cushion: [Flat] [Rippled waffle] [Textured flat] [Reinforced].

1. Weight: <Insert oz./sq. yd. (g/sq. m)>.

2. Thickness: <Insert inches (mm)> plus 5 percent maximum.

3. Compression Resistance: <Insert lb/sq. in. (kg/sq. mm)> at [25] [65] percent per ASTM D 3676.

4. Density: <Insert lb/cu. ft. (kg/cu. m)>.

F. Polyurethane-Foam Cushion: [Grafted prime] [Densified] [Bonded] [Mechanically frothed].

1. Compression Force Deflection at 65 Percent: <Insert lb/sq. in. (kg/sq. mm) of polymer density> per ASTM D 3574.

2. Thickness: <Insert inches (mm)>.

3. Density: <Insert lb/cu. ft. (kg/cu. m)>.

G. Performance Characteristics: As follows:

1. Critical Radiant Flux Classification: Not less than [0.45 W/sq. cm] [0.22 W/sq. cm].

Retain "Noise Reduction Coefficient (NRC)" Subparagraph below if required. Revise if Impact Insulation Class is available and is required to suit Project.

2. Noise Reduction Coefficient (NRC): <Insert NRC> per ASTM C 423.

Retain "Emissions" Subparagraph below if required for LEED-NC, LEED-CS, or LEED-CI Credit EQ 4.3.

3. Emissions: Provide carpet cushion that complies with testing and product requirements of CRI's "Green Label" program.

Retain "Emissions" Subparagraph below if required for LEED for Schools.

4. Emissions: Provide carpet cushion that complies with the product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

2.4 INSTALLATION ACCESSORIES

A. Trowelable Leveling and Patching Compounds: Latex-modified, hydraulic-cement-based formulation provided or recommended by carpet[ cushion] manufacturer.

B. Adhesives: Water-resistant, mildew-resistant, nonstaining type to suit products and subfloor conditions indicated, that complies with flammability requirements for installed carpet and is recommended or provided by [carpet manufacturer] [carpet and carpet cushion manufacturers].

Retain first subparagraph below if required for LEED-NC, LEED-CS, or LEED-CI Credit EQ 4.3.

1. Use adhesives with VOC content not more than 50 g/L when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

Retain subparagraph below if required for LEED for Schools.

2. Use adhesives that comply with the product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

C. Tackless Carpet Stripping: Water-resistant plywood, in strips as required to match cushion thickness and that comply with CRI 104, Section 12.2.

D. Seam Adhesive: Hot-melt adhesive tape or similar product recommended by carpet manufacturer for sealing and taping seams and butting cut edges at backing to form secure seams and to prevent pile loss at seams.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. Examine substrates, areas, and conditions, with Installer present, for compliance with requirements for maximum moisture content, alkalinity range, installation tolerances, and other conditions affecting carpet performance. Examine carpet for type, color, pattern, and potential defects.

B. Concrete Subfloors: Verify that concrete slabs comply with ASTM F 710.

C. Proceed with installation only after unsatisfactory conditions have been corrected.

D. Preparation: Comply with CRI 104, Section 7.3, "Site Conditions; Floor Preparation," and with carpet manufacturer's written installation instructions for preparing substrates.

E. Installation: Comply with CRI 104 and [carpet manufacturer's] [carpet and carpet cushion manufacturers'] written installation instructions for the following:

1. Direct-Glue-Down Installation: Comply with CRI 104, Section 9, "Direct Glue-Down Installation."

2. Double-Glue-Down Installation: Comply with CRI 104, Section 10, "Double-Glue-Down Installation."

3. Carpet with Attached-Cushion Installation: Comply with CRI 104, Section 11, "Attached-Cushion Installations."

4. Preapplied Adhesive Installation: Comply with CRI 104, Section 11.4, "Pre-Applied Adhesive Systems (Peel and Stick)."

5. Hook-and-Loop Installation: Comply with CRI 104, Section 11.5, "Hook and Loop Technology."

6. Stretch-in Installation: Comply with CRI 104, Section 12, "Stretch-in Installations."

7. Stair Installation: Comply with CRI 104, Section 13, "Carpet on Stairs" for [stretch-in] [glue-down] installation.

F. Comply with carpet manufacturer's written recommendations and Shop Drawings for seam locations and direction of carpet; maintain uniformity of carpet direction and lay of pile. At doorways, center seams under the door in closed position.

G. Do not bridge building expansion joints with carpet.

H. Cut and fit carpet to butt tightly to vertical surfaces, permanent fixtures, and built-in furniture including cabinets, pipes, outlets, edgings, thresholds, and nosings. Bind or seal cut edges as recommended by carpet manufacturer.

I. Extend carpet into toe spaces, door reveals, closets, open-bottomed obstructions, removable flanges, alcoves, and similar openings.

J. Maintain reference markers, holes, and openings that are in place or marked for future cutting by repeating on finish flooring as marked on subfloor. Use nonpermanent, nonstaining marking device.

Retain first paragraph below if carpet has pattern.

K. Install pattern parallel to walls and borders to comply with CRI 104, Section 15, "Patterned Carpet Installations" and with carpet manufacturer's written recommendations.

Retain option in first paragraph below for stretch-in installations.

L. Comply with carpet cushion manufacturer's written recommendations.[ Install carpet cushion seams at 90-degree angle with carpet seams.]

M. Perform the following operations immediately after installing carpet:

1. Remove excess adhesive, seam sealer, and other surface blemishes using cleaner recommended by carpet manufacturer.

2. Remove yarns that protrude from carpet surface.

3. Vacuum carpet using commercial machine with face-beater element.

N. Protect installed carpet to comply with CRI 104, Section 16, "Protecting Indoor Installations."

END OF SECTION 096816

	SHEET CARPETING
	096816 - 1



