Copyright 2010 AIA
MasterSpec Professional
02/10

Copyright 2010 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 123619 - WOOD COUNTERTOPS
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

Before editing this Section, review requirements of the Architectural Woodwork Institute (AWI), Architectural Woodwork Manufacturers Association of Canada (AWMAC), and Woodwork Institute's (WI) "Architectural Woodwork Standards." This review helps to avoid repeating or conflicting with requirements of that standard.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Wood countertops.

2. Shop finishing of wood countertops.

1.2 ACTION SUBMITTALS

A. Product Data: For each type of product[, including finishing materials and processes].

B. LEED Submittals:

1. Product Data for Credit MR 4: For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content. Include statement indicating cost for each product having recycled content.

"Product Certificates for Credit MR 5" Subparagraph below applies to LEED-NC, LEED-CS, and LEED for Schools.

2. Product Certificates for Credit MR 5: For products and materials required to comply with requirements for regional materials, certificates indicating location of material manufacturer and point of extraction, harvest, or recovery for each raw material. Include statement indicating distance to Project, cost for each regional material, and fraction by weight that is considered regional.

"Product Certificates for Credit MR 5" Subparagraph below applies to LEED-CI. Retain option for Credit MR 5, Option 2.

3. Product Certificates for Credit MR 5: For products and materials required to comply with requirements for regionally manufactured[ and regionally extracted and manufactured] materials. Include statement indicating cost for each regionally manufactured material.

First subparagraph below applies to LEED-CI Credit MR 5, Option 1 and Option 2.

a. Include statement indicating location of manufacturer and distance to Project for each regionally manufactured material.

First subparagraph below applies to LEED-CI Credit MR 5, Option 2.

b. Include statement indicating location of manufacturer and point of extraction, harvest, or recovery for each raw material used in regionally extracted and manufactured materials. Indicate distance to Project and fraction by weight of each regionally manufactured material that is regionally extracted.

First option in "Certificates for (Credit MR 6) (Credit MR 7)" Subparagraph below applies to LEED-CS; second applies to LEED-NC, LEED-CI, and LEED for Schools.

4. Certificates for [Credit MR 6] [Credit MR 7]: Chain-of-custody certificates indicating that products specified to be made from certified wood comply with forest certification and chain-of-custody requirements. Include statement indicating cost for each certified wood product.

"Product Data for Credit IEQ 4.1" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements for adhesives.

5. Product Data for Credit IEQ 4.1: For installation adhesives, including printed statement of VOC content.

"Laboratory Test Reports for Credit IEQ 4.1" Subparagraph below applies to LEED for Schools.

6. Laboratory Test Reports for Credit IEQ 4.1: For adhesives, documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

"Product Data for Credit IEQ 4.4" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS.

7. Product Data for Credit IEQ 4.4: For adhesives and composite wood products, documentation indicating that products contain no urea formaldehyde.

"Laboratory Test Reports for Credit IEQ 4.4" Subparagraph below applies to LEED for Schools.

8. Laboratory Test Reports for Credit IEQ 4.4: For composite wood products, documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

C. Shop Drawings: Show location of each item, dimensioned plans and elevations, large-scale details, attachment devices, and other components.

D. Samples:

Delete items in subparagraphs below that are not needed for control of grain character, color, and finish, or insert other items. The "Architectural Woodwork Standards" require samples to be "as wide as practical" by 12 inches (300 mm) for lumber and 12 by 12 inches (300 by 300 mm) for panel products.

1. Lumber for transparent finish, for each species and cut, finished on one side and one edge.

2. Veneer leaves representative of and selected from flitches to be used for transparent-finished woodwork.

1.3 INFORMATIONAL SUBMITTALS

A. Woodwork Quality Standard Compliance Certificates: [AWI Quality Certification Program certificates] [WI Certified Compliance Program certificates].

1.4 QUALITY ASSURANCE

Consider retaining one of two options in "Fabricator Qualifications" Paragraph below if AWI quality certification or WI compliance certification is required. Both AWI and WI will inspect work and provide certification for work that passes inspection if fabricator is not certified/licensed.

A. Fabricator Qualifications: [Certified participant in AWI's Quality Certification Program] [Licensee of WI's Certified Compliance Program].

Delete "Installer Qualifications" Paragraph below if not required or available. If woodwork must be FSC certified for LEED, fabricator must either install woodwork or be FSC certified for chain of custody.

B. Installer Qualifications: [Fabricator of products] [Certified participant in AWI's Quality Certification Program] [Licensee of WI's Certified Compliance Program].

1.5 FIELD CONDITIONS

A. Environmental Limitations: Do not deliver or install wood countertops until building is enclosed, wet work is complete, and HVAC system is operating and maintaining temperature and relative humidity at occupancy levels during the remainder of the construction period.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 WOODWORK FABRICATORS

Retain "Fabricators" Paragraph below if a list of preapproved woodworkers is used as a quality-control procedure. See Evaluations. Retain first or second option if additional firms will not be considered; retain third option if they will. If retaining third option, include procedure for approving other firms in the Instructions to Bidders.

A. Fabricators: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available fabricators offering products that may be incorporated into the Work include, but are not limited to, the following]:

See AWI's or WI's member list for names of woodworking firms.

1. <Insert, in separate subparagraphs, names and possibly contact information for preapproved woodworking firms>.

2.2 WOOD COUNTERTOPS

A. Quality Standard: Unless otherwise indicated, comply with the "Architectural Woodwork Standards" for grades indicated for construction, finishes, installation, and other requirements.

If retaining subparagraph below, verify applicability of certification for Project's geographic location. Certification programs of both organizations are available to member and nonmember firms. Both AWI and WI will inspect work and provide certification for work that passes inspection if fabricator is not certified/licensed. Contact either organization for a list of certified woodworkers in Project's location.

1. Provide [labels] [and] [certificates] from [AWI] [WI] certification program indicating that woodwork[, including installation,] complies with requirements of grades specified.

B. Grade: [Premium] [Custom] [Economy].

Retain first "Regional Materials" Paragraph below for LEED-NC, LEED-CS, and LEED for Schools Credit MR 5 and LEED-CI Credit MR 5, Option 2; before retaining, verify availability of materials that comply.

C. Regional Materials: Wood countertops shall be manufactured within 500 miles (800 km) of Project site from materials that have been extracted, harvested, or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

Retain "Regional Materials" Paragraph below for LEED-CI Credit MR 5, Option 1; before retaining, verify availability of materials that comply.

D. Regional Materials: Wood countertops shall be manufactured within 500 miles (800 km) of Project site.

Retain "Certified Wood" Paragraph below if wood products are required to be certified for LEED. Manufacturers certifying products as "FSC Mixed Credit" do not have to use 100 percent certified wood in the products but in their total production must use an amount equal to or greater than the percentage of their production that is labeled as "FSC Mixed Credit."

E. Certified Wood: Wood countertops shall be produced from wood certified as "FSC Pure"[ or "FSC Mixed Credit"] according to FSC STD-01-001, "FSC Principles and Criteria for Forest Stewardship," and FSC STD-40-004, "FSC Standard for Chain of Custody Certification."

Retain one type of top and related requirements in three "Type of Top" paragraphs below, or retain more than one and indicate locations of each on Drawings or in schedules.

F. Type of Top: Solid wide width for transparent finish. Solid wood, edge glued, with crown direction reversed in adjacent boards, to produce widths indicated. Select boards for similarity of color and grain and arrange boards for optimum match between adjacent boards.

1. Wood Species and Cut:[ As indicated.]

a. Species: [Red oak] [White oak] [White ash] [White birch] <Insert species>.

b. Cut: [Plain sawn] [Rift sawn] [Quarter sawn].

First "Type of Top" Paragraph below is for a butcher-block effect; "Type of Top" Paragraph above is for a more uniform effect.

G. Type of Top: Solid butcher block for transparent finish. Narrow strips of lumber glued together. Arrange strips for random mix of color and grain.

1. Wood Species: [Red oak] [Hard maple] [Teak] [As indicated] <Insert species>.

2. Strip Thickness: [3/4 inch (19 mm)] [1-1/2 inches (38 mm)] [As indicated].

H. Type of Top: Panel product for transparent finish (wood veneer laminated over core) as follows:

1. Wood Species and Cut:[ As indicated.]

a. Species: [Red oak] [White oak] [White ash] [White birch] <Insert species>.

b. Cut: [Plain sliced] [Rift cut] [Quarter cut].

Retain one of first three options in "Matching of Adjacent Veneer Leaves" Subparagraph below. Retain last option if tops are longer than veneer leaves or if required for special effect. Show on Drawings.

2. Matching of Adjacent Veneer Leaves: [Book] [slip] [random] [and] [end] match.

Retain one of three options in "Veneer Matching within Panel Face" Subparagraph below.

3. Veneer Matching within Panel Face: [Running] [Balance] [Center-balance] match.

Retain one of three options in "Edge Treatment" Subparagraph below.

4. Edge Treatment: [Solid wood matching face for species and cut] [Wood veneer matching face for species and cut] [As indicated].

2.3 WOOD MATERIALS

A. Wood Products: Provide materials that comply with requirements of referenced quality standard for each type of woodwork and quality grade specified unless otherwise indicated.

Retain one of three ranges of moisture content in "Wood Moisture Content" Subparagraph below. First range applies to Ontario, Quebec, and most of U.S. Second applies to damp coastal areas of southern U.S. and to the Maritime Provinces. Third applies to dry southwestern U.S. and to Alberta, Manitoba, and Saskatchewan. See relative-humidity and moisture-content map in the "Architectural Woodwork Standards." Note that some areas have micro-climates that differ from the surrounding region.

1. Wood Moisture Content: [5 to 10] [8 to 13] [4 to 9] percent.

B. Composite Wood and Agrifiber Products: Provide materials that comply with requirements of referenced quality standard for each type of woodwork and quality grade specified unless otherwise indicated.

Retain "Recycled Content of Medium-Density Fiberboard and Particleboard" Subparagraph below if recycled content is required for LEED Credit MR 4. Recycled content of medium-density fiberboard and particleboard varies greatly; consult manufacturers before inserting requirement.

1. Recycled Content of Medium-Density Fiberboard and Particleboard: Postconsumer recycled content plus one-half of preconsumer recycled content not less than <Insert number> percent.

Retain "Composite Wood and Agrifiber Products" Subparagraph below if required for LEED for Schools Credit IEQ 4.4.

2. Composite Wood and Agrifiber Products: Products shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

Grades for medium-density fiberboard changed with the 2002 edition of ANSI A208.2. Grade 130 is approximately equivalent to the previous Grade MD. If retaining "Medium-Density Fiberboard" Subparagraph below and low-emitting materials are required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.4, retain option for binder containing no urea formaldehyde. Specifying products without urea formaldehyde will decrease competition and may increase costs. ANSI A208.2 requires products to comply with formaldehyde emission limits established by HUD.

3. Medium-Density Fiberboard: ANSI A208.2, [Grade 130] <Insert grade>[, made with binder containing no urea formaldehyde].

If retaining "Particleboard" Subparagraph below and low-emitting materials are required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.4, retain option for binder containing no urea formaldehyde or option requiring exterior-type glue. Specifying products without urea formaldehyde or with exterior-type glue will decrease competition and may increase costs. ANSI A208.1 requires products to comply with formaldehyde emission limits established by HUD.

4. Particleboard: ANSI A208.1, [Grade M-2] [Grade M-2, made with binder containing no urea formaldehyde] [Grade M-2-Exterior Glue].

5. Softwood Plywood: DOC PS 1.

2.4 ACCESSORIES

Sizes in "Grommets for Cable Passage through Countertops" Paragraph below are two of the many offered. Other colors, materials, and styles are also available. 1-1/4-inch (32-mm) grommet is "OG series"; 2-inch (51-mm) grommet is "SG series."

A. Grommets for Cable Passage through Countertops: [1-1/4-inch (32-mm)] [2-inch (51-mm)] <Insert dimension> OD, [brown] [black] <Insert color>, molded-plastic grommets and matching plastic caps with slot for wire passage.

1. Product: Subject to compliance with requirements, provide "[OG] [SG] series" by Doug Mockett & Company, Inc.

B. Paper Slots: [12 inches (305 mm)] [17 inches (432 mm)] long by 1-3/4 inches (45 mm) wide by 1 inch (25 mm) deep; [brown] [black] <Insert color>, molded-plastic, paper-slot liner with 1/4-inch (6.4-mm) lip.

2.5 MISCELLANEOUS MATERIALS

Retain first "Adhesives" Paragraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.4. See Evaluations.

A. Adhesives: Do not use adhesives that contain urea formaldehyde.

Retain "Adhesives" Paragraph below if required for LEED for Schools.

B. Adhesives: Use adhesives that meet the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

Retain "VOC Limits for Installation Adhesives and Sealants" Paragraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.1.

C. VOC Limits for Installation Adhesives and Sealants: Use products that comply with the following limits for VOC content when calculated according to 40 CFR 59, Subpart D (EPA Method 24):

1. Wood Glues: 30 g/L.

2. Multipurpose Construction Adhesives: 70 g/L.

3. Structural Wood Member Adhesive: 140 g/L.

4. Architectural Sealants: 250 g/L.

2.6 FABRICATION

A. Fabricate wood countertops to dimensions, profiles, and details indicated. Ease edges to radius indicated for the following:

1. Solid-Wood (Lumber) Members: 1/16 inch (1.5 mm) unless otherwise indicated.

Retain "Edges of Members More Than 3/4 Inch (19 mm) Thick" Subparagraph below if needed and if acceptable.

2. Edges of Members More Than 3/4 Inch (19 mm) Thick: 1/8 inch (3 mm).

If applicable, insert subparagraph to describe conditions where eased edges are not required.

B. Complete fabrication, including assembly[, finishing,] and hardware application, to maximum extent possible before shipment to Project site. Disassemble components only as necessary for shipment and installation. Where necessary for fitting at site, provide ample allowance for scribing, trimming, and fitting.

C. Shop-cut openings to maximum extent possible to receive hardware, appliances, plumbing fixtures, electrical work, and similar items. Locate openings accurately and use templates or roughing-in diagrams to produce accurately sized and shaped openings. Sand edges of cutouts to remove splinters and burrs.

2.7 SHOP FINISHING

Delete this article if shop finishing is not required. See Evaluations. Shop finishing can be used to help comply with LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.2, which limits VOC content of paints and coatings used within building.

A. General: Finish architectural wood countertops at fabrication shop as specified in this Section. Defer only final touchup, cleaning, and polishing until after installation.

"Finish Materials" Paragraph below applies to LEED for Schools.

B. Finish Materials: Use finish materials that meet the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

C. Preparation for Finishing: Comply with referenced quality standard for sanding, filling countersunk fasteners, sealing concealed surfaces, and similar preparations for finishing architectural woodwork, as applicable to each unit of work.

Generally retain "Backpriming" Subparagraph below. Backpriming helps moderate alternating shrinking and swelling caused by fluctuations in moisture content resulting from variations in relative humidity.

1. Backpriming: Apply one coat of sealer or primer, compatible with finish coats, to concealed surfaces of wood countertops. Apply two coats to end-grain surfaces.

D. Transparent Finish:

1. Grade: [Premium] [Custom] [Economy] [Same as item to be finished].

System - 4 has best resistance to yellowing.

2. Finish: System - 4, water-based latex acrylic.

System - 5 is a durable, repairable, and good general-purpose fine finish.

3. Finish: System - 5, conversion varnish.

4. Finish: System - 6, synthetic penetrating oil.

System - 7 is durable and has good chemical resistance.

5. Finish: System - 7, catalyzed vinyl.

6. Finish: System - 8, water-based cross linking acrylic.

System - 11 is very durable but not easily repaired.

7. Finish: System - 11, catalyzed polyurethane.

8. Finish: System - 12, water-based polyurethane.

Wash coat helps prevent blotchiness with wiping stains.

9. Wash Coat for Closed-Grain Woods: Apply wash-coat sealer to woodwork made from closed-grain wood before staining and finishing.

10. Staining: [None required] [Match approved sample for color] [Match Architect's sample].

Retain "Open Finish for Open-Grain Woods" or "Filled Finish for Open-Grain Woods" Subparagraph below if open-grain wood is used.

11. Open Finish for Open-Grain Woods: Do not apply filler to open-grain woods.

Retain option in "Filled Finish for Open-Grain Woods" Subparagraph below for highest-quality work to prevent solvent in filler from smearing stain.

12. Filled Finish for Open-Grain Woods:[ After staining, apply wash-coat sealer and allow to dry.] Apply paste wood filler and wipe off excess. Tint filler to match stained wood.

Retain one of four options in "Sheen" Subparagraph below; coordinate with effect and finish system retained. Numerical values for gloss ratings are those published in the "Architectural Woodwork Standards." Retain flat sheen with oil finish.

13. Sheen: [Flat, 15-30] [Satin, 31-45] [Semigloss, 46-60] [Gloss, 61-100] gloss units measured on 60-degree gloss meter per ASTM D 523.

PART 3 -  EXECUTION

3.1 PREPARATION

A. Before installation, condition wood countertops to average prevailing humidity conditions in installation areas.

3.2 INSTALLATION

Revise "Grade" Paragraph below if installation grade is different from fabrication grade.

A. Grade: Install wood countertops to comply with same grade as item to be installed.

B. Install wood countertops level, plumb, true, and straight. Shim as required with concealed shims. Install level and plumb to a tolerance of 1/8 inch in 96 inches (3 mm in 2400 mm).

C. Scribe and cut wood countertops to fit adjoining work, refinish cut surfaces, and repair damaged finish at cuts.

D. Countertops: Anchor securely by screwing through corner blocks of base cabinets or other supports into underside of countertop.

1. Install countertops with no more than 1/8 inch in 96-inch (3 mm in 2400-mm) sag, bow, or other variation from a straight line.

Retain first subparagraph below if applied backsplashes are used.

2. Secure backsplashes [to tops with concealed metal brackets at 16 inches (400 mm) o.c.] [and] [to walls with adhesive].

3. Calk space between backsplash and wall with sealant specified in Section 079200 "Joint Sealants."

END OF SECTION 123619

	WOOD COUNTERTOPS
	123619 - 1



