Exterior Stucco Specifications:

1. Comply with ASTM C-841 and C-842. Provide ¾” overall thickness on self-furring diamond mesh galvanized metal lath, 3.4 lb. per square yard, on “Tyvek” Stucco Wrap. Attach lath at “dimples” only, with non-corrosive screws.

2. Metal lath and all accessories to be equal to “Amico”, to include corner beads, casing beads, base screeds, and control joints, all installed with non-corrosive screws. All accessories to be zinc. All corners to be mitered.

3. Stucco to be installed in three coats; scratch, brown, and finish. Finish coat to be Oriental Stucco with sand float finish by U. S. Gypsum.

4. Comply with Manufacturer’s and industry recommendations. Install lath in accordance with ASTM C-1063.

5. Submit data / cut sheets for all items if required.

