
SECTION 03200PRIVATE 


CONCRETE REINFORCEMENT

Provisions of the contract including General and Supplementary General Conditions and the General Requirements apply to the work of this section.
1 PART 1   GENERAL


.1

SECTION INCLUDES



A.
Reinforcing steel bars, wire fabric and accessories and cable slab reinforcing for cast‑in-place concrete. (See cable slab drawings for post-tensioned cable specifications).


.2

RELATED SECTIONS



A.
Section 03100 ‑ Concrete Formwork.



B.
Section 03300 ‑ Cast‑in‑Place Concrete.



C.
Section 03346 ‑ Concrete Floor Finishing: Reinforcement for concrete floor toppings.

D. Section 04300 – Unit Masonry System: Reinforcement for masonry.



E.
Reference to General Conditions.


.3

REFERENCES



A.
ACI 301 ‑ Structural Concrete for Buildings.



B.
ACI SP‑66 ‑ American Concrete Institute ‑ Detailing Manual.



C.
ANSI/ASTM A82 ‑ Cold Drawn Steel Wire for Concrete Reinforcement.



D.
ANSI/ASTM A185 ‑ Welded Steel Wire Fabric for Concrete Reinforcement.



E.
ANSI/ASTM A496 ‑ Deformed Steel Wire Fabric for Concrete Reinforcement.



F.
ASTM A615 ‑ Deformed and Plain Billet Steel Bars for Concrete Reinforcement.



G.
ASTM A617



H.
ASTM A704



I.
ASTM A706



J.  ASTM A767



K.
AWS D12.1 ‑ Welding Reinforcement Steel, Metal Inserts and Connections in Reinforced Concrete Construction.



L.
CRSI ‑ Concrete Reinforcing Steel Institute Manual of Practice.



M.
CRSI 63 ‑ Recommended Practice For Placing Reinforcing Bars.



N. 
CRSI 65 ‑ Recommended Practice For Placing Bar Supports, Specifications and Nomenclature.




.4

SUBMITTALS



A.
Submit under provisions of Section 01300.



B.
Shop Drawings: Indicate bar sizes, spacing, locations, and quantities of reinforcing steel and wire fabric, bending and cutting schedules, and supporting and spacing devices.


.5

QUALITY ASSURANCE



A.
Perform Work in accordance with CRSI 63, 65 and Manual of Practice ACI 301 ACI SP‑66.



B.
Submit certified copies of mill test report of reinforcement materials analysis.



C.
Provide Architect/Engineer with access to fabrication plant to facilitate inspection of reinforcement.  Provide notification of commencement and duration of shop fabrication in sufficient time to allow inspection.


.6

QUALIFICATIONS



A.
Design reinforcement under direct supervision of a Professional Structural Engineer experienced in design of this work and licensed in the State of Louisiana.


.7

COORDINATION



A.
Coordinate work under provisions of Section 01039.



B.
Coordinate with placement of formwork, formed openings and other Work.

2 PART 2   PRODUCTS


.1

REINFORCEMENT



A.
Reinforcing Steel: ASTM A615, 60 ksi yield grade; deformed billet steel bars, plain finish.



B.
Welded Steel Wire Fabric:  ASTM A185 Plain Type ASTM A497 Welded Deformed Type ASTM A497 Deformed Type; in flat sheets; plain finish.


.2

ACCESSORY MATERIALS



A.
Tie Wire:  Minimum 16 gage annealed type.



B.
Chairs, Bolsters, Bar Supports, Spacers:
Sized and shaped for strength and support of reinforcement during concrete placement conditions including load bearing pad on bottom to prevent vapor barrier puncture.



C.
Special Chairs, Bolsters, Bar Supports, Spacers Adjacent to Weather Exposed Concrete Surfaces: Plastic coated steel type; size and shape as required. Fir slabs on grade use supports with sand-plates or horizontal runners.


.3

FABRICATION



A.
Fabricate concrete reinforcing in accordance with CRSI Manual of Practice ACI SP‑66.



B.
Locate reinforcing splices not indicated on Drawings, at point of minimum stress.  Review location of splices with Architect/Engineer.

3 PART 3   EXECUTION


.1

PLACEMENT



A.
Place, support and secure reinforcement against displacement.  Do not deviate from required position.



B.
Do not displace or damage vapor barrier.



C.
Accommodate placement of formed openings.



D.
Conform to applicable code for concrete cover over reinforcement.


.2

FIELD QUALITY CONTROL



A.
Field inspection will be performed under provisions of Section 01400.


END OF SECTION
PAGE  
Error! Main Document Only.
Section 03200 Page 3 of 3      

