
SECTION 04100PRIVATE 


MORTAR

Provisions of the contract including General and Supplementary General Conditions and the General Requirements apply to the work of this section.
1 PART 1   GENERAL


.1

SECTION INCLUDES



A.
Mortar for masonry.


.2

seq level2 \h \r0 

RELATED WORK



A.
Section 01400 ‑ Quality Control: Testing laboratory services.



B.
Section 04300 ‑ Unit Masonry System: Installation of mortar.


C.
Section 08112 ‑ Standard Steel Frames: Grouting steel door     frames.



D.
Reference to General Conditions. 


.3

seq level2 \h \r0 

REFERENCES



A.
ASTM C94 ‑ Ready‑Mixed Concrete.


B.
ASTM C144 ‑ Aggregate for Masonry Mortar.


C.
ASTM C150 ‑ Portland Cement.


D.
ASTM C207 ‑ Hydrated Lime for Masonry Purposes.

.4

seq level2 \h \r0 
seq level2 \h \r0 
DELIVERY, STORAGE, AND HANDLING



A.
Deliver products to site under provisions of Section 01600. 


B.
Store and protect products under provisions of Section 01600.


C.
Maintain packaged materials clean, dry, and protected against dampness, freezing, and foreign matter.


.5
seq level2 \h \r0 
ENVIRONMENTAL REQUIREMENTS



A.
Maintain materials and surrounding air temperatures to minimum 50 degrees F (10 degrees C) prior to, during, and 48 hours after completion of masonry work.

2

seq level1 \h \r0 

seq level2 \h \r0  PART 2   PRODUCTS

.1
seq level2 \h \r0 
MATERIALS



A.
Portland Cement: ASTM C150, Type I, gray color.



B.
Mortar Aggregate: ASTM C144, standard masonry type.


C.
Hydrated Lime: ASTM C207, Type S.

.2
seq level2 \h \r0 
MORTAR MIXES



A.
Mortar for Load Bearing Walls and Partitions: ASTM C270, Type S using the Property Method.



B.
Mortar for Non‑load Bearing Walls and Partitions: ASTM C270, Type S using the Property Method.


.3
seq level2 \h \r0 
MORTAR MIXING



A.
Thoroughly mix mortar ingredients in quantities needed for immediate use in accordance with ASTM C270.



B.
Do not use anti‑freeze compounds to lower the freezing point of mortar.


C.
If water is lost by evaporation, re-temper only within two hours of mixing.


D.
Use mortar within two hours after mixing at temperatures of 80 degrees F (26 degrees C), or two‑and‑one‑half hours at temperatures under 50 degrees F (10 degrees C).



.4
seq level2 \h \r0 
GROUT MIXES



A.
Bond beams: 3000-psi strength at 28 days; 7‑8 inches (175‑200 mm) slump.

.5
seq level2 \h \r0 
GROUT MIXING



A.
Mix concrete in accordance with ASTM C94



B.
Do not use anti‑freeze compounds to lower the freezing point of grout.
3

seq level1 \h \r0 

seq level2 \h \r0  PART 3   EXECUTION


.1

EXAMINATION



A.
Request inspection of spaces to be grouted.


.2

seq level2 \h \r0 

PREPARATION



A.
Apply bonding agent to existing concrete surfaces.



B.
Plug clean-out holes with block masonry units to prevent leakage of grout materials. Brace masonry for wet grout pressure.


.3

seq level2 \h \r0 

INSTALLATION



A.
Install mortar and grout to requirements of the specific masonry Section.



B.  Work grout into masonry cores and cavities to eliminate voids.



B.
Do not displace reinforcement while placing grout.



C.
Remove grout spaces of excess mortar.








END OF SECTION
PAGE  
Section 04100 Page 1 of 3

