
SECTION 06112PRIVATE 


FRAMING AND SHEATHING

1 PART 1 GENERAL


.1
SECTION INCLUDES



A.
Structural floor, wall, and roof framing.



B.
Built-up structural beams.



C.
Diaphragm trusses built on site.



D.
Floor, wall, and roof sheathing.



E.
Sill flashing.



F.
Preservative treatment of wood.



G.
Fire retardant treatment of wood.



H.
Miscellaneous framing and sheathing.



I.
Telephone and electrical panel boards.



J.
Concealed wood blocking for support of toilet and bath accessories wall cabinets and wood trim.


.2
PRODUCTS FURNISHED BUT NOT INSTALLED UNDER THIS SECTION



A.
Placement of steel fabrications into concrete and masonry.


.3
RELATED SECTIONS



A.
Setting anchors in concrete.



B.
Section:  Prefabricated steel structural supports.



C.
Section 06125 - Wood Decking.



D.
Heavy Timber Framing.



E.
Timber Trusses.



F.
Plywood Web Joists.



G.
Reference to General Conditions.


.4
REFERENCES



A.
ALSC - American Lumber Standards Committee:  Softwood Lumber Standards.



B.
ANSI A208.1 – Mat-Formed Wood Particleboard.



C.
ANSI/AHA A135.4 - Basic Hardboard.



D.
APA:  American Plywood Association.



E.
AWPA (American Wood Preservers Association) C1 - All Timber Products Preservative Treatment by Pressure Process.



F.
AWPA (American Wood Preservers Association) C20 -Structural Lumber Fire Retardant Treatment by Pressure Process.



G.
NFPA:  National Forest Products Association.



H.
RIS:  Redwood Inspection Service.



I.
SPIB:  Southern Pine Inspection Bureau.



J.
WCLIB:
West Coast Lumber Inspection Bureau.



K.
WWPA:  Western Wood Products Association.


.5
SUBMITTALS



A.
Submit under provisions of Section 01300.



B.
Shop Drawings For Site Fabricated Truss Frame:  Indicate dimensions, wood species and grades, component profiles, drilled holes, fasteners, connectors, erection details and sequence.



C.
Product Data:  Provide technical data on insulated sheathing, wood preservative materials, and application instructions.


.6
QUALITY ASSURANCE



A.
Perform Work in accordance with the following agencies:




1.
Lumber Grading Agency:
Certified by ALSC.




2.
Plywood Grading Agency:  Certified by APA.



B.
In lieu of grade stamping exposed to view lumber and plywood, submit manufacturer's certificate under provisions of Section 01400 that products meet or exceed specified requirements


.7
DELIVERY, STORAGE, AND HANDLING



A.
Deliver, store, protect, and handle products to site under provisions of Section 01600.



B.
Protect site framed structural site fabricated trusses from warping or other distortion by stacking in vertical position, braced to resist movement.

2 PART 2 PRODUCTS


.1
LUMBER MATERIALS



A.
Lumber Grading Rules: SPIB.



B.
Beam Framing: 19 percent maximum moisture content.



C.
Joist Framing: 19 percent maximum moisture content.



D.
Rafter Framing: 19 percent maximum moisture content.



E.
Non-structural Light Framing: SYP species, 19 percent maximum moisture content.


F.
Studding:  Stress Group SYP species, 19 percent maximum moisture content.



G.
Framing in contact with foundation: Pressure treated SYP.



H.
Miscellaneous Framing: SYP species, 19 percent maximum moisture content.


.2
SHEATHING MATERIALS



A.
Particleboard Roof Sheathing: ANSI A208.1 Oriented Strand Board.




B.
Particleboard Wall Sheathing: ANSI A208.1 Oriented Strand Board, set with waterproof resin binder unsanded faces.





C.
Particleboard Floor Sheathing:   ANSI A208.1 Oriented Strand Board set with waterproof resin binder.


.3
UNDERLAYMENT MATERIALS



A.
Plywood Underlayment:  APA  Structural [II],  Exposure Durability 1; unsanded.


.4
ACCESSORIES



A.
Fasteners and Anchors:


1.
Drywall Screws:  Bugle head, hardened steel, power driven type, length three times thickness of sheathing.




2.
Anchors: Expansion shields and lag bolt type for anchorage to solid masonry or concrete. 


B.
Die Stamped Connectors: hot dipped galvanized steel.



C.
Joist Hangers: Hot dipped galvanized steel, sized to suit framing conditions.



D.
Building Paper: No. 15 asphalt felt.


.5
FACTORY WOOD TREATMENT



A.
Wood Preservative (Pressure Treatment):  AWPA Treatment C1 using water borne preservative with 0.25 percent retainage.

3 PART 3 EXECUTION


.1
FRAMING



A.
Set structural members level and plumb, in correct position.



B.
Make provisions for erection loads, and for sufficient temporary bracing to maintain structure safe, plumb, and in true alignment until completion of erection and installation of permanent bracing.



C.
Place horizontal members flat, crown side up.



D.
Construct load bearing framing and curb members full length without splices.



E.
Double members at openings over [24] inches wide.  Space short studs over and under opening to stud spacing.



F.
Construct double joist headers at floor and ceiling openings and under wall stud partitions that are parallel to floor joists.  Frame rigidly into joists.


.2
SHEATHING



A.
Secure roof sheathing perpendicular to framing members with ends staggered and sheet ends over firm bearing.  Use sheathing clips between sheets between roof framing members.  



B.
Secure wall sheathing with long dimension  perpendicular to wall studs, with ends over firm bearing and staggered.



C.
Place plywood or structural-use panel sheeting at building corners for a horizontal distance of 48 inches.



D.
Place building paper horizontally over wall sheathing, weather lap edges and ends.



E.
Secure sub-floor perpendicular to floor framing with end joints staggered and sheet ends over firm bearing.  Attach with sub-floor glue and drywall screws.

F. Install plywood to two span continuous. 



G.
Install telephone and electrical panel boards with plywood sheathing material where required.  Over size the panel by [12] inches on all sides.


.3
SITE APPLIED WOOD TREATMENT



A.
Apply preservative treatment in accordance with manufacturer's instructions.



B.
Brush apply one coats of preservative treatment on wood in contact with cementitious materials roofing and related metal flashings.



C.
Allow preservative to dry prior to erecting members.


.4
TOLERANCES



A.
Framing Members: ¼ inch from true position, maximum.



B.
Surface Flatness of Floor: ¼ inch in 10 feet maximum, and ½ inch maximum in feet.


.5
SCHEDULES



A.
Above Grade Joist, Rafter, and Stud Framing:
S/P/F species, 19 percent maximum moisture content.



B.
Sloped Roof Sheathing: Plywood, 3/8 inch thick, 4 x 8 sized sheets, square edges; appearance grade facing inward.


C.
Blocking and Cants: S/P/F species, pressure preservative treatment.


END OF SECTION

PAGE  
Section 06112 Page 3 of 6
Error! Main Document Only.

