

SECTION 08800PRIVATE 


GLAZING

Provisions of the contract including General and Supplementary General Conditions and the General Requirements apply to the work of this section.
1 PART 1   GENERAL


.1

SECTION INCLUDES



A.
Glass and glazing for Sections referencing this Section for products and installation.


.2

REFERENCES



A.
ANSI/ASTM E330 ‑ Structural Performance of Exterior Windows, Curtain Walls, and Doors by Uniform Static Air Pressure Difference.



B.
ANSI Z97.1 ‑ Safety Performance Specifications and Methods of Test for Safety Glazing Used in Buildings.



C.
ASTM C1036 ‑ Flat Glass.



D.
ASTM C1048 ‑ Heat‑Treated Flat Glass ‑ Kind HS, Kind FT Coated and Uncoated Glass.



E.
ASTM E546 ‑ Test Method For Frost Point of Sealed Insulating Glass Units.



F.
ASTM E576 ‑ Test Method For Dew/Frost Point of Sealed Insulating Glass Units in Vertical Position.



G.
ASTM E773 ‑ Test Method for Seal Durability of Sealed Insulating Glass Units.



H.
ASTM E774 ‑ Sealed Insulating Glass Units.



I.
FGMA ‑ Glazing Manual.



J.
FGMA ‑ Sealant Manual.



K.
FS TT‑C‑00598 ‑ Caulking Compound, Oil and Resin Base Type.



L.
FS TT‑S‑001657 ‑ Sealing Compound, Single Component, Butyl Rubber Based, Solvent Release Type.



M.
FS TT‑S‑00227 ‑ Sealing Compound, Rubber Base, Two Component.



N.
FS TT‑S‑00230 ‑ Sealing Compounds, Synthetic‑Rubber Base, Single Component, Chemically Curing.



O.
FS TT‑S‑01543 ‑ Sealing Compound, Silicone Rubber Base.



P.
FS TT‑G‑410 ‑ Glazing Compound, Sash (Metal) for Back Bedding and Face Glazing (Not for Channel or Stop Glazing).



Q.
Laminators Safety Glass Association ‑ Standards Manual.

R. SIGMA ‑ Sealed Insulated Glass Manufacturers Association.



S.
Reference to General Conditions.


.3

SUBMITTALS



A.
Manufacturer's Installation Instructions: Indicate special precautions required.



B.
Manufacturer's Certificate:  Certify that sealed insulated glass, meet or exceed specified requirements.


.4

QUALITY ASSURANCE



A.
Perform Work in accordance with FGMA Glazing Manual, FGMA Sealant Manual and Laminators Safety Glass Association ‑ Standards Manual for glazing installation methods.


.5

ENVIRONMENTAL REQUIREMENTS



A.
Do not install glazing when ambient temperature is less than 50 degrees F (10 degrees C).



B.
Maintain minimum ambient temperature before, during and 24  hours after installation of glazing compounds.


.6

FIELD MEASUREMENTS



A.
Verify that field measurements are as indicated on Drawings instructed by the manufacturer.


.7

COORDINATION



A.
Coordinate Work under provisions of Section 01039.



B.
Coordinate the Work with glazing frames, wall openings, and perimeter air and vapor seal to adjacent Work.


.8

WARRANTY



A.
Provide ten year manufacturer's warranty under provisions of Section 01700.



B.
Warranty:  Include coverage for sealed glass units from seal failure, interpane dusting or misting, and replacement of same.


2 PART 2   PRODUCTS


.1

FLAT GLASS MATERIALS



A.
Wire Glass (Type FG‑G): Clear, polished both sides diagonal  mesh of woven stainless steel wire of 1/2  inch (12 mm) grid size; 1/4  inch (6 mm) thick.




.2

SEALED INSULATING GLASS MATERIALS



A.
Insulated Glass Units (Type SG-A): ASTM E774 and E773; double pane with glass to mastic edge seal, outer pane of clear glass inner pane of clear glass.  Interpane space purged dry thermetic air, total unit thickness of 5’8 inch minimum.


.3

SEALED INSULATING GLASS MATERIALS



A.
Insulated Glass Units (Type SG‑A):  ASTM E774 and E773; double pane with glass to mastic  edge seal; outer pane of clear glass inner pane of clear glass, interpane space purged dry hermetic air; total unit thickness of 5’8 inch minimum.

3 PART 3   EXECUTION


.1

EXAMINATION



A.
Verify prepared openings under provisions of Section 01039.



B.
Verify that openings for glazing are correctly sized and within tolerance.



C.
Verify that surfaces of glazing channels or recesses are clean, free of obstructions, and ready to receive glazing.


.2

PREPARATION



A.
Clean contact surfaces with solvent and wipe dry.



B.
Seal porous glazing channels or recesses with substrate compatible primer or sealer.



C.
Prime surfaces scheduled to receive sealant.


.3

INTERIOR ‑ DRY METHOD (TAPE AND TAPE)



A.
Cut glazing tape to length and set against permanent stops, projecting 1/16 inch (1.6 mm) above sight line.



B.
Place setting blocks at 1/4 points with edge block no more than 6 inches (150 mm) from corners.



C.
Rest glazing on setting blocks and push against tape for full contact at perimeter of pane or unit.



D.
Place glazing tape on free perimeter of glazing in same manner described above.



E.
Install removable stop without displacement of tape.




Exert pressure on tape for full continuous contact.



F.
Knife trim protruding tape.


.4

INTERIOR ‑ WET METHOD (COMPOUND AND COMPOUND)



A.
Install glazing resting on setting blocks.  Install applied stop and center pane by use of spacer shims at 24-inch (600 mm) centers, kept 1/4 inch (6 mm) below sight line.


.5

CLEANING



A.
Clean work under provisions of 01700.



B.
Remove glazing materials from finish surfaces.



C.
Remove labels after work is complete.



D.
Clean glass.


.6

PROTECTION OF FINISHED WORK



A.
Protect finished Work under provisions of Section 01500.


END OF SECTION
PAGE  
Error! Main Document Only.
Section 08800 Page 2 of 4

