

SECTION 09312PRIVATE 


CERAMIC TILE WALL FINISH

Provisions of the contract including General and Supplementary General Conditions and the General Requirements apply to the work of this section.
1 PART 1   GENERAL


.1

SECTION INCLUDES



A.
Ceramic tile walls finish using the thinset application method.


.2

seq level2 \h \r0 

RELATED SECTIONS



A.
Section 04300 – Unit Masonry: Wall substrate surface.

.3
seq level2 \h \r0 
REFERENCES



A.
ANSI/TCA A108.4 ‑ Installation of Ceramic Tile with Water Resistant Organic Adhesive.



B.
ANSI/TCA A108.5 ‑ Ceramic Tile Installed with Dry‑Set Portland Cement Mortar or Latex Portland Cement Mortar.



C.
ANSI/TCA A118.1 ‑ Dry‑Set Portland Cement Mortar.


D.
ANSI/TCA A118.4 ‑ Latex‑Portland Cement Mortar.


E.
ANSI/TCA A136.1 ‑ Organic Adhesives for Installation of Ceramic Tile, Type 1 and Type 2.


F.
ANSI/TCA A137.1 ‑ Specifications for Ceramic Tile.


G.
TCA (Tile Council of America) ‑ Handbook for Ceramic Tile Installation.

.4
seq level2 \h \r0 
SUBMITTALS



A.
Submit product data under provisions of Section 01300.



B.
Submit product data indicating material specifications, characteristics, and instructions for using adhesives and grouts.


C.
Submit samples under provisions of Section 01300.


D.
Submit manufacturer's installation instructions under provisions of Section 01300.


E.
Submit maintenance data under provisions of Section 01700.


F.
Include recommended cleaning and stain removal methods, and cleaning materials.



G.
Reference to General Conditions.

.5
seq level2 \h \r0 
QUALITY ASSURANCE



A.
Conform to ANSI/TCA A137.1



B.
Conform to TCA Handbook for Ceramic Tile Installation. 


.6
seq level2 \h \r0 
DELIVERY, STORAGE, AND HANDLINGseq level2 \h \r0 


A.
Deliver products to site under provisions of Section 01600.



B.
Store and protect products under provisions of Section 01600. 



C.
Protect adhesives from freezing or overheating in accordance with manufacturer's instructions.


.7
seq level2 \h \r0 
ENVIRONMENTAL REQUIREMENTS



A.
Do not install adhesives in a closed, unventilated environment.



B.
Maintain 50 degrees F (10 degrees C) during installation of mortar materials.

2

seq level1 \h \r0 

seq level2 \h \r0  PART 2   PRODUCTS


.1

MANUFACTURERS ‑ TILE



A.
American Ocean


B.
Florida Tile; Natural Liberty.


C.
Substitutions: Under provisions of Section 01600.

.2
seq level2 \h \r0 
TILE MATERIAL



A.
Ceramic Wall Tile: ANSI/TCA A137.1, conforming to the following:




Moisture Absorption 

 0 to 0.5 percent




Size





 12” x 12” 

Edge





 Square












Surface Finish


 Matte glazed






 




Color




 As selected


B.
Wainscot Cap: Match wall tile for moisture absorption, surface finish, and color, tile length, bullnosed top edge.

.3
seq level2 \h \r0 
seq level2 \h \r0 ADHESIVE MATERIALS



A.
Organic Adhesive: ANSI/TCA A136.1, Type 1; thinset bond type.


.4
seq level2 \h \r0 

MORTAR MATERIALSseq level2 \h \r0 


A.
Mortar Materials: ANSI/TCA A118.1; Portland cement, sand, latex additive, and water.


.5
seq level2 \h \r0 
GROUT MATERIALS



A.
Grout: Cementitious type with latex additive.


.6seq level2 \h \r0 

MORTAR MIX AND GROUT MIX



A.
Mix and proportion pre‑mix grout materials in accordance with TCA Handbook for Ceramic Tile Installation.

3

seq level1 \h \r0 

seq level2 \h \r0  PART 3   EXECUTION


.1

EXAMINATION



A.
Verify that surfaces are ready to receive work.



B.
Beginning of installation means installer accepts condition of existing surfaces.


.2
seq level2 \h \r0 
PREPARATION



A.
Protect surrounding work from damage or disfiguration.



B.
Vacuum clean existing surfaces and damp clean.


C.
Seal substrate surface cracks with filler.  Level existing substrate surfaces to acceptable flatness tolerances.



D.
Apply sealer to surfaces as recommended by adhesive manufacturer.


.3

seq level2 \h \r0 

INSTALLATION ‑ THINSET METHOD



A.
Install adhesive, tile, and grout to TCA Handbook for Ceramic Tile Installation.


B.
Request tile pattern from Architect/Engineer.  Do not interrupt tile pattern around openings.


C.
Cut and fit tile tight to penetrations through tile.
 Form corners neatly.  Align wall, base, and floor joints.


D.
Place tile joints uniform in width, subject to variance in tolerance allowed in tile size.  Make joints watertight, without voids, cracks, excess mortar or excess grout.


E.
Form internal angles coved and external angles bullnosed.


F.
 Sound tile after setting. Replace hollow sounding units.


G.
Allow tile to set for a minimum of 48 hours prior to grouting


H.
Grout tile joints.


I.
Apply sealant to junction of tile and dissimilar materials and at junction of dissimilar planes.

.4
seq level2 \h \r0 
CLEANING


A.
Clean work under provisions of 01700.



B.
Clean tile surfaces.


END OF SECTION
PAGE  
Section 09312 Page 2 of 4

