1.19
GLASS/GLAZING
1.19.1
Scope

The Contractor shall furnish all labor, material, and equipment necessary to complete all glass and glazing as indicated on the drawings and specified herein.

1.19.2
General 

Items of work include wire laminated glass and tempered safety glass where shown on the drawings.

1.19.3
Reference Publications, Codes and Standards


Federal Specifications DD-G-451d 1977



Federal Specifications DD-G-1403b 1972



(ANSI) American National Standards Institute 297.1, 1975



The Glass Tempering Association Standards



The Federal Safety Glazing Certification Council 16 CFR 1201

1.19.4
Materials 
1.19.4.1
All tempered glass designated on the drawings shall be tempered float glass as manufactured by Guardian Industries Corp.  The glass shall be the size and thickness shown on the drawings.  The glass shall meet the requirements of Federal Specification DD-G-1403b.

1.19.4.2
All wire laminated glass shall be "Polished Misco Wired" as manufactured by Libby-Owens-Ford.  The laminated glass shall be 1/4 inch thick, clear, float with diamond pattern wire mesh embedded therein and shall conform to Federal Specification DD-G-451d.

1.19.4.3
Glazing tape to be non-skinning, non-oily, reinforced type, performed compound Dap "1231 Flexiglaze" or Tremco "440 Tape".

1.19.5
Delivery and Handling

All glass shall be delivered in standard protective packages and stored in a safe location as directed until installed.  Each pane of glass shall be factory labeled, and labels shall remain on glass until final cleaning.

1.19.6
Performance Requirements 

All tempered glass shall have a permanent logo which signifies compliance with the Federal Standards 16 CFR 1201.

1.19.7
Workmanship 
1.19.7.1
All glass shall be fully and evenly bedded and compounded.  The face shall be compounded on a neatly sloped plane, and corners shall be reasonably true miters, neatly struck.  All excess compound shall be removed throughout, and the back struck off smooth and flush with the glazing bead.

1.19.7.2
Unless otherwise specified herein, install glass and glazing in accordance with the manufacturer's recommendations and procedures of the "Glazing Manual" of the Flat Glass Jobbers Association.

1.19.7.3
Center glass in glazing rabbet to maintain recommended clearances and provide for expansion and contraction.

1.19.7.4
The actual size of the glass is determined by the frames that receive the glass.  All sizes for the glass shall be taken from the actual frames.  The Contractor shall assume all responsibility in regard to correctly sizing glass panes.  Any sizes noted on the drawings are approximate only.

1.19.8
Inspection
1.19.8.1
Immediately after installation, crisscross the glass with masking tape or other materials that make it readily apparent that the glass is installed.  During construction, the manufacturer's identification labels shall be left on all glass.

1.19.8.2
Upon completion of construction and prior to its acceptance, all broken, cracked, or imperfect glass shall be replaced in kind without additional cost, manufacturer's labels and other markings shall be removed, and the glass, glazing, and adjacent surfaces shall be thoroughly cleaned and polished.

1.19.9
Special Conditions
STD SPEC
1.19 - 2

