1.30
METAL LINERS
1.30.1
Scope

The Contractor shall provide all labor, equipment, materials, and accessories to complete all work concerning metal liners as specified in this section or on drawings.

1.30.2
General

Metal liners of the types and sizes shown on the plan or as called for in these specifications shall be manufactured by                                    to conform with all requirements of the American Society For Testing and Materials Standards (ASTM).

1.30.3
Reference Publications, Codes and Standards



ASTM A-446 Grade A "Steel Sheet, Zinc Coated (Galvanized) Steel".

1.30.4
Materials

Metal liner sheets shall consist of the following components:



Liner sheets shall be 18 gauge galvanized annealed (galvannealed) steel sheets, meeting the requirements of "Standard Specifications for zinc coated (galvanized) steel sheets of structural quality, coils and cut lengths," ASTM A-446, Grade A.  Zinc coating shall be a minimum of 1.25 ounces per square foot.



Fasteners shall be No. 6 X 1-3'-4" pan head zinc plated steel tapping screws for attaching to metal studs and "Star" 3/16" X 7/8" drive in masonry anchors with dome head.

1.30.5
Work To Be Performed
1.30.5.1
Sheet metal lining shall be butt jointed sheets secured to the wall with water dispersed contact adhesive.

1.30.5.2
Joints shall be covered with a two inch finished joint strip of 18 gauge galvanized sheet steel.  Break edge of joint strip 3/8 inch in from each side.  Secure joint strip to each panel with number 6 panhead screws at six inch centers.  Remove all burrs and dress edges.

1.30.5.3
During installation of the elevator support clips and other structural members, large holes will be made in the existing walls.  The salvaged metal may then be used to patch "over cuts" or make escutcheons for pipes and conduit.

STD SPEC
1.30 - 1

