2.11
Baffles (Thermal Oxidizer)

2.11.1
Scope

This section covers structures located inside the combustion chamber which are used to control or direct air flow.

2.11.2
General 


All internal metal components used to construct or support baffles shall be 600 INCONEL.


Baffles for each thermal oxidizer shall consist of vertical and horizontal baffle plates and a perforated plate.


The Contractor shall take care to use special welding materials for welding INCONEL and particularly for welding dissimilar metals.

2.11.3
Vertical and Horizontal Baffle Plates


Baffle plates shall be constructed from 11 gauge 600 INCONEL.


All seams in the corrugated plates shall be welded.


All angles and channel used to support the baffles shall be 600 INCONEL.

2.11.4
Perforated Baffle Plates

The perforated plate shall be constructed from 11 gauge 600 INCONEL.


All seams in a perforated plate shall be welded.


Perforations shall consist of 1/2 inch diameter holes on 7/8 inch centers over the entire face of the plate.

STD SPEC
2.11 - 1

