Copyright 2006 AIA
MASTERSPEC Full Length
05/06

Copyright 2006 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 081433 - STILE AND RAIL WOOD DOORS
Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

A. Section Includes:

1. Exterior stile and rail wood doors[ and sidelites].

2. Interior stile and rail wood doors.

3. Interior fire-rated, stile and rail wood doors.

4. Interior fire-rated, wood door[ and sidelite] frames.

5. [Priming] [Finishing] stile and rail wood doors.

6. Fitting stile and rail wood doors to frames and machining for hardware.

7. Prehanging doors in frames.

B. Related Sections:

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.

Retain one of first two subparagraphs below if any doors are blueprint matched with architectural woodwork or wood paneling.  Division 06 Section "Wood Paneling" contains stile and rail paneling.

1. Division 06 Section "Interior Architectural Woodwork" for requirements for veneers from the same flitches for both architectural woodwork and stile and rail wood doors.

2. Division 06 Section "Wood Paneling" for requirements for veneers from the same flitches for both wood paneling and stile and rail wood doors.

3. Division 09 Section "[Exterior Painting] [Interior Painting] [Staining and Transparent Finishing]" for field finishing stile and rail doors.

1.3 SUBMITTALS

First five paragraphs below are defined in Division 01 Section "Submittal Procedures" as "Action Submittals."

A. Product Data:  For each type of product indicated.

1. Include details of construction[ and glazing].

2. Include factory finishing specifications.

B. LEED Submittals:

Retain first subparagraph below and "Forest Certification" Paragraph in "Quality Assurance" Article if stile and rail wood doors are required to be certified for LEED-NC or LEED-CI Credit MR 7, which requires that a minimum of 50 percent of wood-based materials be certified.  Retain option in subparagraph below and "Manufacturer Qualifications" Paragraph in "Quality Assurance" Article if chain-of-custody certification is required.  Note that USGBC will allow credit for the full value of the door as certified wood if door manufacturer is listed for chain-of-custody certification and if at least 70 percent of wood materials in the door are from certified forests; otherwise, it only allows credit for the value of certified wood materials used in making the door.

1. Certificates for Credit MR 7:  Chain-of-custody certificates certifying that wood used for stile and rail wood doors complies with forest certification requirements.[  Include evidence that manufacturer is certified for chain of custody by an FSC-accredited certification body.]

a. Include statement indicating costs for each certified wood product.

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.4.

2. Product Data for Credit EQ 4.4:  For adhesives and composite wood materials, documentation indicating that products contain no urea formaldehyde.

C. Shop Drawings:  For stile and rail wood doors.  Indicate location, size, and hand of each door; elevation of each kind of door; construction details not covered in Product Data, including those for stiles, rails, panels, and moldings (sticking); and other pertinent data[.][, including the following:]

1. Dimensions of doors for factory fitting.

2. Locations and dimensions of mortises and holes for hardware.

3. Requirements for veneer matching.

4. Doors to be factory finished, and finish requirements.

5. Fire ratings for fire-rated doors.

D. Samples for Initial Selection:  For factory-finished doors.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled.  Retain first paragraph below with or without above.

E. Samples for Verification:  Corner sections of doors, approximately [8 by 10 inches (200 by 250 mm)] <Insert dimensions>, with door faces and edgings representing typical range of color and grain for each species of veneer and solid lumber required.[  Finish Sample with same materials proposed for factory-finished doors.]

Remaining paragraphs are defined in Division 01 Section "Submittal Procedures" as "Informational Submittals."

Retain first paragraph below for product certificates from manufacturer.

F. Product Certificates:  For each type of door, from manufacturer.

G. Warranty:  Sample of special warranty.

1.4 QUALITY ASSURANCE

Retain first paragraph below if required for LEED-NC or LEED-CI Credit MR 7.  Before retaining, verify that manufacturers selected comply.  Note that USGBC will allow credit for the full value of the door as certified wood if door manufacturer is listed for chain-of-custody certification and if at least 70 percent of wood materials in the door are from certified forests; otherwise, it only allows credit for the value of certified wood materials used in making the door.

A. Manufacturer Qualifications:  A qualified manufacturer that is certified for chain of custody by an FSC-accredited certification body.

Retain one or more of first three paragraphs below if needed to help ensure product uniformity.

B. Source Limitations:  Obtain [stile and rail wood doors] [each type of stile and rail wood door] from single manufacturer.

C. Source Limitations:  Obtain[ custom] stile and rail wood doors from same fabricator as work in Division 06 Section "[Interior Architectural Woodwork] [Wood Paneling]."

D. Source Limitations:  Provide[ custom] stile and rail wood doors finished in same shop as work in Division 06 Section "[Interior Architectural Woodwork] [Wood Paneling]."

Retain first paragraph below if stile and rail wood doors are required to be made from wood products certified for LEED-NC or LEED-CI Credit MR 7, which requires that a minimum of 50 percent of wood-based materials be certified.  See Evaluations.  An alternative method of complying with Credit MR 7 requirement is to retain requirement in Division 01 Section "Sustainable Design Requirements" that gives Contractor the option and responsibility for determining how Credit MR 7 requirement will be met.

E. Forest Certification:  Provide doors made with [veneers] [not less than 70 percent of wood products] [all wood products] obtained from forests certified by an FSC-accredited certification body to comply with FSC STD-01-001, "FSC Principles and Criteria for Forest Stewardship."

Retain first paragraph below if applicable.  Do not retain both "UL 10B" and "UL 10C" options below.  UL 10B is a neutral-pressure test; UL 10C is a positive-pressure test.  NFPA 252 contains two choices for test pressure: "positive pressure" and "as close to neutral pressure as possible."  UBC Standard 7-2 requires testing at positive pressure for "side-hinged or pivoted swinging doors."

F. Fire-Rated Door Assemblies:  Assemblies complying with NFPA 80 that are listed and labeled by a qualified testing agency, for fire-protection ratings indicated, based on testing at [positive pressure] [as close to neutral pressure as possible] according to [NFPA 252] [UBC Standard 7-2] [or] [UL 10B] [UL 10C].

Retain subparagraph below if required.  The International Building Code allows an exception for buildings equipped throughout with fire-suppression sprinklers.

1. Temperature-Rise Limit:  [Where indicated] [At vertical exit enclosures and exit passageways], provide doors that have a maximum transmitted temperature end point of not more than 450 deg F (250 deg C) above ambient after 30 minutes of standard fire-test exposure.

Usually retain paragraph below for glass in doors or sidelites, or if glass for doors is not specified in Division 08 Section "Glazing." Decorative glass may not be required to comply with below.

G. Safety Glass:  Provide products complying with testing requirements in 16 CFR 1201, for Category II materials, unless those of Category I are expressly indicated and permitted.

1.5 DELIVERY, STORAGE, AND HANDLING

A. Comply with manufacturer's written instructions and requirements of quality standard referenced in Part 2.

Retain first paragraph below for prefinished doors and high-quality unfinished doors.

B. Package doors individually in opaque plastic bags or cardboard cartons.

C. Mark each door on top and bottom edge with opening number used on Shop Drawings.

1.6 PROJECT CONDITIONS

Retain one of two paragraphs below, usually the first.  Retain second paragraph if humidity will be controlled during occupancy.  If retaining second paragraph, retain one of three relative-humidity ranges or insert another based on local climatological data.  First option applies to most of U.S., Ontario, and Quebec; second, to damp coastal areas of southern U.S. and the Maritime Provinces; and third, to dry southwestern U.S. and to Alberta, Manitoba, and Saskatchewan.  See map and discussion about relative humidity and moisture content at the end of Section 1700 in AWI's quality standards.

A. Environmental Limitations:  Do not deliver or install doors until spaces are enclosed and weathertight, wet work in spaces is complete and dry, and temporary HVAC system is operating and maintaining ambient temperature and humidity conditions at occupancy levels during the remainder of the construction period.

B. Environmental Limitations:  Do not deliver or install doors until spaces are enclosed and weathertight, wet work in spaces is complete and dry, and HVAC system is operating and maintaining temperature between 60 and 90 deg F (16 and 32 deg C) and relative humidity between [25 and 55] [43 and 70] [17 and 50] <Insert humidity range> percent during the remainder of the construction period.

1.7 WARRANTY

When warranties are required, verify with Owner's counsel that special warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

A. Special Warranty:  Manufacturer's standard form in which manufacturer agrees to repair or replace doors that fail in materials or workmanship, or have warped (bow, cup, or twist) more than 1/4 inch (6.4 mm) in a 42-by-84-inch (1067-by-2134-mm) section.

Retain or delete first subparagraph below to suit Project.  This provision is not standard with most manufacturers and could be an added cost if retained.

1. Warranty shall also include installation and finishing that may be required due to repair or replacement of defective doors.

Revise subparagraph below to suit Project.  Standard manufacturer's warranty generally goes into effect on date of shipment, not Project acceptance.

2. Warranty shall be in effect during the following period of time from date of Substantial Completion:

Retain one option in each of first two subparagraphs below.  Before retaining, verify available warranty periods with manufacturers listed in Part 2 articles.

a. Exterior Doors:  [None] [One year] [Two years] [Five years].

b. Interior Doors:  [One year] [Five years] [Life of installation].

Retain subparagraph below if applicable.  Before retaining, verify available warranty periods with manufacturers listed in Part 2 articles.

c. Insulating[ Leaded] Glass Vision Panels:  [Three] [Five] years.

PART 2 -  PRODUCTS

2.1 MATERIALS

A. General:  Use only materials that comply with referenced standards and other requirements specified.

1. Assemble exterior doors and sidelites, including components, with wet-use adhesives complying with ASTM D 5572 for finger joints and with ASTM D 5751 for joints other than finger joints.

2. Assemble interior doors, frames, and sidelites, including components, with either dry-use or wet-use adhesives complying with ASTM D 5572 for finger joints and with ASTM D 5751 for joints other than finger joints.

Retain first paragraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.4.  Verify availability before retaining.

B. Low-Emitting Materials:  Provide doors made with adhesives and composite wood products that do not contain urea-formaldehyde resins.

C. Panel Products:  Any of the following:

Revise subparagraphs below to suit Project.

1. Particleboard made from wood particles[, with binder containing no urea-formaldehyde resin], complying with ANSI A208.1, Grade M-2.

Retain first subparagraph below and delete other subparagraphs if required for LEED-NC or LEED-CI Credit MR 6; verify availability of doors made with product in first subparagraph before deleting other subparagraphs.

2. Particleboard made from straw, complying with ANSI A208.1, Grade M-2, except for density.

3. Medium-density fiberboard made from wood fiber[, with binder containing no urea-formaldehyde resin], complying with ANSI A208.2, Grade 130.

4. Hardboard, complying with AHA A135.4.

5. Veneer core plywood[, made with adhesive containing no urea-formaldehyde resin].

2.2 EXTERIOR STILE AND RAIL WOOD DOORS

Retain first paragraph below if using manufacturers' stock exterior doors complying with WDMA I.S.6.

A. Exterior Stile and Rail Wood Doors[ Type SRD-<#>]:  Stock exterior doors complying with WDMA I.S.6, "Industry Standard for Wood Stile and Rail Doors," and with other requirements specified.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain one of first two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Manufacturers:  Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

2. Basis-of-Design Product:  Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

Many local woodwork firms produce stile and rail doors.  Insert local firms that produce suitable doors if required.

a. Belentry Doors LLC.

b. International Door and Latch.

c. Jeld-Wen, Inc.

d. Karona, Inc.

e. McPhillips Manufacturing Company.

f. QSM Doors, Inc.

g. Simpson Door Company.

h. <Insert manufacturer's name>.

3. Finish and Grade:  [Transparent and Premium or Select] [Opaque and Standard].

Options in first subparagraph below are examples only.  First option is suitable for transparent or opaque finish; second is only for opaque finish.  Insert other species only after verifying availability with manufacturers.

4. Wood Species:  [Idaho white, lodgepole, ponderosa, or sugar pine] [Manufacturer's standard softwood species and cut] <Insert species>.

Consider retaining first two subparagraphs below for minimal control of construction quality.

5. Stile and Rail Construction:  [Edge-glued solid lumber] [or] [veneered, structural composite lumber] [or] [veneered edge- and end-glued lumber].

6. Panel Construction:  [Edge-glued solid lumber] [or] [veneered panel product].

Revise first subparagraph below if using flat panels.  Thickness varies among design groups in WDMA I.S.6.  See Evaluations.

7. Raised-Panel Thickness:  [Manufacturer's standard, but not less than that required by WDMA I.S.6 for design group indicated] [As indicated].

8. Molding Profile (Sticking):  [Manufacturer's standard] [As selected by Architect from manufacturer's full range].

Options in first subparagraph below are examples only.  Revise if using another glass type or thickness.

9. Glass:  Uncoated, clear, [fully tempered float glass, 5.0 mm thick] [laminated glass made from two lites of 3.0-mm-thick annealed glass] [insulating-glass units made from two lites of 3.0-mm-thick, fully tempered glass with 1/4-inch (6.4-mm) interspace] complying with Division 08 Section "Glazing."

First subparagraph below can be deleted if designs are indicated on Drawings or in schedules.  WDMA design group and panel design designation can be replaced with a manufacturer's name and model number.

10. WDMA Design Group:  [1-3/4 Front Entrance Doors (Exterior)] [1-3/4 Thermal (Insulated-Glass) Doors (Exterior)] [8'-0" High Doors] [Side Lights] [1-3/4 and 1-3/8 Entrance Doors (Exterior)] [Combination Doors] [Screen Doors].

a. Panel Design:  <Insert WDMA designation>.

11. Mark, label, or otherwise identify stile and rail wood doors as complying with WDMA I.S.6 and grade specified.  Include panel design number if applicable.

Retain paragraph below if using exterior doors complying with AWI's "Architectural Woodwork Quality Standards," WI's "Manual of Millwork," or WDMA I.S.6A.  Retain one of last three options.  See Evaluations.  Review standard retained and coordinate its requirements with requirements retained.

B. Exterior Stile and Rail Wood Doors[ Type SRD-<#>]:  [Stock] [Custom] exterior doors complying with [AWI's "Architectural Woodwork Quality Standards,"] [WI's "Manual of Millwork,"] [WDMA I.S.6A, "Industry Standard for Architectural Stile and Rail Doors,"] and with other requirements specified.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain one of first two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Manufacturers:  Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

2. Basis-of-Design Product:  Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

Many local woodwork firms produce stile and rail doors.  Insert local firms that produce suitable doors if required.

a. Algoma Hardwoods, Inc.

b. Artistic Doors and Windows, Inc.

c. Belentry Doors LLC.

d. Buell Door Company.

e. Dimension Millworks.

f. Eggers Industries.

g. Enjo Architectural Millwork.

h. Harring Doors.

i. Ideal Architectural Doors & Plywood.

j. Maiman Company (The).

k. Marshfield DoorSystems, Inc.

l. McPhillips Manufacturing Company.

m. Pinecrest, Inc.

n. Select Interior Door, Ltd.

o. Sun-Dor-Co.

p. Woodtech Trading Company.

q. <Insert manufacturer's name>.

Retain first subparagraph below if panel designs are indicated on Drawings; delete if "Basis-of-Design Product" Subparagraph dictates panel design.

3. Panel Designs:  Indicated by Drawings.  Do not modify intended aesthetic effects, as judged solely by Architect, except with Architect's approval.  If modifications are proposed, submit comprehensive explanatory data to Architect for review.

4. Grade:  [Premium] [Custom].

5. Finish:  [Transparent] [Opaque].

Options in first subparagraph below are examples for transparent-finished doors.  Fourth option is an example for use where several species are required; if retaining, indicate species in a door schedule on Drawings or insert a schedule at the end of Part 3.

6. Wood Species and Cut for Transparent Finish:  [Idaho white, lodgepole, ponderosa, or sugar pine, plain sawed/sliced] [Douglas fir or western hemlock, quarter sawed/sliced (vertical grain)] [Red oak, quarter sawed/sliced stiles and rails, plain sawed/sliced panels] [Species indicated in schedule, plain sawed/sliced] <Insert species and cut>.

Insert provisions here for blueprint-matching doors with architectural wood work or wood paneling if matching is required.

First subparagraph below may be deleted if any construction allowed by the selected quality standard is acceptable.

7. Door Construction for Transparent Finish:

Retain stile and rail and panel construction in subparagraphs below.  Revise if using doors with flat panels.  Generally use solid-lumber construction only for softwoods or mahogany.  WDMA I.S.6A does not allow solid-lumber construction.  Note that matching requirements for veneered panels are included in referenced quality standards.

a. Stile and Rail Construction:  Clear lumber; may be edge glued for width.  Select lumber for similarity of grain and color, and arrange for optimum match between adjacent pieces.

b. Stile and Rail Construction:  Veneered, structural composite lumber[ or veneered, edge- and end-glued clear lumber].  Select veneers for similarity of grain and color, and arrange for optimum match between adjacent pieces.[  Use veneers not less than 1/16 inch (1.6 mm) thick.]

c. Raised-Panel Construction:  Clear lumber; edge glued for width.  Select lumber for similarity of grain and color, and arrange for optimum match between adjacent pieces.

First "Raised-Panel Construction" Subparagraph below is most expensive; third is least expensive but may not be available if doors are custom fabricated by a woodworking shop.

d. Raised-Panel Construction:  Edge-glued, clear lumber; glued to both sides of a wood-based panel product.  Select lumber for similarity of grain and color, and arrange for optimum match between adjacent pieces.

e. Raised-Panel Construction:  Veneered, wood-based panel product with mitered, raised rims made from matching clear lumber.

f. Raised-Panel Construction:  Veneered, shaped, wood-based panel product with veneer conforming to raised-panel shape.

First subparagraph below may be deleted if any construction allowed by the selected quality standard is acceptable.

8. Door Construction for Opaque Finish:

Retain stile and rail and panel construction in subparagraphs below.  WDMA I.S.6A does not allow solid-lumber construction.  Revise if using doors with flat panels.

a. Stile and Rail Construction:  Clear softwood; may be edge glued for width and finger jointed.

b. Stile and Rail Construction:  Veneered, structural composite lumber[ or veneered edge- and end-glued lumber].

c. Raised-Panel Construction:  Clear softwood lumber; edge glued for width.

d. Raised-Panel Construction:  Veneered, wood-based panel product.

9. Stile and Rail Widths:  [As indicated.] [Manufacturer's standard, but not less than the following:]

First two subparagraphs below are WI minimums; revise to suit Project.

a. Stiles, Top and Intermediate Rails:  5-3/8 inches (137 mm).

b. Bottom Rails:  11-3/8 inches (289 mm).

Retain one option in first subparagraph below; last option is AWI minimum for 1-3/4-inch (44-mm) doors.  Revise if using doors with flat panels.

10. Raised-Panel Thickness:  [As indicated] [1-3/4 inches (44 mm)] [1-3/8 inches (35 mm)] [Manufacturer's standard, but not less than 1-1/8 inches (29 mm)].

11. Molding Profile (Sticking):  [Bead and cove] [Ogee] [Ovalo] [Recessed bevel] [Recessed square] [Manufacturer's standard] [As selected by Architect from manufacturer's full range].

Options in first subparagraph below are examples only.

12. Glass:  Uncoated, clear, [fully tempered float glass, 5.0 mm thick] [laminated glass made from two lites of 3.0-mm-thick annealed glass] [insulating-glass units made from two lites of 3.0-mm-thick, fully tempered glass with 1/4-inch (6.4-mm) interspace], complying with Division 08 Section "Glazing."

Coordinate subparagraphs retained below with standard referenced in first paragraph of this article.

13. Provide AWI Quality Certification Labels or an AWI letter of licensing for Project indicating that doors comply with requirements of grades specified.

14. Provide WI-Certified Compliance Certificate indicating that doors comply with requirements of grades specified.

15. Mark, label, or otherwise identify stile and rail wood doors as complying with WDMA I.S.6A and grade specified.

2.3 INTERIOR STILE AND RAIL WOOD DOORS

Retain first paragraph below if using manufacturers' stock interior doors complying with WDMA I.S.6.

A. Interior Stile and Rail Wood Doors[ Type SRD-<#>]:  Stock interior doors complying with WDMA I.S.6, "Industry Standard for Wood Stile and Rail Doors," and with other requirements specified.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain one of first two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Manufacturers:  Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

2. Basis-of-Design Product:  Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

Many local woodwork firms produce stile and rail doors.  Insert local firms that produce suitable doors if required.

a. Belentry Doors LLC.

b. International Door and Latch.

c. Jeld-Wen, Inc.

d. Karona, Inc.

e. McPhillips Manufacturing Company.

f. QSM Doors, Inc.

g. Simpson Door Company.

h. <Insert manufacturer's name>.

3. Finish and Grade:  [Transparent and Premium or Select] [Opaque and Standard].

Options in first subparagraph below are examples only.  First three options are for transparent finish; fourth is for opaque finish.  Insert other species only after verifying availability with manufacturers.

4. Wood Species:  [Idaho white, lodgepole, ponderosa, or sugar pine] [Douglas fir or western hemlock, vertical sawed/sliced] [Red oak, quarter sawed/sliced] [Manufacturer's standard softwood species and cut] <Insert species>.

Consider retaining first subparagraph below, and possibly second and third subparagraphs, for minimal control of construction quality.

5. Stile and Rail Construction:  [Edge-glued solid lumber] [or] [veneered, structural composite lumber] [or] [veneered edge- and end-glued lumber].

First two options in first subparagraph below are suitable for either transparent or opaque finish; fourth is suitable only for opaque finish.

6. Raised-Panel Construction:  [Edge-glued solid lumber] [Veneered panel product] [or] [shaped, medium-density fiberboard].

First option in first subparagraph below is suitable for either transparent or opaque finish; third is suitable only for opaque finish.

7. Flat-Panel Construction:  [Veneered panel product] [or] [hardboard or medium-density fiberboard].

Retain one of first two subparagraphs below.

8. Raised-Panel Thickness:  [Manufacturer's standard, but not less than that required by WDMA I.S.6 for design group indicated] [As indicated].

9. Flat-Panel Thickness:  [Manufacturer's standard, but not less than that required by WDMA I.S.6 for design group indicated] [As indicated].

10. Molding Profile (Sticking):  [Manufacturer's standard] [As selected by Architect from manufacturer's full range].

Options in first subparagraph below are examples only.

11. Glass:  Uncoated, clear, [fully tempered float glass, 5.0 mm thick] [laminated glass made from two lites of 3.0-mm-thick annealed glass] complying with Division 08 Section "Glazing."

First subparagraph below can be deleted if designs are indicated on Drawings or in schedules.  WDMA design group and panel design designation can be replaced with a manufacturer's name and model number.

12. WDMA Design Group:  [1-3/8 Interior Panel Doors] [French Doors] [8'-0" High Doors] [Bifold Doors].

a. Panel Design:  <Insert WDMA designation>.

13. Mark, label, or otherwise identify stile and rail wood doors as complying with WDMA I.S.6 and grade specified.  Include panel design number if applicable.

Retain first paragraph below if using interior doors complying with AWI's "Architectural Woodwork Quality Standards," WI's "Manual of Millwork," or WDMA I.S.6A.  Retain one of last three options.  See Evaluations.  Review standard retained and coordinate its requirements with requirements retained.

B. Interior Stile and Rail Wood Doors[ Type SRD-<#>]:  [Stock] [Custom] interior doors complying with [AWI's "Architectural Woodwork Quality Standards,"] [WI's "Manual of Millwork,"] [WDMA I.S.6A, "Industry Standard for Architectural Stile and Rail Doors,"] and with other requirements specified.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain one of first two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Manufacturers:  Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

2. Basis-of-Design Product:  Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

Many local woodwork firms produce stile and rail doors.  Insert local firms that produce suitable doors if required.

a. Algoma Hardwoods, Inc.

b. Artistic Doors and Windows, Inc.

c. Belentry Doors LLC.

d. Buell Door Company.

e. Dimension Millworks.

f. Eggers Industries.

g. Enjo Architectural Millwork.

h. Harring Doors.

i. Ideal Architectural Doors & Plywood.

j. Maiman Company (The).

k. Marshfield DoorSystems, Inc.

l. McPhillips Manufacturing Company.

m. Pinecrest, Inc.

n. Select Interior Door, Ltd.

o. Sun-Dor-Co.

p. Woodtech Trading Company.

q. <Insert manufacturer's name>.

Retain first subparagraph below if panel designs are indicated on Drawings; delete if "Basis-of-Design Product" Subparagraph dictates panel design.

3. Panel Designs:  Indicated by Drawings.  Do not modify intended aesthetic effects, as judged solely by Architect, except with Architect's approval.  If modifications are proposed, submit comprehensive explanatory data to Architect for review.

4. Grade:  [Premium] [Custom].

5. Finish:  [Transparent] [Opaque].

Options in first subparagraph below are examples for transparent-finished doors.  Fourth option is an example for use where several species are required; if retaining, indicate species in a door schedule on Drawings or insert a schedule at the end of Part 3.

6. Wood Species and Cut for Transparent Finish:  [Idaho white, lodgepole, ponderosa, or sugar pine, plain sawed/sliced] [Douglas fir or western hemlock, quarter sawed/sliced (vertical grain)] [Red oak, quarter sawed/sliced stiles and rails, plain sawed/sliced panels] [Species indicated in schedule, plain sawed/sliced] <Insert species and cut>.

Insert provisions here for blueprint-matching doors with architectural wood work or wood paneling if matching is required.

First subparagraph below may be deleted if any construction allowed by the selected quality standard is acceptable.

7. Door Construction for Transparent Finish:

Retain stile and rail and panel construction in subparagraphs below.  Generally use solid-lumber construction only for softwoods or mahogany.  WDMA I.S.6A does not allow solid-lumber construction.  Note that matching requirements for veneered panels are included in referenced quality standards.

a. Stile and Rail Construction:  Clear lumber; may be edge glued for width.  Select lumber for similarity of grain and color, and arrange for optimum match between adjacent pieces.

b. Stile and Rail Construction:  Veneered, structural composite lumber[ or veneered, edge- and end-glued clear lumber].  Select veneers for similarity of grain and color, and arrange for optimum match between adjacent pieces.[  Use veneers not less than 1/16 inch (1.6 mm) thick.]

c. Raised-Panel Construction:  Clear lumber; edge glued for width.  Select lumber for similarity of grain and color, and arrange for optimum match between adjacent pieces.

First "Raised-Panel Construction" Subparagraph below is most expensive; third is least expensive but may not be available if doors are custom fabricated by a woodworking shop.

d. Raised-Panel Construction:  Edge-glued, clear lumber; glued to both sides of a wood-based panel product.  Select lumber for similarity of grain and color, and arrange for optimum match between adjacent pieces.

e. Raised-Panel Construction:  Veneered, wood-based panel product with mitered, raised rims made from matching clear lumber.

f. Raised-Panel Construction:  Veneered, shaped, wood-based panel product with veneer conforming to raised-panel shape.

g. Flat-Panel Construction:  Veneered, wood-based panel product.

First subparagraph below may be deleted if any construction allowed by the selected quality standard is acceptable.

8. Door Construction for Opaque Finish:

Retain stile and rail and panel construction in subparagraphs below.  WDMA I.S.6A does not allow solid-lumber construction.

a. Stile and Rail Construction:  Clear softwood; may be edge glued for width and finger jointed.

b. Stile and Rail Construction:  Veneered, structural composite lumber[ or veneered edge- and end-glued lumber].

c. Raised-Panel Construction:  Clear softwood lumber; edge glued for width.

d. Raised-Panel Construction:  Shaped, medium-density fiberboard.

e. Flat-Panel Construction:  [Veneered, wood-based panel product] [Medium-density fiberboard].

9. Stile and Rail Widths:  [As indicated.] [Manufacturer's standard, but not less than the following:]

First two subparagraphs below are WI minimums; revise to suit Project.

a. Stiles, Top and Intermediate Rails:  4-1/2 inches (114 mm).

b. Bottom Rails:  9 inches (229 mm).

Retain one option in first subparagraph below or delete subparagraph if no raised panels.  Last option is AWI minimum for Custom and Premium grades.

10. Raised-Panel Thickness:  [As indicated] [1-3/4 inches (44 mm)] [1-3/8 inches (35 mm)] [Manufacturer's standard, but not less than 1-1/8 inches (29 mm)] [Manufacturer's standard, but not less than 3/4 inch (19 mm)].

Retain one option in first subparagraph below or delete subparagraph if no flat panels.

11. Flat-Panel Thickness:  [As indicated] [1/2 inch (13 mm)] [3/8 inch (10 mm)] [1/4 inch (6.4 mm)].

12. Molding Profile (Sticking):  [Bead and cove] [Ogee] [Ovalo] [Recessed bevel] [Recessed square] [Manufacturer's standard] [As selected by Architect from manufacturer's full range].

Options in first subparagraph below are examples only.

13. Glass:  Uncoated, clear, [fully tempered float glass, 5.0 mm thick] [laminated glass made from two lites of 3.0-mm-thick annealed glass], complying with Division 08 Section "Glazing."

Coordinate subparagraphs retained below with standard referenced in first paragraph of this article.

14. Provide AWI Quality Certification Labels or an AWI letter of licensing for Project indicating that doors comply with requirements of grades specified.

15. Provide WI-Certified Compliance Certificate indicating that doors comply with requirements of grades specified.

16. Mark, label, or otherwise identify stile and rail wood doors as complying with WDMA I.S.6A and grade specified.

Retain first paragraph below if using interior fire-rated (20-minute rating) doors complying with AWI's "Architectural Woodwork Quality Standards" or WI's "Manual of Millwork."  Indicate door rating on Drawings or in schedules.

C. Interior Stile and Rail Wood Doors[ Type SRD-<#>]:  Fire-rated (20-minute rating) doors complying with [AWI's "Architectural Woodwork Quality Standards,"] [WI's "Manual of Millwork,"] [WDMA I.S.6A, "Industry Standard for Architectural Stile and Rail Doors,"] and with other requirements specified.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain one of first two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Manufacturers:  Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

2. Basis-of-Design Product:  Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

Many local woodwork firms produce stile and rail doors.  Insert local firms that produce suitable doors if required.

a. Algoma Hardwoods, Inc.

b. Artistic Doors and Windows, Inc.

c. Buell Door Company.

d. Dimension Millworks.

e. Eggers Industries.

f. Enjo Architectural Millwork.

g. Harring Doors.

h. Maiman Company (The).

i. Marshfield DoorSystems, Inc.

j. Pinecrest, Inc.

k. Select Interior Door, Ltd.

l. Sun-Dor-Co.

m. Woodtech Trading Company.

n. <Insert manufacturer's name>.

Retain first subparagraph below if panel designs are indicated on Drawings; delete if "Basis-of-Design Product" Subparagraph dictates panel design.

3. Panel Designs:  Indicated by Drawings.  Do not modify intended aesthetic effects, as judged solely by Architect, except with Architect's approval.  If modifications are proposed, submit comprehensive explanatory data to Architect for review.

4. Grade:  [Premium] [Custom].

5. Finish:  [Transparent] [Opaque].

Options in first subparagraph below are examples for transparent-finished doors.  Fourth option is an example for use where several species are required; if retaining, indicate species in door schedule on Drawings or insert a schedule at the end of Part 3.

6. Wood Species and Cut for Transparent Finish:  [Idaho white, lodgepole, ponderosa, or sugar pine, plain sawed/sliced] [Douglas fir or western hemlock, quarter sawed/sliced (vertical grain)] [Red oak, quarter sawed/sliced stiles and rails, plain sawed/sliced panels] [Species indicated in schedule, plain sawed/sliced] <Insert species and cut>.

Insert provisions here for blueprint-matching doors with architectural wood work or wood paneling if matching is required.

First subparagraph below may be deleted if any construction allowed by the selected quality standard and complying with requirements for fire-resistance rating is acceptable.

7. Door Construction for Transparent Finish:  1-3/4-inch- (44-mm-) thick stiles and rails and veneered [flat panels not less than 5/8 inch (16 mm) thick] [raised panels not less than 1-1/8 inches (29 mm) thick].

a. Stile and Rail Construction:  Veneered, structural composite lumber[ or veneered, edge- and end-glued clear lumber].  Select veneers for similarity of grain and color, and arrange for optimum match between adjacent pieces.[  Use veneers not less than 1/16 inch (1.6 mm) thick.]

b. Raised-Panel Construction:  Veneered, shaped, wood-based panel product with veneer conforming to raised-panel shape.

c. Flat-Panel Construction:  Veneered, wood-based panel product.

First subparagraph below may be deleted if any construction allowed by the selected quality standard and complying with requirements for fire-resistance rating is acceptable.

8. Door Construction for Opaque Finish:  1-3/4-inch- (44-mm-) thick stiles and rails and veneered [flat panels not less than 5/8 inch (16 mm) thick] [raised panels not less than 1-1/8 inches (29 mm) thick].

a. Stile and Rail Construction:  Veneered, structural composite lumber[ or veneered edge- and end-glued lumber].

b. Raised-Panel Construction:  Shaped, medium-density fiberboard.

c. Flat-Panel Construction:  [Veneered, wood-based panel product] [Medium-density fiberboard].

9. Stile and Rail Widths:  [As indicated.] [Manufacturer's standard, but not less than the following:]

First two subparagraphs below are WI minimums; revise to suit Project.

a. Stiles, Top and Intermediate Rails:  4-1/2 inches (114 mm).

b. Bottom Rails:  9 inches (229 mm).

10. Molding Profile (Sticking):  [Bead and cove] [Ogee] [Ovalo] [Recessed bevel] [Recessed square] [Manufacturer's standard] [As selected by Architect from manufacturer's full range].

Coordinate subparagraphs retained below with standard referenced in first paragraph of this article.

11. Provide AWI Quality Certification Labels or an AWI letter of licensing for Project indicating that doors comply with requirements of grades specified.

12. Provide WI-Certified Compliance Certificate indicating that doors comply with requirements of grades specified.

13. Mark, label, or otherwise identify stile and rail wood doors as complying with WDMA I.S.6A and grade specified.

Retain paragraph below if using interior fire-rated (45-minute rating) doors complying with AWI's "Architectural Woodwork Quality Standards" or WI's "Manual of Millwork."  Revise if doors with 60- or 90-minute ratings are required; verify availability with manufacturers selected.  Indicate door rating on Drawings or in schedules.

D. Interior Stile and Rail Wood Doors[ Type SRD-<#>]:  Fire-rated (45-minute rating) doors complying with [AWI's "Architectural Woodwork Quality Standards,"] [WI's "Manual of Millwork,"] and with other requirements specified.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain one of first two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Manufacturers:  Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

2. Basis-of-Design Product:  Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

Many local woodwork firms produce stile and rail doors.  Insert local firms that produce suitable doors if required.

a. Algoma Hardwoods, Inc.

b. Artistic Doors and Windows, Inc.

c. Buell Door Company.

d. Dimension Millworks.

e. Eggers Industries.

f. Enjo Architectural Millwork.

g. Harring Doors.

h. Maiman Company (The).

i. Marshfield DoorSystems, Inc.

j. Pinecrest, Inc.

k. Select Interior Door, Ltd.

l. Sun-Dor-Co.

m. Woodtech Trading Company.

n. <Insert manufacturer's name>.

Retain first subparagraph below if panel designs are indicated on Drawings; delete if "Basis-of-Design Product" Subparagraph dictates panel design.

3. Panel Designs:  Indicate by Drawings.  Do not modify intended aesthetic effects, as judged solely by Architect, except with Architect's approval.  If modifications are proposed, submit comprehensive explanatory data to Architect for review.

4. Grade:  [Premium] [Custom].

5. Finish:  [Transparent] [Opaque].

Options in first subparagraph below are examples for transparent-finished doors.  Fourth option is an example for use where several species are required; if retaining, indicate species in door schedule on Drawings or insert a schedule at the end of Part 3.

6. Wood Species and Cut for Transparent Finish:  [Idaho white, lodgepole, ponderosa, or sugar pine, plain sawed/sliced] [Douglas fir or western hemlock, quarter sawed/sliced (vertical grain)] [Red oak, quarter sawed/sliced stiles and rails, plain sawed/sliced panels] [Species indicated in schedule, plain sawed/sliced] <Insert species and cut>.

Insert provisions here for blueprint-matching doors with architectural wood work or wood paneling if matching is required.  Verify availability of matching for fire-rated doors before inserting requirements.

Verify panel thickness with manufacturers selected.  Indicate door rating on Drawings or in schedules.

7. Interior Fire-Rated Door Construction:  1-3/4-inch- (44-mm-) thick, edged and veneered mineral-core stiles and rails and 1-1/8-inch- (29-mm-) thick, veneered mineral-core raised panels.

8. Edge Construction:  At hinge stiles, provide laminated-edge construction with improved screw-holding capability and split resistance.  Comply with specified requirements for exposed edges.

Requirements in first subparagraph below are from WDMA I.S.1A, which is for flush wood doors.  Options are performance duty levels for Extra Heavy Duty, Heavy Duty, and Standard Duty, respectively.  Before retaining, verify that products of selected manufacturers comply with requirement selected.

a. Screw-Holding Capability:  [550 lbf (2440 N)] [475 lbf (2110 N)] [400 lbf (1780 N)] per NWWDA T.M.-10.

9. Stile and Rail Widths:  [As indicated.] [Manufacturer's standard, but not less than the following:]

First two subparagraphs below are WI minimums; revise to suit Project.

a. Stiles, Top and Intermediate Rails:  4-1/2 inches (114 mm).

b. Bottom Rails:  9 inches (229 mm).

10. Molding Profile (Sticking):  [Bead and cove] [Ogee] [Ovalo] [Recessed bevel] [Recessed square] [Manufacturer's standard] [As selected by Architect from manufacturer's full range].

Coordinate subparagraphs retained below with standard referenced in first paragraph of this article.

11. Provide AWI Quality Certification Labels or an AWI letter of licensing for Project indicating that doors comply with requirements of grades specified.

12. Provide WI-Certified Compliance Certificate indicating that doors comply with requirements of grades specified.

2.4 INTERIOR FIRE-RATED WOOD DOOR FRAMES

Products in this article primarily apply to office-suite entry doors that require only a 20-minute fire rating.  Steel frames trimmed with wood may be a more practical alternative where a wood appearance is desired and fire ratings longer than 20 minutes are required.

A. Interior Fire-Rated Wood Door Frames:  Frames, complete with[ sidelite frames and] casings, fabricated from solid fire-retardant-treated wood or from veneered fire-retardant particleboard, fire-retardant medium-density fiberboard, or mineral board.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain one of two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Manufacturers:  Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

2. Basis-of-Design Product:  Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

Manufacturers listed below make fire-rated wood door frames and fire-rated stile and rail wood doors; additional manufacturers of fire-rated wood door frames are listed in UL's "Building Equipment Directory" under Category Code GVTV; other manufacturers may also be listed by other agencies.

a. Algoma Hardwoods, Inc.

b. Eggers Industries.

c. Maiman Company (The).

d. Marshfield DoorSystems, Inc.

e. <Insert manufacturer's name>.

B. Species:  [Red oak] [White oak] [White maple] [Cherry] <Insert species>.

2.5 STILE AND RAIL WOOD DOOR FABRICATION

Retain one of first two paragraphs below.  Before retaining, verify availability of factory fitting with manufacturers selected.  Factory fitting is almost always done for custom doors, factory-finished doors, fire-rated doors, and doors hung in hollow-metal frames.  Wood frames sometimes have extended jambs that can be trimmed to required height so that doors fabricated in standard sizes can be used.  Field fitting allows doors to be more closely fitted at the bottom.

A. Fabricate stile and rail wood doors in sizes indicated for field fitting.

B. Factory fit doors to suit frame-opening sizes indicated, with the following uniform clearances and bevels unless otherwise indicated:

First subparagraph below describes typical prefit clearances; revise to suit office practice and for doors thicker than 1-3/4 inches (44 mm).

1. Clearances:  Provide 1/8 inch (3 mm) at heads, jambs, and between pairs of doors.  Provide 1/2 inch (13 mm) from bottom of door to top of decorative floor finish or covering.  Where threshold is shown or scheduled, provide not more than 3/8 inch (10 mm) from bottom of door to top of threshold.

a. Comply with NFPA 80 for fire-rated doors.

2. Bevel non-fire-rated doors 1/8 inch in 2 inches (3-1/2 degrees) at lock and hinge edges.

3. Bevel fire-rated doors 1/8 inch in 2 inches (3-1/2 degrees) on lock edge; trim stiles and rails only to extent permitted by labeling agency.

First paragraph below is applicable to doors of special design and construction, factory-finished doors, and doors hung in hollow-metal frames.  Before retaining, verify availability of factory machining with manufacturers selected.

C. Factory machine doors for hardware that is not surface applied.  Locate hardware to comply with DHI-WDHS-3.  Comply with final hardware schedules, door frame Shop Drawings, DHI A115-W Series standards, and hardware templates.

1. Coordinate measurements of hardware mortises in metal frames to verify dimensions and alignment before factory machining.

Retain one of first two paragraphs below.  Usually retain first and specify field glazing for custom doors made by a woodworking shop.  Usually retain second for stock doors and for custom doors made by door manufacturers.

D. Glazed Openings:  Trim openings indicated for glazing with solid wood moldings, with one side removable.  Miter wood moldings at corner joints.

E. Glazed Openings:  Glaze doors at factory with glass of type and thickness indicated, complying with Division 08 Section "Glazing." Install glass using manufacturer's standard elastomeric glazing sealant complying with ASTM C 920.  Secure glass in place with removable wood moldings.  Miter wood moldings at corner joints.

F. Transom and Side Panels:  Fabricate panels to match adjoining doors in materials, finish, and quality of construction.

G. Exterior Doors:  Factory treat exterior doors after fabrication with water-repellent preservative to comply with WDMA I.S.4.  Flash top of outswinging doors with manufacturer's standard metal flashing.

H. Prehung Doors:  Provide stile and rail doors as prehung units including doors, frames, [weather stripping, ]and hardware.

1. Provide wood door frames[, other than fire-rated wood door frames,] that comply with Division 06 Section "[Interior Finish Carpentry] [Interior Architectural Woodwork]."

2. Provide hardware[, including weather stripping and thresholds,] that complies with Division 08 Section "Door Hardware."

2.6 SHOP PRIMING

Usually retain this article if factory-finished or shop-finished doors are not required.  Factory fitting is recommended to minimize damage to shop-primed doors.  Retain one or both paragraphs below as applicable.

A. Doors for Opaque Finish:  Shop prime doors with one coat of wood primer specified in Division 09 Section "[Exterior Painting] [Interior Painting]." Seal all four edges, edges of cutouts, and mortises with primer.

B. Doors for Transparent Finish:  Shop prime doors with stain (if required), other required pretreatments, and first coat of finish as specified in Division 09 Section "Staining and Transparent Finishing." Seal all four edges, edges of cutouts, and mortises with first coat of finish.

2.7 FINISHING

Retain this article if factory or shop finishing is required.  Off-site finishing can be used to help comply with LEED-NC or LEED-CI Credit EQ 4.2, which limits VOC content of paints and coatings used within building.  Factory finishing also has other advantages.  See Evaluations.

Retain one of first three paragraphs below.  Revise if finishing is performed at another location, such as at woodworking shop.

A. Finish wood doors at [factory] [woodworking shop].

B. Finish wood doors at [factory] [woodworking shop] that are indicated to receive transparent finish.  Wood doors that are indicated to receive opaque finish may be field finished.

C. Finish wood doors at [factory] [woodworking shop] where indicated in schedules or on Drawings.  Wood doors that are not indicated to be [factory] [shop] finished may be field finished.

D. For doors indicated to be [factory] [shop] finished, comply with [AWI's "Architectural Woodwork Quality Standards,"] [WI's "Manual of Millwork,"] [WDMA I.S.6A, "Industry Standard for Architectural Stile and Rail Doors,"] and with other requirements specified.

1. Finish faces and all four edges of doors, including mortises and cutouts.  Stains and fillers may be omitted on[ top and] bottom edges, edges of cutouts, and mortises.

Both paragraphs below are examples only; revise to suit Project.  Verify availability with manufacturers selected.  Finish systems can vary among manufacturers; require Samples for verification.

E. Transparent Finish:

Usually retain same grade for finish as specified for doors.

1. Grade:  [Premium] [Custom].

Retain one of three "Finish" subparagraphs below and one or more options in subparagraph retained, or insert another option.  Before specifying, verify availability of finishes with manufacturers selected.

2. Finish:  [AWI conversion varnish] [or] [AWI catalyzed polyurethane] <Insert finish designation> system.

3. Finish:  [WDMA TR-4 conversion varnish] [or] [WDMA TR-6 catalyzed polyurethane] <Insert finish designation>.

4. Finish:  [WI System 4 clear conversion varnish] [WI System 5 catalyzed polyurethane] [or] [WI System 8 UV-curable coating] <Insert finish designation>.

5. Staining:  [Match Architect's sample] [As selected by Architect from manufacturer's full range] [None required].

Retain one of three options in last subparagraph above and usually one of three options in first subparagraph below.  Before retaining "Filled finish" option below, verify availability with manufacturers selected; filling is best done by hand, not on a finishing line.  Delete subparagraph below if using only closed-grain wood species.

6. Effect:  [Open-grain finish] [Filled finish] [Semifilled finish, produced by applying an additional finish coat to partially fill the wood pores].

Retain one of two options in subparagraph below or revise to suit Project.

7. Sheen:  [Satin] [Semigloss].

Verify availability of opaque finishes in paragraph below with manufacturers selected.

F. Opaque Finish:

Usually retain same grade for finish as specified for doors.

1. Grade:  [Premium] [Custom].

Retain one of three "Finish" subparagraphs below and one or more options in subparagraph retained, or insert another option.  Before specifying, verify availability of finishes with manufacturers selected.

2. Finish:  [AWI conversion varnish] [or] [AWI catalyzed polyurethane] <Insert finish designation> system.

3. Finish:  [WDMA OP-4 conversion varnish] [or] [WDMA OP-6 catalyzed polyurethane] <Insert finish designation>.

4. Finish:  [WI System 4 conversion varnish] [WI System 5 catalyzed polyurethane] [or] [WI System 8 UV-curable coating] <Insert finish designation>.

5. Color:  [Match Architect's sample] [As selected by Architect from manufacturer's full range].

Retain one of three options in subparagraph below or revise to suit Project.

6. Sheen:  [Satin] [Semigloss] [Gloss].

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine doors and substrates, with Installer present, for suitable conditions where wood stile and rail doors[ and fire-rated wood door frames] will be installed.

Delete first subparagraph below if all wood stile and rail doors are installed in fire-rated wood door frames specified in this Section.

1. Verify that installed frames comply with indicated requirements for type, size, location, and swing characteristics and have been installed with level heads and plumb jambs.

2. Reject doors with defects.

B. Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 INSTALLATION

Retain first paragraph below for fire-rated wood door frames.

A. Install fire-rated wood door frames level, plumb, true, and aligned with adjacent materials.  Use concealed shims where necessary for alignment.

1. Countersink fasteners, fill surface flush, and sand smooth.

B. Hardware:  For installation, see Division 08 Section "Door Hardware."

C. Install wood doors to comply with manufacturer's written instructions, [WDMA I.S.6, "Industry Standard for Wood Stile and Rail Doors,"] [AWI's "Architectural Woodwork Quality Standards,"] [WI's "Manual of Millwork,"] [WDMA I.S.6A, "Industry Standard for Architectural Stile and Rail Doors,"] and other requirements specified.

1. Provide WI-Certified Compliance Certificate for Installation.

2. Install fire-rated doors in corresponding fire-rated frames according to NFPA 80.

Retain first paragraph below if all doors are not factory fitted.

D. Field-Fitted Doors:  Align and fit doors in frames with uniform clearances and bevels as indicated below; do not trim stiles and rails in excess of limits set by manufacturer or permitted with fire-rated doors.  Machine doors for hardware.  Seal cut surfaces after fitting and machining.

Clearances in first subparagraph below are based on customary clearances for flush wood doors; revise to suit Project if required.

1. Clearances:  Provide 1/8 inch (3 mm) at heads, jambs, and between pairs of doors.  Provide [1/8 inch (3 mm)] [1/4 inch (6 mm)] [3/8 inch (10 mm)] [1/2 inch (13 mm)] from bottom of door to top of decorative floor finish or covering.  Where threshold is shown or scheduled, provide [1/4 inch (6 mm)] [3/8 inch (10 mm)] from bottom of door to top of threshold.

a. Comply with NFPA 80 for fire-rated doors.

2. Bevel non-fire-rated doors 1/8 inch in 2 inches (3-1/2 degrees) at lock and hinge edges.

Subparagraph above is standard bevel; revise to suit Project if required.  See Evaluations.  Retain subparagraph below for fire-rated doors or if not factory fitted.  Fire-rated doors with more than 20-minute rating can only be trimmed to a limited extent because of narrow wood edges of stiles and rails.

3. Bevel fire-rated doors 1/8 inch in 2 inches (3-1/2 degrees) on lock edge; trim stiles and rails only to extent permitted by labeling agency.

E. Factory-Fitted Doors:  Align in frames for uniform clearance at each edge.

F. [Factory] [Shop]-Finished Doors:  Restore finish before installation if fitting or machining is required at Project site.

3.3 ADJUSTING

A. Operation:  Rehang or replace doors that do not swing or operate freely.

B. Finished Doors:  Replace doors that are damaged or do not comply with requirements.  Doors may be repaired or refinished if Work complies with requirements and shows no evidence of repair or refinishing.

END OF SECTION 081433

	STILE AND RAIL WOOD DOORS
	081433 - 1



