Copyright 2005 AIA
MASTERSPEC Full Length
05/05 (R 05/06)

Copyright 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 096519 - RESILIENT TILE FLOORING
Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

A. Section Includes:

1. Solid vinyl floor tile.

2. Rubber floor tile.

3. Vinyl composition floor tile.

4. Resilient terrazzo floor tile.

B. Related Sections:

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.

1. Division 09 Section "Resilient Base and Accessories" for resilient base, reducer strips, and other accessories installed with resilient floor coverings.

2. Division 09 Section "Resilient Sheet Flooring" for resilient sheet floor coverings.

3. Division 09 Section "Linoleum Flooring" for linoleum floor coverings.

4. Division 09 Section "Static-Control Resilient Flooring" for resilient floor coverings designed to control electrostatic discharge.

5. Division 09 Section "Resilient Athletic Flooring" for resilient floor coverings for use in athletic-activity or support areas.

1.3 SUBMITTALS

First seven paragraphs below are defined in Division 01 Section "Submittal Procedures" as "Action Submittals."

A. Product Data:  For each type of product indicated.

B. LEED Submittals:

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1; coordinate with requirements selected in Part 2 for adhesives, sealants, and chemical-bonding compounds.

1. Product Data for Credit EQ 4.1:  For [adhesives] [sealants] [and] [chemical-bonding compounds], including printed statement of VOC content.

Retain first paragraph below if required.

C. Shop Drawings:  For each type of floor tile.  Include floor tile layouts, edges, columns, doorways, enclosing partitions, built-in furniture, cabinets, and cutouts.

1. Show details of special patterns.

D. Samples for Initial Selection:  For each type of floor tile indicated.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled.  Retain first paragraph below with or without above.

E. Samples for Verification:  Full-size units of each color and pattern of floor tile required.

1. For heat-welding bead, manufacturer's standard-size Samples, but not less than [9 inches (230 mm)] <Insert dimension> long, of each color required.

Floor tile is sometimes specified for seamless installation.  Retain first paragraph below for heat-welded or chemically bonded seams.

F. Seam Samples:  For seamless-installation technique indicated and for each flooring product, color, and pattern required; with seam running lengthwise and in center of [6-by-9-inch (150-by-230-mm)] <Insert size> Sample applied to a rigid backing and prepared by Installer for this Project.

G. Product Schedule:  For floor tile.[  Use same designations indicated on Drawings.]

Remaining paragraphs are defined in Division 01 Section "Submittal Procedures" as "Informational Submittals."

Coordinate first paragraph below with qualification requirements in Division 01 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

H. Qualification Data:  For qualified Installer.

I. Maintenance Data:  For each type of floor tile to include in maintenance manuals.

1.4 QUALITY ASSURANCE

Retain option in first paragraph below for heat-welded or chemically bonded seams.

A. Installer Qualifications:  A qualified installer who employs workers for this Project who are competent in techniques required by manufacturer for floor tile installation[ and seaming method] indicated.

Not all manufacturers train or certify installers.  Before retaining subparagraph below, verify availability with manufacturers selected; retain with "Qualification Data" Paragraph in "Submittals" Article.

1. Engage an installer who employs workers for this Project who are trained or certified by manufacturer for installation techniques required.

Delete first paragraph below if fire-test-response testing is not required by authorities having jurisdiction.  In most building codes, floor tile is exempt from fire-test-response requirements.  See "Fire-Test-Response Characteristics" Article in the Evaluations in Division 09 Section "Resilient Flooring" for additional information.

B. Fire-Test-Response Characteristics:  As determined by testing identical products according to ASTM E 648 or NFPA 253 by a qualified testing agency.

1. Critical Radiant Flux Classification:  Class I, not less than 0.45 W/sq. cm.

C. Mockups:  Build mockups to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

1. Build mockups for floor tile including[ resilient base and] accessories.

a. Size:  Minimum 100 sq. ft. (9.3 sq. m) for each type, color, and pattern [in locations indicated] [in locations directed by Architect] <Insert location requirements>.

1.5 DELIVERY, STORAGE, AND HANDLING

A. Store floor tile and installation materials in dry spaces protected from the weather, with ambient temperatures maintained within range recommended by manufacturer, but not less than 50 deg F (10 deg C) or more than 90 deg F (32 deg C).  Store floor tiles on flat surfaces.

1.6 PROJECT CONDITIONS

Ambient temperature range for installation varies among manufacturers.  Consult manufacturers for recommendations and revise first paragraph below to suit Project.

A. Maintain ambient temperatures within range recommended by manufacturer, but not less than [70 deg F (21 deg C)] <Insert temperature> or more than [95 deg F (35 deg C)] <Insert temperature>, in spaces to receive floor tile during the following time periods:

1. 48 hours before installation.

2. During installation.

3. 48 hours after installation.

B. Until Substantial Completion, maintain ambient temperatures within range recommended by manufacturer, but not less than [55 deg F (13 deg C)] <Insert temperature> or more than [95 deg F (35 deg C)] <Insert temperature>.

C. Close spaces to traffic during floor tile installation.

D. Close spaces to traffic for 48 hours after floor tile installation.

E. Install floor tile after other finishing operations, including painting, have been completed.

1.7 EXTRA MATERIALS

A. Furnish extra materials that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

Revise subparagraph below to suit Project.

1. Floor Tile:  Furnish 1 box for every [50] <Insert number> boxes or fraction thereof, of each type, color, and pattern of floor tile installed.

PART 2 -  PRODUCTS

2.1 SOLID VINYL FLOOR TILE <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

See Editing Instruction No. 1 in the Evaluations in Division 09 Section "Resilient Flooring" for cautions about naming manufacturers and products.  See Division 01 Section "Product Requirements."

A. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1. Altro Group; <Insert product name or designation>.

2. Amtico Studio (The), Amtico International Inc.; <Insert product name or designation>.

3. Armstrong World Industries, Inc.; <Insert product name or designation>.

4. Burke Mercer Flooring Products, Division of Burke Industries Inc.; <Insert product name or designation>.

5. Estrie Products International, American Biltrite (Canada) Ltd.; <Insert product name or designation>.

6. Flexco; <Insert product name or designation>.

7. Gemtec Inc.; <Insert product name or designation>.

8. Gerflor, Architectural Floor Systems, Inc.; <Insert product name or designation>.

9. Johnsonite; <Insert product name or designation>.

10. Polyflor, Ltd., Distributed by Gerbert Limited; <Insert product name or designation>.

11. Roppe Corporation, USA; <Insert product name or designation>.

12. Tarkett, Inc.; <Insert product name or designation>.

13. TOLI International; <Insert product name or designation>.

14. VPI, LLC, Floor Products Division; <Insert product name or designation>.

15. <Insert manufacturer's name; product name or designation>.

B. Tile Standard:  ASTM F 1700.

1. Class:  [As indicated by product designations] [Class I, monolithic vinyl tile] [Class II, surface-decorated vinyl tile] [Class III, printed film vinyl tile].

2. Type:  [Type A, smooth surface] [Type B, embossed surface].

C. Thickness:  [0.080 inch (2.0 mm)] [0.100 inch (2.5 mm)] [0.120 inch (3.0 mm)] [0.125 inch (3.2 mm)] <Insert thickness>.

D. Size:  [12 by 12 inches (305 by 305 mm)] [18 by 18 inches (457 by 457 mm)] [24 by 24 inches (610 by 610 mm)] [36 by 36 inches (914 by 914 mm)] [3 by 36 inches (76 by 914 mm)] <Insert size>.

Revise first paragraph below to suit Project.  Generally, only some large-size tiles can be heat welded or chemically bonded.  See "General Comments" Article in the Evaluations in Division 09 Section "Resilient Flooring" for a discussion of seamless-installation techniques.

E. Seaming Method:  [Heat welded] [Chemically bonded] [Standard] <Insert requirements>.

Retain paragraph below if colors and patterns are not indicated in a separate schedule.

F. Colors and Patterns:  [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from full range of industry colors].

2.2 RUBBER FLOOR TILE <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

See Editing Instruction No. 1 in the Evaluations in Division 09 Section "Resilient Flooring" for cautions about naming manufacturers and products.  See Division 01 Section "Product Requirements."

A. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1. Burke Mercer Flooring Products, Division of Burke Industries Inc.; <Insert product name or designation>.

2. Endura Rubber Flooring, a division of Burke Industries Inc.; <Insert product name or designation>.

3. Estrie Products International, American Biltrite (Canada) Ltd.; <Insert product name or designation>.

4. Flexco; <Insert product name or designation>.

5. Johnsonite; <Insert product name or designation>.

6. Mondo Rubber International, Inc.; <Insert product name or designation>.

7. Nora Rubber Flooring, Freudenberg Building Systems, Inc.; <Insert product name or designation>.

8. PRF USA Inc.; <Insert product name or designation>.

9. R.C.A. Rubber Company (The); <Insert product name or designation>.

10. Roppe Corporation, USA; <Insert product name or designation>.

11. <Insert manufacturer's name; product name or designation>.

B. Tile Standard:  ASTM F 1344, [Class I-A, homogeneous rubber tile, solid color] [Class I-B, homogeneous rubber tile, through mottled] [Class II-A, laminated rubber tile, solid-color wear layer] [Class II-B, laminated rubber tile, mottled wear layer].

See "Rubber Floor Tile" Article in the Evaluations in Division 09 Section "Resilient Flooring" for a discussion of hardness values.

C. Hardness:  [Not less than 85 as required by ASTM F 1344, measured using Shore, Type A durometer per ASTM D 2240] [Manufacturer's standard hardness].

D. Wearing Surface:  [Smooth] [Textured] [Molded pattern].

1. Molded-Pattern Figure:  [Raised discs] [Raised squares] <Insert pattern>.

For molded-pattern (raised-pattern) rubber tile, overall thickness is generally measured at the thickest cross-sectional area of the flooring product.  Revise first paragraph below to include overall thickness for molded-pattern rubber tile.

E. Thickness:  [0.125 inch (3.2 mm)] <Insert thickness>.

F. Size:  [12 by 12 inches (305 by 305 mm)] [24 by 24 inches (610 by 610 mm)] <Insert size>.

Revise first paragraph below to suit Project.  Generally, only some large-size tiles can be heat welded or chemically bonded.  See "General Comments" Article in the Evaluations in Division 09 Section "Resilient Flooring" for a discussion of seamless-installation techniques.

G. Seaming Method:  [Heat welded] [Chemically bonded] [Standard] <Insert requirements>.

Retain paragraph below if colors and patterns are not indicated in a separate schedule.

H. Colors and Patterns:  [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from full range of industry colors].

Several manufacturers offer product selections with seamless installation.  Insert requirements here for heat-welded or other seamless treatment if required by Project.

2.3 VINYL COMPOSITION FLOOR TILE <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

See Editing Instruction No. 1 in the Evaluations in Division 09 Section "Resilient Flooring" for cautions about naming manufacturers and products.  See Division 01 Section "Product Requirements."

A. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1. AB ColorPlus, American Biltrite (Canada) Ltd.; <Insert product name or designation>.

2. Armstrong World Industries, Inc.; <Insert product name or designation>.

3. Congoleum Corporation; <Insert product name or designation>.

4. Mannington Mills, Inc.; <Insert product name or designation>.

5. Tarkett, Inc.; <Insert product name or designation>.

6. Vinylasa Tile, Distributed by American Tile Inc.; <Insert product name or designation>.

7. <Insert manufacturer's name; product name or designation>.

B. Tile Standard:  ASTM F 1066, [Class 1, solid-color tile] [Class 2, through-pattern tile] [Class 3, surface-pattern tile].

C. Wearing Surface:  [Smooth] [Embossed].

A limited number of products are available in 3/32- and 3/16-inch (2.4- and 4.8-mm) thicknesses; if applicable, insert in first paragraph below.

D. Thickness:  [0.125 inch (3.2 mm)] <Insert thickness>.

E. Size:  12 by 12 inches (305 by 305 mm).

Retain paragraph below if colors and patterns are not indicated in a separate schedule.

F. Colors and Patterns:  [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from full range of industry colors].

2.4 RESILIENT TERRAZZO FLOOR TILE <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

A. Resilient Terrazzo Floor Tile:  Marble or granite chips embedded in flexible, thermoset-polyester-resin matrix; electrically nonconductive and chemical, oil, and corrosion resistive, with smooth wearing surface and manufacturer's standard factory-applied, protective urethane coating.

See Editing Instruction No. 1 in the Evaluations in Division 09 Section "Resilient Flooring" for cautions about naming manufacturers and products.  See Division 01 Section "Product Requirements."

1. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Fritz Industries; <Insert product name or designation>.

b. <Insert manufacturer's name; product name or designation>.

B. Thickness:  [1/8 inch (3.0 mm)] [3/16 inch (4.8 mm)].

C. Size:  12 by 12 inches (305 by 305 mm).

D. Performance Characteristics:

1. Compressive Strength:  2900 to 5000 psi (20 to 34.5 MPa), ASTM C 109/C 109M or ASTM D 695.

2. Abrasion Resistance:  Maximum 0.0196 cubic centimeters volume loss, ASTM F 510, Taber abrader, S-39 wheels, at 500 cycles with 1000-gram load.

3. Static Load Limit:  0.0007-inch (0.0177-mm) maximum indentation, ASTM F 970 at 125 lb (57 kg).

4. Resin Matrix Hardness:  Not less than 78, as measured using Shore, Type D durometer per ASTM D 2240.

Retain paragraph below if colors and patterns are not indicated in a separate schedule.

E. Colors and Patterns:  [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from full range of industry colors].

2.5 INSTALLATION MATERIALS

A. Trowelable Leveling and Patching Compounds:  Latex-modified, portland cement based or blended hydraulic-cement-based formulation provided or approved by manufacturer for applications indicated.

B. Adhesives:  Water-resistant type recommended by manufacturer to suit floor tile and substrate conditions indicated.

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.

1. Use adhesives that comply with the following limits for VOC content when calculated according to 40 CFR 59, Subpart D (EPA Method 24):

LEED establishes no VOC limitation for resilient terrazzo floor tiles; revise if extending VOC limits to this floor tile type.

a. VCT and Asphalt Tile Adhesives:  Not more than 50 g/L.

b. Rubber Floor Adhesives:  Not more than 60 g/L.

C. Seamless-Installation Accessories:

1. Heat-Welding Bead:  Manufacturer's solid-strand product for heat welding seams.

a. Color:  [As selected by Architect from manufacturer's full range to contrast with floor tile] [Match floor tile] <Insert color>.

2. Chemical-Bonding Compound:  Manufacturer's product for chemically bonding seams.

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.  VOC limits are those for plastic cement welding compounds and PVC welding compounds, respectively.

a. Use chemical-bonding compound that has a VOC content of [350] [510] <Insert value> g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

Retain first paragraph below for use with most vinyl composition floor tile and some solid vinyl floor tile.  Liquid floor polish is generally used instead of paste wax.  See "Maintenance Procedures" Article in the Evaluations in Division 09 Section "Resilient Flooring" for additional information.

D. Floor Polish:  Provide protective liquid floor polish products as recommended by manufacturer.

Retain both paragraphs below for resilient terrazzo floor tile.

E. Joint Sealant for Resilient Terrazzo Floor Tile:  Silicone sealant of type and grade as recommended in writing by manufacturer to suit resilient terrazzo floor tile.

Retain first subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.

1. Use sealant that has a VOC content of not more than 250 g/L when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

2. Joint-Sealant Color:  [White] [As selected by Architect from manufacturer's full range to match floor tile] [Match floor tile] <Insert color>.

F. Sealers and Finish Coats for Resilient Terrazzo Floor Tile:  Premium-type products as recommended by manufacturer for resilient terrazzo floor tile.

PART 3 -  EXECUTION

3.1 EXAMINATION

Coordinate requirements specified in other Sections for subfloor construction and tolerances to ensure that they are appropriate for floor tile selected.

A. Examine substrates, with Installer present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

B. Verify that finishes of substrates comply with tolerances and other requirements specified in other Sections and that substrates are free of cracks, ridges, depressions, scale, and foreign deposits that might interfere with adhesion of floor tile.

C. Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 PREPARATION

Extensive surface preparation is required over substrates from which existing products have been removed.  Requirements vary among manufacturers.  Insert requirements to suit Project.

A. Prepare substrates according to manufacturer's written instructions to ensure adhesion of resilient products.

B. Concrete Substrates:  Prepare according to ASTM F 710.

1. Verify that substrates are dry and free of curing compounds, sealers, and hardeners.

2. Remove substrate coatings and other substances that are incompatible with adhesives and that contain soap, wax, oil, or silicone, using mechanical methods recommended by manufacturer.  Do not use solvents.

3. Alkalinity and Adhesion Testing:  Perform tests recommended by manufacturer.  Proceed with installation only after substrates pass testing.

4. Moisture Testing:  Perform tests recommended by manufacturer[ and as follows].  Proceed with installation only after substrates pass testing.

Follow manufacturer's requirements for moisture testing.  Retain one or both subparagraphs below.

a. Perform anhydrous calcium chloride test, ASTM F 1869.  Proceed with installation only after substrates have maximum moisture-vapor-emission rate of [3 lb of water/1000 sq. ft. (1.36 kg of water/92.9 sq. m)] <Insert emission> in 24 hours.

b. Perform relative humidity test using in situ probes, ASTM F 2170.  Proceed with installation only after substrates have a maximum [75%] <Insert acceptable percentage> relative humidity level measurement.

Retain first paragraph below for floor tile installed on access flooring.

C. Access Flooring Panels:  Remove protective film of oil or other coating using method recommended by access flooring manufacturer.

D. Fill cracks, holes, and depressions in substrates with trowelable leveling and patching compound and remove bumps and ridges to produce a uniform and smooth substrate.

E. Do not install floor tiles until they are same temperature as space where they are to be installed.

1. Move resilient products and installation materials into spaces where they will be installed at least 48 hours in advance of installation.

F. Sweep and vacuum clean substrates to be covered by resilient products immediately before installation.

3.3 FLOOR TILE INSTALLATION

A. Comply with manufacturer's written instructions for installing floor tile.

B. Lay out floor tiles from center marks established with principal walls, discounting minor offsets, so tiles at opposite edges of room are of equal width.  Adjust as necessary to avoid using cut widths that equal less than one-half tile at perimeter.

1. Lay tiles [square with room axis] [at a 45-degree angle with room axis] [in pattern indicated] <Insert requirements>.

C. Match floor tiles for color and pattern by selecting tiles from cartons in the same sequence as manufactured and packaged, if so numbered.  Discard broken, cracked, chipped, or deformed tiles.

1. Lay tiles [with grain running in one direction] [with grain direction alternating in adjacent tiles (basket-weave pattern)] [in pattern of colors and sizes indicated].

If built-in items are required to be set on top of tile, indicate on Drawings and revise first paragraph below.

D. Scribe, cut, and fit floor tiles to butt neatly and tightly to vertical surfaces and permanent fixtures including built-in furniture, cabinets, pipes, outlets, and door frames.

E. Extend floor tiles into toe spaces, door reveals, closets, and similar openings.  Extend floor tiles to center of door openings.

F. Maintain reference markers, holes, and openings that are in place or marked for future cutting by repeating on floor tiles as marked on substrates.  Use chalk or other nonpermanent, nonstaining marking device.

Retain first paragraph below for tile installed on covers.

G. Install floor tiles on covers for telephone and electrical ducts, building expansion-joint covers, and similar items in finished floor areas.  Maintain overall continuity of color and pattern between pieces of tile installed on covers and adjoining tiles.  Tightly adhere tile edges to substrates that abut covers and to cover perimeters.

Revise first paragraph below if other-than-full-spread adhesive method is recommended by manufacturer for substrate and tile products selected.

H. Adhere floor tiles to flooring substrates using a full spread of adhesive applied to substrate to produce a completed installation without open cracks, voids, raising and puckering at joints, telegraphing of adhesive spreader marks, and other surface imperfections.

Retain paragraph below if seamless installation is required.

I. Seamless Installation:

1. Heat-Welded Seams:  Comply with ASTM F 1516.  Rout joints and heat weld with welding bead to permanently fuse sections into a seamless floor covering.  Prepare, weld, and finish seams to produce surfaces flush with adjoining floor covering surfaces.

2. Chemically Bonded Seams:  Bond seams with chemical-bonding compound to permanently fuse sections into a seamless floor covering.  Prepare seams and apply compound to produce tightly fitted seams without gaps, overlays, or excess bonding compound on floor covering surfaces.

3.4 CLEANING AND PROTECTION

A. Comply with manufacturer's written instructions for cleaning and protection of floor tile.

B. Perform the following operations immediately after completing floor tile installation:

1. Remove adhesive and other blemishes from exposed surfaces.

2. Sweep and vacuum surfaces thoroughly.

3. Damp-mop surfaces to remove marks and soil.

C. Protect floor tile products from mars, marks, indentations, and other damage from construction operations and placement of equipment and fixtures during remainder of construction period.

Before retaining first paragraph below, verify manufacturer's floor polish recommendations.  Floor polish is used with most vinyl composition floor tile and some solid vinyl floor tile.

D. Floor Polish:  Remove soil, visible adhesive, and surface blemishes from floor tile surfaces before applying liquid floor polish.

Revise subparagraph below to suit products selected.

1. Apply [one] [two] [three] <Insert requirements> coat(s).

Retain first two paragraphs below for resilient terrazzo floor tile.

E. Joint Sealant:  Apply sealant to resilient terrazzo floor tile perimeter and around columns, at door frames, and at other joints and penetrations.

F. Sealers and Finish Coats:  Remove soil, visible adhesive, and surface blemishes from resilient terrazzo floor tile surfaces before applying liquid cleaners, sealers, and finish products.

1. Sealer:  Apply two base coats of liquid sealer.

2. Finish:  Apply [two] [three] <Insert requirements> coats of liquid floor finish.

G. Cover floor tile until Substantial Completion.

END OF SECTION 096519

RESILIENT TILE FLOORING
096519 - 1

