Copyright 2004 and 2005 AIA
MASTERSPEC Full Length
11/04 (R 05/06)

Copyright 2004 and 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 096623 - RESINOUS MATRIX TERRAZZO FLOORING
Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

A. Section Includes:

1. Thin-set epoxy-resin terrazzo flooring[ and base].

2. Precast terrazzo units.

B. Related Section:

Retain subparagraph below for requirements that Contractor might expect to find in this Section but are specified in other Sections; retain for sealants installed in movement joints or in joints between precast terrazzo units.

1. Division 07 Section "Joint Sealants" for sealants installed with terrazzo.

Allowances are sometimes used for special terrazzo patterns.  If allowances apply to Work of this Section, insert brief paragraph here to alert Contractor and reference appropriate Division 01 Section for specific details.

1.3 SUBMITTALS

First five paragraphs below are defined in Division 01 Section "Submittal Procedures" as "Action Submittals."

A. Product Data:  For each type of product indicated.

B. LEED Submittals:

Retain first subparagraph below if recycled content is required for LEED-NC or LEED-CI Credits MR 4.1 and MR 4.2; coordinate with requirements selected in Part 2 for granular materials.

1. Product Data for Credit MR 4.1[ and Credit MR 4.2]: For [marble chips,] [aggregates,] documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a. Include statement that indicates cost for each product having recycled content.

Retain subparagraph below if low-emitting materials used on the interior of the building are required for LEED-NC or LEED-CI Credit EQ 4.1; coordinate with requirements selected in Part 2 for adhesives.

2. Product Data for Credit EQ 4.1:  For adhesives, including printed statement of VOC content.

C. Shop Drawings:  Include terrazzo installation requirements.  Include plans, elevations, sections, component details, and attachments to other work.  Show layout of the following:

1. Divider strips.

2. Control-joint strips.

3. Accessory strips.

4. Abrasive strips.

5. Stair treads, risers, and landings.

6. Precast terrazzo jointing and edge configurations.

7. Terrazzo patterns.

8. <Insert requirements>.

D. Samples for Initial Selection:  [NTMA] [Manufacturer's] color plates showing the full range of colors and patterns available for each terrazzo type indicated.

Delete "Samples for Initial Selection" Paragraph above if colors, patterns, and other characteristics are preselected and specified or scheduled.  Retain first paragraph below with or without above.

E. Samples for Verification:  For each type, material, color, and pattern of terrazzo and accessory required showing the full range of color, texture, and pattern variations expected.  Label each terrazzo sample to identify manufacturer's matrix color and [marble-chip] [aggregate] types, sizes, and proportions.  Prepare samples of same thickness and from same material to be used for the Work in size indicated below:

1. Terrazzo:  [6-inch- (150-mm-)] <Insert size> square Samples.

2. Precast Terrazzo:  [6-inch- (150-mm-)] <Insert size> square Samples.

3. Accessories:  [6-inch- (150-mm-)] <Insert size> long Samples of each exposed strip item required.

Remaining paragraphs are defined in Division 01 Section "Submittal Procedures" as "Informational Submittals."

Retain first paragraph below if Installer certification is required in "Quality Assurance" Article.

F. Installer Certificates:  Signed by manufacturers certifying that installers comply with requirements.

Coordinate first paragraph below with qualification requirements in Division 01 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

G. Qualification Data:  For qualified Installer.

Retain first paragraph below for material or product certificates from manufacturers.

H. Material Certificates:  For each type of terrazzo material or product, from manufacturer.

NTMA publishes recommendations for minimum maintenance-program requirements.

I. Maintenance Data:  For terrazzo to include in maintenance manuals.

1.4 QUALITY ASSURANCE

A. Installer Qualifications:  A qualified installer who is acceptable to terrazzo manufacturer to install manufacturer's products.

If applicable for manufacturers selected, retain first subparagraph below with "Installer Certificates" Paragraph in "Submittals" Article.  See "Installer Considerations" Article in the Evaluations in Division 09 Section "Terrazzo Flooring."

1. Engage an installer who is certified in writing by terrazzo manufacturer as qualified to install manufacturer's products.

If applicable for Project location and if contractor membership is desired, retain subparagraph below.

2. Engage an installer who is a contractor member of NTMA.

B. Source Limitations:  Obtain primary terrazzo materials from one source from a single manufacturer.  Provide secondary materials including patching and fill material, joint sealant, and repair materials of type and from source recommended by manufacturer of primary materials.

C. Source Limitations for [Marble Chips] [Aggregates]:  Obtain each color, grade, type, and variety of granular materials from one source with resources to provide materials of consistent quality in appearance and physical properties.

D. NTMA Standards:  Comply with NTMA's "Terrazzo Specifications and Design Guide" and with written recommendations for terrazzo type indicated unless more stringent requirements are specified.

E. Mockups:  Build mockups to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

1. Build mockups for terrazzo including accessories.

a. Size:  Minimum 100 sq. ft. (9 sq. m) of typical poured-in-place flooring[ and base] condition for each color and pattern [in locations indicated] [in locations directed by Architect] <Insert location requirements>.

Insert mockup requirements for precast terrazzo units if any.

Retain subparagraph below if mockups are installed as part of building rather than erected separately and the intention is to make an exception to the default requirement in Division 01 Section "Quality Requirements" for demolishing and removing mockups when directed unless otherwise indicated.

2. Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Retain paragraph below if Work of this Section is extensive or complex enough to justify a preinstallation conference.

F. Preinstallation Conference:  Conduct conference at [Project site] <Insert location>.

Retain subparagraph below if additional requirements are necessary; include information about conference.

1. Review methods and procedures related to terrazzo including, but not limited to, the following:

a. Inspect and discuss condition of substrate and other preparatory work performed by other trades.

b. Review and finalize construction schedule and verify availability of materials, Installer's personnel, equipment, and facilities needed to make progress and avoid delays.

c. Review special terrazzo designs and patterns.

d. Review dust-control procedures.

e. <Insert agenda items>.

If needed, insert list of conference participants not mentioned in Division 01 Section "Project Management and Coordination."

1.5 DELIVERY, STORAGE, AND HANDLING

A. Deliver materials to Project site in supplier's original wrappings and containers, labeled with source's or manufacturer's name, material or product brand name, and lot number if any.

B. Store materials in their original, undamaged packages and containers, inside a well-ventilated area protected from weather, moisture, soiling, extreme temperatures, and humidity.

1.6 PROJECT CONDITIONS

Epoxy-resin terrazzo is generally used at interior locations because ground terrazzo is often too smooth or slippery for exterior use.  Also, epoxy-resin matrices tend to yellow when exposed to sunlight.

A. Environmental Limitations:  Comply with manufacturer's written instructions for substrate temperature, ambient temperature, moisture, ventilation, and other conditions affecting terrazzo installation.

Retain first paragraph below for precast terrazzo.

B. Field Measurements:  Verify actual dimensions of construction contiguous with precast terrazzo by field measurements before fabrication.

C. Provide permanent lighting or, if permanent lighting is not in place, simulate permanent lighting conditions during terrazzo installation.

D. Close spaces to traffic during terrazzo application and for not less than 24 hours after application unless manufacturer recommends a longer period.

E. Control and collect dust produced by grinding operations.  Protect adjacent construction from detrimental effects of grinding operations.

Retain subparagraph below if required.

1. Provide dustproof partitions and temporary enclosures to limit dust migration and to isolate areas from noise.

PART 2 -  PRODUCTS

2.1 EPOXY-RESIN TERRAZZO

Epoxy-resin terrazzo is the predominant interior resinous matrix system.  Polyacrylate-modified cement and polyester-resin terrazzo are not included in the Section Text because of their limited use.

See Editing Instruction No. 1 in the Evaluations in Division 09 Section "Terrazzo Flooring" for cautions about naming manufacturers and products.  See Division 01 Section "Product Requirements."

A. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1. Crossfield Products Corp., Dex-O-Tex Division; [Cheminert] [Micro] Terrazzo.

2. General Polymers Corporation; Terrazzo [1100] [2000].

3. Key Resin Company; Key Epoxy Terrazzo.

4. Master Terrazzo Technologies LLC; Morricite.

5. Polymerica Incorporated; MasterPiece ETS.

6. Quadrant Chemical Corporation; Quadset Epoxy Terrazzo.

7. TEC Specialty Construction Brands, Inc.; Tuff-Lite Epoxy Terrazzo.

8. Terrazzo & Marble Supply Companies; Terroxy Resin Systems.

9. <Insert manufacturer's name; product name or designation>.

B. Materials:

Delete first subparagraph below if not required.  NTMA is silent on the use of flexible reinforcing membranes; consult terrazzo manufacturers for recommendations.

1. Flexible Reinforcing Membrane:  Manufacturer's resinous membrane for substrate crack preparation and reflective crack reduction.

Delete first subparagraph below if not required; consult manufacturers for recommendations.

a. Reinforcement:  Fiberglass scrim.

2. Primer:  [Manufacturer's product recommended for substrate and use indicated] <Insert requirements>.

3. Epoxy-Resin Matrix:  [Manufacturer's standard recommended for use indicated] <Insert requirements> and in color required for mix indicated.

Physical property requirements in first two subparagraphs below are based on NTMA's "Terrazzo Specifications and Design Guide." Revise to suit products selected.  If conductive system is required, insert electrical-resistance requirements.

a. Physical Properties without [Marble Chips] [Aggregates]:

1) Hardness:  60 to 85 per ASTM D 2240, Shore D.

2) Minimum Tensile Strength:  3000 psi (20.7 MPa) per ASTM D 638 for a 2-inch (51-mm) specimen made using a "C" die per ASTM D 412.

3) Minimum Compressive Strength:  10,000 psi (6.9 MPa) per ASTM D 695, Specimen B cylinder.

4) Chemical Resistance:  No deleterious effects by contaminants listed below after seven-day immersion at room temperature per ASTM D 1308.

a) Distilled water.

b) Mineral water.

c) Isopropanol.

d) Ethanol.

e) 0.025 percent detergent solution.

f) 1.0 percent soap solution.

g) 10 percent sodium hydroxide.

h) 10 percent hydrochloric acid.

i) 30 percent sulfuric acid.

j) 5 percent acetic acid.

b. Physical Properties with [Marble Chips] [Aggregates]:  For resin blended with Georgia white marble, ground, grouted, and cured per requirements in NTMA's "Terrazzo Specifications and Design Guide," comply with the following:

1) Flammability:  Self-extinguishing, maximum extent of burning 0.25 inch (6.35 mm) per ASTM D 635.

2) Thermal Coefficient of Linear Expansion:  0.0025 inch/inch per deg F (0.0025 mm/mm per 0.5556 deg C) for temperature range of minus 12 to plus 140 deg F (minus 24 to plus 60 deg C) per ASTM D 696.

Marble chips are the most commonly employed granular material.  Aggregate sizing may not be based on NTMA gradation standards for marble chips.  Consult NTMA and manufacturers for recommendations and incorporate requirements.

4. [Marble Chips] [Aggregates]:  Complying with NTMA gradation standards for mix indicated and containing no deleterious or foreign matter.

a. Abrasion and Impact Resistance:  Less than 40 percent loss per ASTM C 131.

b. 24-Hour Absorption Rate:  Less than 0.75 percent.

c. Dust Content:  Less than 1.0 percent by weight.

Retain first subparagraph below if recycled content of granular materials is required for LEED-NC or LEED-CI Credits MR 4.1 and MR 4.2.  An alternative method of meeting Credit MR 4.1 and MR 4.2 requirements is to retain requirement in Division 01 Section "Sustainable Design Requirements" that gives Contractor option and responsibility for determining how Credit MR 4.1 and MR 4.2 requirements will be met.

d. Recycled Content:  Provide products with average recycled content such that postconsumer recycled content plus one-half of preconsumer recycled content is not less than <Insert value> percent.

If desired for decorative effect, insert requirements for aggregates other than marble chips, such as granite, quartz, pea gravel, mother-of-pearl, metal, glass, plastic, or other suitable granules.  Consult NTMA for recommendations.

5. Finishing Grout:  Resin based.

See "Terrazzo Matrices" Article in the Evaluations in Division 09 Section "Terrazzo Flooring" for a discussion of NTMA plate number designations and custom design mixes.

Retain first paragraph below for NTMA-formulated design mixes.  Mixes that match NTMA thin-set plates are available but generally require a 3/8-inch (9.5-mm) topping thickness.

C. Terrazzo:  Comply with NTMA's "Terrazzo Specifications and Design Guide" and manufacturer's written instructions for matrix and marble-chip proportions and mixing.

1. Formulated Mix Color and Pattern:  [As selected by Architect from manufacturer's full range] [As selected by Architect from NTMA standard-terrazzo plates] [As selected by Architect from NTMA thin-set terrazzo plates] <Insert manufacturer's or NTMA's color plate designation>.

Retain paragraph below for custom design mixes.

D. Terrazzo:  Comply with NTMA's "Terrazzo Specifications and Design Guide" and manufacturer's written instructions for matrix and [marble-chip] [aggregate] proportions and mixing.

1. Custom Mix Color and Pattern:  [Match Architect's sample] [Match existing] <Insert custom design mix attributes>.

2.2 STRIP MATERIALS

Retain one of first two paragraphs below for thin-set or heavy-top divider-strip requirements.  Retain thin-set strips for 1/4-inch- (6.4-mm-) thick, epoxy-resin terrazzo.  Retain heavy-top strips for thicker installations.  Refer to "Strip Materials" Article in the Evaluations in Division 09 Section "Terrazzo Flooring" for discussion of strip material types, finishes, and placement.

A. Thin-Set Divider Strips:  L-type angle or T-type, 1/4 inch (6.4 mm) deep.

Brass may react with resinous matrices.  Verify that material retained in first subparagraph below is acceptable to terrazzo manufacturers.

1. Material:  [White-zinc alloy] [Brass] [Aluminum] [Plastic, in color selected from manufacturer's full range].

2. Top Width:  [1/8 inch (3.2 mm)] [1/4 inch (6.4 mm)] <Insert dimension>.

B. Heavy-Top Divider Strips:  L-type angle in depth required for topping thickness indicated.

1. Bottom-Section Material:  [Galvanized steel] [Matching top-section material].

Brass may react with resinous matrices.  Verify that material retained in first subparagraph below is acceptable to terrazzo manufacturers.

2. Top-Section Material:  [White-zinc alloy] [Brass] [Aluminum] [Plastic, in color selected from manufacturer's full range].

3. Top-Section Width:  [1/8 inch (3.2 mm)] [1/4 inch (6.4 mm)] [3/8 inch (9.5 mm)] [1/2 inch (12.7 mm)] <Insert dimension>.

C. Control-Joint Strips:  Separate, double L-type angles, positioned back to back, that match material, thickness, and color of divider strips and in depth required for topping thickness indicated.

D. Accessory Strips:  Match divider strip width, material, and color unless otherwise indicated.  Use the following types of accessory strips as required to provide a complete installation:

Revise list below to suit Project.

1. Base-bead strips for exposed top edge of terrazzo base.

2. Edge-bead strips for exposed edges of terrazzo.

3. Nosings for terrazzo stair treads and landings.

4. <Insert requirements>.

Retain paragraph below for terrazzo stair treads and landings.

E. Abrasive Strips:  Silicon carbide or aluminum oxide, or combination of both, in epoxy-resin binder and set in channel.

1. Width:  [1/2 inch (12.7 mm)] <Insert dimension>.

2. Depth:  As required by terrazzo thickness.

3. Length:  [4 inches (100 mm) less than stair width] [As indicated] <Insert dimension>.

4. Color:  [As selected by Architect from manufacturer's full range] <Insert requirements>.

2.3 MISCELLANEOUS ACCESSORIES

A. Strip Adhesive:  Epoxy-resin adhesive recommended by adhesive manufacturer for this use and acceptable to terrazzo manufacturer.

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.  VOC limit is that for multipurpose construction adhesives

1. Use adhesives that have a VOC content of 70 g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

B. Anchoring Devices:

Revise list below to suit Project.

1. Strips:  Provide mechanical anchoring devices for strip materials as required for secure attachment to substrate.

2. Precast Terrazzo:  Provide mechanical anchoring devices as recommended by fabricator for proper anchorage and support of units for conditions of installation and support.

C. Patching and Fill Material:  Terrazzo manufacturer's resinous product approved and recommended by manufacturer for application indicated.

D. Joint Compound:  Terrazzo manufacturer's resinous product approved and recommended by manufacturer for application indicated.

E. Cleaner:  Chemically neutral cleaner with pH factor between 7 and 10 that is biodegradable, phosphate free, and recommended by sealer manufacturer for use on terrazzo type indicated.

Revise paragraph below for sealer type.  Consult NTMA and terrazzo manufacturers for recommendations.

F. Sealer:  [Slip- and stain-resistant penetrating-type sealer that is chemically neutral with pH factor between 7 and 10; does not affect color or physical properties of terrazzo; is recommended by sealer manufacturer; and complies with NTMA's "Terrazzo Specifications and Design Guide" for terrazzo type indicated] [Acrylic] [Urethane] [Chemical-resistant epoxy] <Insert requirements>.

2.4 PRECAST TERRAZZO

A. Precast Terrazzo Units:  Precast epoxy-resin terrazzo [base] [stair tread] [threshold] [bench] [and] [planter] <Insert requirements> units.

See Editing Instruction No. 1 in the Evaluations in Division 09 Section "Terrazzo Flooring" for cautions about naming manufacturers.  Retain one of two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Manufacturers:  Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

2. Basis-of-Design Product:  Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

a. Romoco Precast Terrazzo Products.

b. <Insert manufacturer's name>.

B. Precast Terrazzo Base Units:  1/4 inch (6.4 mm) thick; cast in maximum lengths possible, but not less than 36 inches (900 mm); with rounded, finished top edge.

1. Type:  [Coved with minimum 3/4-inch (19-mm) radius] [Straight] [Splayed] [As indicated].

2. Height:  [6 inches (152 mm)] [4 inches (101 mm)] [As indicated] <Insert height>.

3. Outside Corner Units:  With finished returned edges at outside corner.

4. Color, Pattern, and Finish:  [As selected by Architect from manufacturer's full range] [Match Architect's sample] [Match adjacent poured-in-place terrazzo flooring] <Insert requirements>.

Verify requirements of authorities having jurisdiction for treads.

C. Precast Terrazzo Stair Treads:  1/2 inch (12.7 mm) thick with rounded nosing edge.

1. Abrasive Strips:  [Three-line] [Two-line] [One-line] [Abrasive nosing strip and two-line] <Insert description> abrasive inserts at nosings.

2. Color, Pattern, and Finish:  [As selected by Architect from manufacturer's full range] [Match Architect's sample] [Match adjacent poured-in-place terrazzo flooring] <Insert requirements>.

Insert requirements for other types of precast terrazzo units to suit Project.

Retain paragraph below for custom precast terrazzo components.

D. Precast Terrazzo Finishing:

1. Finish exposed-to-view edges or reveals to match face finish.

2. Ease exposed edges to 1/8-inch (3-mm) radius.

3. <Insert requirements>.

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine substrates and areas, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance.

B. Proceed with installation only after unsatisfactory conditions, including levelness tolerances, have been corrected.

3.2 PREPARATION

A. Clean substrates of substances, including oil, grease, and curing compounds, that might impair terrazzo bond.  Provide clean, dry, and neutral substrate for terrazzo application.

Retain first paragraph below for concrete substrates or insert requirements for other substrates such as wood or quarry tile; consult manufacturers for recommendations.

B. Concrete Slabs:

1. Provide sound concrete surfaces free of laitance, glaze, efflorescence, curing compounds, form-release agents, dust, dirt, grease, oil, and other contaminants incompatible with terrazzo.

a. Shot-blast surfaces with an apparatus that abrades the concrete surface, contains the dispensed shot within the apparatus, and recirculates the shot by vacuum pickup.

b. Repair damaged and deteriorated concrete according to terrazzo manufacturer's written recommendations.

c. Use patching and fill material to fill holes and depressions in substrates according to terrazzo manufacturer's written instructions.

2. Verify that concrete substrates are visibly dry and free of moisture.

Requirements for concrete dryness after curing vary among manufacturers.  Comply with terrazzo manufacturer's individual requirements for moisture testing.

3. Moisture Testing:

Retain first subparagraph below for moisture testing according to ASTM F 1869 if recommended by terrazzo manufacturer.

a. Test for moisture by anhydrous calcium chloride method according to ASTM F 1869.  Proceed with installation only after substrates have maximum moisture-vapor-emission rate of [3 lb of water/1000 sq. ft. (1.36 kg of water/92.9 sq. m)] <Insert emission rate> in 24 hours.

Retain first subparagraph below for moisture testing according to ASTM F 2170 if recommended by terrazzo manufacturer.

b. Test for moisture by relative humidity probe and digital meter method according to ASTM F 2170.  Proceed with installation only after substrates have a maximum relative-humidity-measurement reading of [70 to 75 percent] <Insert relative humidity measurement> in 24 hours.

c. Test for moisture content by [method recommended in writing by terrazzo manufacturer] <Insert test method>.  Proceed with installation only after substrates pass testing.

C. Protect other work from dust generated by grinding operations.  Control dust to prevent air pollution and comply with environmental protection regulations.

Retain subparagraph below if required.

1. Erect and maintain temporary enclosures and other suitable methods to limit dust migration and to ensure adequate ambient temperatures and ventilation conditions during installation.

D. Installation of terrazzo indicates acceptance of surfaces and conditions.

3.3 EPOXY-RESIN TERRAZZO INSTALLATION

A. General:

1. Comply with NTMA's written recommendations for terrazzo and accessory installation.

2. Place, rough grind, grout, cure grout, fine grind, and finish terrazzo according to manufacturer's written instructions and NTMA's "Terrazzo Specifications and Design Guide."

3. Installation Tolerance:  Limit variation in terrazzo surface from level to [1/4 inch in 10 feet (6 mm in 3 m)] <Insert dimensions>; noncumulative.

4. Ensure that matrix components and fluids from grinding operations do not stain terrazzo by reacting with divider and control-joint strips.

5. Delay fine grinding until heavy trade work is complete and construction traffic through area is restricted.

B. Thickness:  [1/4 inch (6.4 mm)] [3/8 inch (9.5 mm)] [As indicated] <Insert thickness> nominal.

Delete first paragraph below if not required.  Refer to "Resinous Matrix Terrazzo" Article in the Evaluations in Division 09 Section "Terrazzo Flooring" for discussion on flexible reinforcing membrane.

C. Flexible Reinforcing Membrane:

1. Prepare and prefill substrate cracks with membrane material.

Delete first subparagraph below if full substrate coverage is not required.

2. Install membrane to produce full substrate coverage in areas to receive terrazzo.

Delete first subparagraph below if membrane is not reinforced.

3. Reinforce membrane with fiberglass scrim.

4. Prepare membrane according to manufacturer's written instructions before applying substrate primer.

D. Primer:  Apply to terrazzo substrates according to manufacturer's written instructions.

Revise first paragraph below to suit Project.  Indicate location and spacing of strip materials on Drawings or insert below.

E. Strip Materials:

1. Divider and Control-Joint Strips:

a. Locate divider strips [in locations indicated] <Insert requirements>.

b. Install control-joint strips [back to back directly above concrete-slab control joints] [in locations indicated] <Insert requirements>.

c. Install control-joint strips with [1/4-inch (6.4-mm)] <Insert dimension> gap between strips, and install sealant in gap.

d. Install strips in adhesive setting bed without voids below strips, or mechanically anchor strips as required to attach strips to substrate, as recommended by strip manufacturer.

Retain first subparagraph below for accessory strips.

2. Accessory Strips:  Install accessory strips [as required to provide a complete installation] [in locations indicated] <Insert requirements>.

Retain subparagraph below for abrasive strips.  First option is based on NTMA recommendations for precast stair treads; second, on Romoco's product literature.

3. Abrasive Strips:  Install with surface of abrasive strip positioned [1/16 inch (1.6 mm)] [1/32 inch (0.8 mm)] <Insert dimension> higher than terrazzo surface.

F. Fine Grinding:  Grind with stones 120 grit or finer until all grout is removed from surface.  Repeat rough grinding, grout coat, and fine grinding if large voids exist after initial fine grinding.  Produce surface with a minimum of 70 percent aggregate exposure.

G. Repair:  Remove and replace terrazzo areas that evidence lack of bond with substrate.  Cut out terrazzo areas in panels defined by strips and replace to match adjacent terrazzo, or repair panels according to NTMA's written recommendations, as approved by Architect.

3.4 PRECAST TERRAZZO INSTALLATION

A. Install precast terrazzo units using method recommended NTMA and manufacturer unless otherwise indicated.

B. Installation Tolerance:  Set units with alignment level and true to dimensions, varying [1/8-inch (3.2-mm)] <Insert dimension> maximum in length, height, or width; noncumulative.

C. Do not install units that are chipped, cracked, discolored, or not properly finished.

D. Seal joints between units with [joint compound matching precast terrazzo matrix] [joint sealant] <Insert requirements>.

3.5 CLEANING AND PROTECTION

A. Cleaning:

1. Remove grinding dust from installation and adjacent areas.

2. Wash surfaces with cleaner according to NTMA's written recommendations and manufacturer's written instructions; rinse surfaces with water and allow to dry thoroughly.

B. Sealing:

1. Seal surfaces according to NTMA's written recommendations.

2. Apply sealer according to sealer manufacturer's written instructions.

C. Protection:  Provide final protection and maintain conditions, in a manner acceptable to Installer, that ensure that terrazzo is without damage or deterioration at time of Substantial Completion.

END OF SECTION 096623

RESINOUS MATRIX TERRAZZO FLOORING
096623 - 1

