Copyright 2004 and 2005 AIA
MASTERSPEC Full Length
08/04 (R 05/06)

Copyright 2004 and 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 123640 - STONE COUNTERTOPS
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

A. This Section includes stone countertops.

B. Related Sections include the following:

List below only products and construction that the reader might expect to find in this Section but are specified elsewhere.

Retain subparagraph below if stone types for all stonework Sections are described in Section below.  Using one stone schedule helps ensure uniformity of stone supplied under different Sections.

1. Division 04 Section "Exterior Stone Cladding" for descriptions of stone types required by this Section.

1.3 SUBMITTALS

A. Product Data:  For the following:

Adjust list below to suit Project.

1. Each variety of stone.[  Include data on physical properties required by referenced ASTM standards.]

2. Stone accessories and other manufactured products.

B. Shop Drawings:  Include plans, sections, details, and attachments to other work.

Samples may serve to define acceptable range of colors, patterns, etc., if other methods cannot be used due to cost.  Stone Samples may not show full range of appearance characteristics, especially with highly variable stone types.

C. Samples for Verification:

1. For each stone type indicated, in sets of Samples not less than 12 inches (300 mm) square.  Include [two] [three] or more Samples in each set and show the full range of variations in appearance characteristics expected in completed Work.

Retain paragraph and subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1; coordinate with requirements selected in Part 2 for adhesives and sealants.

D. LEED Submittal:

1. Product Data for Credit EQ 4.1:  For [adhesives] [and] [sealants], documentation including printed statement of VOC content.

Coordinate first paragraph below with qualification requirements in Division 01 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

E. Qualification Data:  For [Installer] [fabricator].

F. Sealant Compatibility Test Report:  From sealant manufacturer, complying with requirements in Division 07 Section "Joint Sealants" and indicating that sealants will not stain or damage stone.

G. Maintenance Data:  For stone countertops to include in maintenance manuals.  Include Product Data for stone-care products used or recommended by Installer, and names, addresses, and telephone numbers of local sources for products.

1.4 QUALITY ASSURANCE

Delete first paragraph below if not required by Project size, fabrication, or installation details.

A. Fabricator Qualifications:  Shop that employs skilled workers who custom-fabricate stone countertops similar to that indicated for this Project and whose products have a record of successful in-service performance.

B. Installer Qualifications:  Fabricator of products.

C. Source Limitations for Stone:  Obtain each variety of stone from a single quarry with resources to provide materials of consistent quality in appearance and physical properties.

Delete subparagraph below if no other stone Sections are used or if stone for other Sections is another variety.

1. Obtain each variety of stone from a single quarry, whether specified in this Section or in another Section of the Specifications.

Delete subparagraph and associated subparagraphs below if not required.  If many countertops are required, supplier must have adequate stock of slabs to allow selection, or procedure below will not be beneficial.

2. Make stone slabs available for Architect to examine for appearance characteristics.

a. Architect will select aesthetically acceptable slabs and will indicate aesthetically unacceptable portions of slabs.

b. Segregate slabs selected for use on Project and mark backs indicating approval.

Subparagraph below may be advantageous for stone that is highly variable; otherwise, it may not be necessary.

c. Mark and photograph aesthetically unacceptable portions of slabs as directed by Architect.

Usually delete paragraph and subparagraphs below.  A mockup may be a reasonable precaution for projects that require many stone countertops but may not be practical for other applications.

D. Mockup:  Build mockup to demonstrate aesthetic effects and set quality standards for materials and execution.

Indicate on Drawings that portion of countertop represented by mockup or draw mockup as separate element.

1. Build mockup of typical countertop as shown on Drawings.

Retain subparagraph below if the intention is to make an exception to the default requirement in Division 01 Section "Quality Requirements" for demolishing and removing mockups when directed, unless otherwise indicated.

2. Approved mockup may become part of the completed Work if undisturbed at time of Substantial Completion.

1.5 DELIVERY, STORAGE, AND HANDLING

Consider deleting this Article.  Most stone countertops will be lifted by hand and will be delivered right before installation, not stored.

A. Lift stone with wide-belt slings; do not use wire rope or ropes that might cause staining.  Move stone, if required, using dollies with cushioned wood supports.

B. Store stone on wood A-frames or pallets with nonstaining separators and nonstaining, waterproof covers.  Ventilate under covers to prevent condensation.

1.6 PROJECT CONDITIONS

Indicating field measurements on Shop Drawings may not be practical.  Field measurements are often taken and corresponding adjustments made right before delivering countertops for installation.

A. Field Measurements:  Verify dimensions of construction to receive stone countertops by field measurements before fabrication[ and indicate measurements on Shop Drawings].

PART 2 -  PRODUCTS

2.1 STONE

Retain this Article and delete first five articles below if stone varieties and sources are specified in Division 04 Section "Exterior Stone Cladding." Specifying all stone types in one Section helps ensure uniformity of stone supplied under different Sections.

A. Varieties and Sources:  Subject to compliance with requirements, provide stone of varieties and from sources complying with Division 04 Section "Exterior Stone Cladding."

Delete "Stone" Article and retain one or more of first five articles below to describe stone types used if stone types are not specified in Division 04 Section "Exterior Stone Cladding." If articles describing stone types are retained here and only one type from each category is required, the generic name can be retained and used on Drawings instead of a stone-type designation; otherwise, copy and re-edit Article selected for each type required, inserting a different stone-type designation each time.

2.2 GRANITE <Insert drawing designation>

Some varieties of granite that are suitable for interior use do not comply with ASTM C 615; verify that granite selected will comply before retaining paragraph below.

A. Granite:  Comply with ASTM C 615.

Paragraph below is an example of a generic description that can be retained and edited for a nonproprietary specification.  For a more explicit specification, delete and list varieties and sources.

B. Description:  Uniform, [fine] [medium]-grained, [white] [pink] [gray] [black] <Insert color> stone[ without veining].

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  If naming varieties and sources, retain one of three paragraphs and list below.  See Division 01 Section "Product Requirements."

C. Available Varieties and Sources:  Subject to compliance with requirements, stone varieties that may be incorporated into the Work include, but are not limited to, the following:

D. Varieties and Sources:  Subject to compliance with requirements, provide one of the following:

E. Variety and Source:  Subject to compliance with requirements, provide the following:

1. <Insert, in separate subparagraphs, names of varieties and producers, distributors, or importers.>

Delete paragraph below if variety selected has no veining.

F. Cut:  [Vein] [Fleuri] cut.

Delete first paragraph below if not applicable.

G. Cut stone from contiguous, matched slabs in which natural markings occur.

H. Finish:  [Polished] [Honed] [Thermal] [As indicated] [Match Architect's sample] <Insert finish>.

Retain paragraph below for added quality control if required.

I. Match Architect's samples for color, finish, and other stone characteristics relating to aesthetic effects.

2.3 MARBLE <Insert drawing designation>

Many varieties of marble that are suitable for interior use do not comply with ASTM C 503; verify that marble selected will comply before retaining paragraph below.

A. Marble:  Comply with ASTM C 503.

Consider retaining subparagraph below.  Value of 10 is required by ASTM C 503 for floors and can be considered appropriate for countertops.  Verify that stone selected complies before retaining.

1. Stone Abrasion Resistance:  Minimum value of [10] <Insert value>, based on testing according to ASTM C 241 or ASTM C 1353.

Paragraph below is an example of a generic description that can be retained and edited for a nonproprietary specification.  For a more explicit specification, delete and list varieties and sources below.  Below describes a crystalline calcite marble; revise to describe other varieties of marble if required.

B. Description:  Uniform, fine- to medium-grained, [white] <Insert color> stone with only slight veining.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  If naming varieties and sources, retain one of first three paragraphs and list below.  See Division 01 Section "Product Requirements."

C. Available Varieties and Sources:  Subject to compliance with requirements, stone varieties that may be incorporated into the Work include, but are not limited to, the following:

D. Varieties and Sources:  Subject to compliance with requirements, provide one of the following:

E. Variety and Source:  Subject to compliance with requirements, provide the following:

1. <Insert, in separate subparagraphs, names of varieties and producers, distributors, or importers.>

F. Cut:  [Vein] [Fleuri] cut.

Delete first paragraph below if not applicable.

G. Cut stone from contiguous, matched slabs in which natural markings occur.

H. Finish:  [Polished] [Honed] [As indicated] [Match Architect's sample] <Insert finish>.

Retain paragraph below for added quality control if required.

I. Match Architect's samples for color, finish, and other stone characteristics relating to aesthetic effects.

2.4 SERPENTINE <Insert drawing designation>

If retaining this Article, select one of two classifications in paragraph below.  Classification I Exterior requires lower absorption and higher strength; verify that serpentine selected complies with this classification before retaining.

A. Serpentine:  Comply with ASTM C 1526, Classification [I Exterior] [II Interior].

Consider retaining subparagraph below.  Value of 10 is required by ASTM C 1526 for floors and can be considered appropriate for countertops.  Verify that stone selected complies before retaining.

1. Stone Abrasion Resistance:  Minimum value of [10] <Insert value>, based on testing according to ASTM C 241 or ASTM C 1353.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  If naming varieties and sources, retain one of three paragraphs and list below.  See Division 01 Section "Product Requirements."

B. Available Varieties and Sources:  Subject to compliance with requirements, stone varieties that may be incorporated into the Work include, but are not limited to, the following:

C. Varieties and Sources:  Subject to compliance with requirements, provide one of the following:

D. Variety and Source:  Subject to compliance with requirements, provide the following:

1. <Insert, in separate subparagraphs, names of varieties and producers, distributors, or importers.>

Delete first paragraph below if not applicable.

E. Cut stone from contiguous, matched slabs in which natural markings occur.

F. Finish:  [Polished] [Honed] [As indicated] [Match Architect's sample] <Insert finish>.

Retain paragraph below for added quality control if required.

G. Match Architect's samples for color, finish, and other stone characteristics relating to aesthetic effects.

2.5 SLATE <Insert drawing designation>

If retaining this Article, select one of two classifications in paragraph below.  Classification I Exterior requires lower absorption and better acid resistance in addition to higher strength; verify that slate selected complies with this classification before retaining.

A. Slate:  Comply with ASTM C 629, Classification [I Exterior] [II Interior], with a fine, even grain[ and unfading color,] from clear, sound stock.

Consider retaining subparagraph below.  Value of 8 is required by ASTM C 629 for floors and may be considered appropriate for countertops.  Verify that stone selected complies before retaining.

1. Stone Abrasion Resistance:  Minimum value of [8] <Insert value>, based on testing according to ASTM C 241 or ASTM C 1353.

Subparagraph below is an example of a generic description that can be retained and edited for a nonproprietary specification.  For a more explicit specification, list varieties and sources below.

2. Color:  [Black] [Blue-black] [Gray] [Blue-gray] [Green] [Purple] [Mottled purple and green] [Red].

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  If naming varieties and sources, retain one of first three paragraphs and list below.  See Division 01 Section "Product Requirements."

B. Available Varieties and Sources:  Subject to compliance with requirements, stone varieties that may be incorporated into the Work include, but are not limited to, the following:

C. Varieties and Sources:  Subject to compliance with requirements, provide one of the following:

D. Variety and Source:  Subject to compliance with requirements, provide the following:

1. <Insert, in separate subparagraphs, names of varieties and producers, distributors, or importers.>

E. Finish:  [Honed] [Sand rubbed] [Natural cleft] [As indicated] [Match Architect's sample] <Insert finish>.

Retain paragraph below for added quality control if required.

F. Match Architect's samples for color, finish, and other stone characteristics relating to aesthetic effects.

2.6 OTHER STONE <Insert drawing designation>

A. Provide sound natural stone as follows:

1. Maximum Absorption per ASTM C 97:  <Insert value.>

2. Minimum Compressive Strength per ASTM C 170:  <Insert value.>

3. Minimum Flexural Strength per ASTM C 880:  <Insert value.>

Consider retaining subparagraph below.  Value of 10 is generally recommended for floors and can be considered appropriate for countertops.  Verify that stone selected complies before retaining.

4. Stone Abrasion Resistance:  Minimum value of [10] <Insert value>, based on testing according to ASTM C 241 or ASTM C 1353.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  If naming varieties and sources, retain one of first three paragraphs and list below.  See Division 01 Section "Product Requirements."

B. Available Varieties and Sources:  Subject to compliance with requirements, stone varieties that may be incorporated into the Work include, but are not limited to, the following:

C. Varieties and Sources:  Subject to compliance with requirements, provide one of the following:

D. Variety and Source:  Subject to compliance with requirements, provide the following:

1. <Insert, in separate subparagraphs, names of varieties and producers, distributors, or importers.>

E. Finish:  [Polished] [Honed] [Sand rubbed] [Natural cleft] [As indicated] [Match Architect's sample] <Insert finish>.

Retain paragraph below for added quality control if required.

F. Match Architect's samples for color, finish, and other stone characteristics relating to aesthetic effects.

2.7 ADHESIVES, GROUT, SEALANTS, AND STONE ACCESSORIES

A. General:  Use only adhesives formulated for stone and ceramic tile and recommended by their manufacturer for the application indicated.

Adhesive in paragraph below is generally used for setting stone countertops.  Retain option if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.  VOC limit is that for ceramic tile adhesives.

B. Water-Cleanable Epoxy Adhesive:  ANSI A118.3[, with a VOC content of 65 g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24)].

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  If naming manufacturers, retain one of two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Available Manufacturers:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

2. Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

a. Bonsal, W. R. Company.

b. Bonstone Materials Corporation.

c. C-Cure.

d. Custom Building Products.

e. Laticrete International, Inc.

f. MAPEI Corp.

g. Summitville Tiles, Inc.

h. <Insert manufacturer's name.>

MIA recommends grout in paragraph below for joints in countertops.

C. Water-Cleanable Epoxy Grout:  ANSI A118.3, chemical-resistant, water-cleanable, tile-setting and -grouting epoxy.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  If naming manufacturers, retain one of two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Available Manufacturers:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

2. Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

a. Boiardi Products Corporation.

b. W. R. Bonsal Company.

c. Bostik Findley Inc.

d. C-Cure.

e. Custom Building Products.

f. Laticrete International, Inc.

g. MAPEI Corp.

h. Summitville Tiles, Inc.

i. TEC Incorporated; H. B. Fuller Company.

j. <Insert manufacturer's name.>

Retain paragraph and subparagraphs below if joints in countertops are bonded rather than grouted or sealant filled.  Retain last option in paragraph if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.  VOC limit is that for ceramic tile adhesives.

D. Stone Adhesive:  2-part [epoxy] [or] [polyester] adhesive, formulated specifically for bonding stone to stone, with an initial set time of not more than 2 hours at 70 deg F (21 deg C)[, and with a VOC content of 65 g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24)].

1. Color:  [Clear] [Match stone].

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  If naming manufacturers and products, retain one of two subparagraphs and list of manufacturers and products below.  See Division 01 Section "Product Requirements."

2. Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

3. Products:  Subject to compliance with requirements, provide one of the following:

a. Epoxy Adhesive:  Akemi North America; Akepox.

b. Epoxy Adhesive:  Axson North America, Inc., Wood & Stone Company; Akabond Epoxy.

c. Epoxy Adhesive:  Bonstone Materials Corporation; Touchstone Ratio Pac Clear Gel Epoxy.

d. Epoxy Adhesive:  Bonstone Materials Corporation; Touchstone Last Patch.

e. Epoxy Adhesive:  <Insert manufacturer's name; product name or designation.>

f. Polyester Adhesive:  Akemi North America; Platinum Clear Polyester Adhesive.

g. Polyester Adhesive:  Axson North America, Inc., Wood & Stone Company; Wood & Stone Polyester.

h. Polyester Adhesive:  Bonstone Materials Corporation; Gripstone L-200KG.

i. Polyester Adhesive:  <Insert manufacturer's name; product name or designation.>

Sealant may be required for joints at backsplash even if countertop joints are grouted or bonded.  If retaining paragraph and subparagraphs below, coordinate with Division 07 Section "Joint Sealants."

E. Sealant for Countertops:  Manufacturer's standard sealant of characteristics indicated below that comply with applicable requirements in Division 07 Section "Joint Sealants" and will not stain the stone it is applied to.

Acid-curing silicone sealants may etch polished marble.  Before retaining products, verify that they will not stain stone.

1. Single-component, [neutral] [acid]-curing silicone sealant[ ES-<#>].

2. Color:  [Clear] [As selected by Architect from manufacturer's full range].

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.  VOC limit is that for architectural sealants.  If retaining below, verify that manufacturers' products selected can comply with VOC limit.

3. Use sealants that have a VOC content of [250] <Insert limit> g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

Delete first paragraph below if joints are not allowed or if splined joints are not required.

F. Stone Joint Splines:  Stainless-steel or brass washers approximately 1 inch (25 mm) in diameter and of thickness to fit snugly in saw-cut kerf in edge of stone units.

G. Stone Cleaner:  Cleaner specifically formulated for stone types, finishes, and applications indicated, as recommended by stone producer[ and, if a sealer is specified, by sealer manufacturer].  Do not use cleaning compounds containing acids, caustics, harsh fillers, or abrasives.

Delete paragraph and subparagraphs below if not required or recommended for stone type.

H. Stone Sealer:  Colorless, stain-resistant sealer that does not affect color or physical properties of stone surfaces, as recommended by stone producer for application indicated.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  If naming manufacturers, retain one of two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Available Manufacturers:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

2. Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

a. Bostik Findley Inc.

b. Custom Building Products.

c. Hillyard, Inc.

d. HMK Stone Care System.

e. Miracle Sealants Company.

f. Stone Care International Inc.

g. Summitville Tiles, Inc.

h. <Insert manufacturer's name.>

2.8 STONE FABRICATION, GENERAL

A. Select stone for intended use to prevent fabricated units from containing cracks, seams, and starts that could impair structural integrity or function.

Delete subparagraph below if stone varieties used do not require repairs.

1. Repairs that are characteristic of the varieties specified are acceptable provided they do not impair structural integrity or function and are not aesthetically unpleasing, as judged by Architect.

Retain first paragraph below for multiple countertops that require a degree of matching, such as those with applied backsplashes.

B. Grade and mark stone for final locations to produce assembled countertop units with an overall uniform appearance.

C. Fabricate stone countertops in sizes and shapes required to comply with requirements indicated, including details on Drawings and Shop Drawings.

Retain applicable references in first two subparagraphs below.  No specific reference for slate currently exists, but related information is included in MIA's "Dimension Stone - Design Manual."

1. For granite, comply with recommendations in NBGQA's "Specifications for Architectural Granite."

2. For [marble] [and] [serpentine], comply with recommendations in MIA's "Dimension Stone--Design Manual."

3. Clean sawed backs of stones to remove rust stains and iron particles.

4. Dress joints straight and at right angle to face, unless otherwise indicated.

5. Cut and drill sinkages and holes in stone for anchors, supports, and attachments.

6. Provide openings, reveals, and similar features as needed to accommodate adjacent work.

Delete first subparagraph below if not applicable.

7. Fabricate molded edges with machines having abrasive shaping wheels made to reverse contour of edge profile to produce uniform shape throughout entire length of edge and with precisely formed arris slightly eased to prevent snipping, and matched at joints between units.  Form corners of molded edges as indicated with outside corners slightly eased, unless otherwise indicated.

8. Finish exposed faces of stone to comply with requirements indicated for finish of each type of stone required and to match approved Samples and mockups.  Provide matching finish on exposed edges of countertops, splashes, and cutouts.

D. Carefully inspect finished stone units at fabrication plant for compliance with requirements for appearance, material, and fabrication.  Replace defective units.

2.9 STONE COUNTERTOPS

A. General:  Comply with recommendations in MIA's "Dimension Stone - Design Manual."

Although 3/4-inch (20-mm) stone will generally provide adequate strength for countertops without large cutouts, where cutouts leave only a narrow strip of stone at front and back of counter, 1-1/4-inch (32-mm) material will provide better assurance against breakage.

B. Nominal Thickness:  Provide thickness indicated, but not less than [3/4 inch (20 mm)] [7/8 inch (22 mm)] [1-1/4 inches (32 mm)].  Gage backs to provide units of identical thickness.

Options in paragraph below are examples only.  See MIA's "Dimension Stone - Design Manual."

C. Edge Detail:  [Straight, slightly eased at top] [3/8-inch (10-mm) bevel] [3/4-inch (20-mm) full bullnose] [1-1/4-inch (20-mm) full bullnose] [3/8-inch (10-mm) radius with 2-inch (50-mm) apron] [1-1/2-inch (40-mm) laminated bullnose] [As indicated].

Revise height and thickness in paragraph and subparagraphs below to suit Project.  Delete if splashes are not required.

D. Splashes:  Provide 3/4-inch- (20-mm-) thick [backsplashes] [and] [end splashes], unless otherwise indicated.

1. Height:  [4 inches (100 mm)] [As indicated] <Insert height>.

Options in subparagraph below are examples only; select one of first four options or revise subparagraph if details are not shown on Drawings.

2. Top-Edge Detail:  [Straight, slightly eased at corner] [3/8-inch (10-mm) bevel] [3/4-inch (20-mm) radius] [3/8-inch (10-mm) radius] [As indicated].

Select one of first two paragraphs below.  First will not be possible with very large or complex countertops.  If retaining second, show joint locations on Drawings.

E. Joints:  Fabricate countertops without joints.

F. Joints:  Fabricate countertops in sections for joining in field, with joints at locations indicated and as follows:

Select one of three subparagraphs below or revise to suit Project.

1. Bonded Joints:  1/32 inch (0.8 mm) or less in width.

2. Grouted Joints:  1/16 inch (1.5 mm) in width.

3. Sealant-Filled Joints:  1/16 inch (1.5 mm) in width.

Consider retaining subparagraph below for higher-quality work.  Metal splines may be an unnecessary expense at typical joints but may be advantageous if narrow strips of stone are used between joints to form large openings for kitchen sinks, cooktops, etc.  See details in MIA's "Dimension Stone--Design Manual."

4. Splined Joints:  Accurately cut kerfs in edges at joints for insertion of metal splines to maintain alignment of surfaces at joints[ where indicated].  Make width of cuts slightly more than thickness of splines to provide snug fit.[  Provide at least three splines in each joint.]

G. Cutouts and Holes:

1. Undercounter Fixtures:  Make cutouts for undercounter fixtures in shop using template or pattern furnished by fixture manufacturer.  Form cutouts to smooth, even curves.

Retain one of three subparagraphs below to describe profile of cutout edges or show on Drawings.

a. Provide vertical edges, slightly eased at juncture of cutout edges with top and bottom surfaces of countertop and projecting 3/16 inch (5 mm) into fixture opening.

b. Provide vertical edges, rounded to 3/8-inch (10-mm) radius at juncture of cutout edges with top surface of countertop, slightly eased at bottom, and projecting 3/16 inch (5 mm) into fixture opening.

c. Provide 3/4-inch (20-mm) full bullnose edges projecting 3/8 inch (10 mm) into fixture opening.

Retain "Undercounter Fixtures" Subparagraph above for undercounter lavatories and sinks and subparagraph below for counter-mounted cooktops, lavatories, sinks, etc.  Replace the word "fixtures" in subparagraph above or below with "cooktops," "lavatories," "sinks," etc., if required.  Shop fabrication usually provides better results, but large openings, such as for kitchen sinks, are better completed after top is in place to avoid possibility of breakage during delivery or installation.

2. Counter-Mounted Fixtures:  Prepare countertops in shop for field cutting openings for counter-mounted fixtures.  Mark tops for cutouts and drill holes at corners of cutout locations.  Make corner holes of largest radius practical.

Retain subparagraph below if deck-mounted fittings or soap dispensers are used.

3. Fittings:  Drill countertops in shop for plumbing fittings, undercounter soap dispensers, and similar items.

PART 3 -  EXECUTION

3.1 EXAMINATION

Coordinate conditions required by Work of this Section with requirements in other Sections in which substrates are specified.

A. Examine substrates indicated to receive stone countertops and conditions under which stone countertops will be installed, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance.

1. For the record, prepare written report, endorsed by Installer, listing conditions detrimental to performance of stone countertops.

Delete subparagraph above if not required.  Always retain below.

2. Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 PREPARATION

Delete first paragraph below if no preset inserts are required.

A. Advise installers of other work about specific requirements for placement of inserts and similar items to be used by stone countertop Installer for anchoring stone countertops.  Furnish installers of other work with Drawings or templates showing locations of these items.

B. Clean dirty or stained stone surfaces by removing soil, stains, and foreign materials before setting.  Clean stone by thoroughly scrubbing with fiber brushes and then drenching with clear water.  Use only mild cleaning compounds that contain no caustic or harsh materials or abrasives.  Allow stone to dry before installing.

3.3 CONSTRUCTION TOLERANCES

Retain, delete, or revise tolerances in this Article to suit Project and office practice.

A. Variation from Plumb:  For vertical lines and surfaces, do not exceed 1/16 inch in 48 inches (1.5 mm in 1200 mm).

B. Variation from Level:  Do not exceed 1/8 inch in 96 inches (3 mm in 2400 mm), 1/4 inch (6 mm) maximum.

C. Variation in Joint Width:  Do not vary joint thickness more than 1/4 of nominal joint width.

D. Variation in Plane at Joints (Lipping):  Do not exceed 1/64-inch (0.4-mm) difference between planes of adjacent units.

E. Variation in Line of Edge at Joints (Lipping):  Do not exceed 1/64-inch (0.4-mm) difference between edges of adjacent units, where edge line continues across joint.

3.4 INSTALLATION OF COUNTERTOPS

Retain one of two paragraphs below.  For best work, retain first paragraph and show subtops on Drawings.  Second paragraph is generally suitable only for residential work and only if countertops are adequately supported.  Second paragraph may also be used with lavatory tops supported by steel angle framing if framing is adequately spaced for stone strength and thickness and has flush top surface.

A. General:  Install countertops over plywood subtops with full spread of water-cleanable epoxy adhesive.

B. General:  Install countertops by adhering to supports with water-cleanable epoxy adhesive.

Retain one of first two paragraphs below.

C. Do not cut stone in field, unless otherwise indicated.  If stone countertops or splashes require additional fabrication not specified to be performed at Project site, return to fabrication shop for adjustment.

D. Do necessary field cutting as stone is set.  Use power saws with diamond blades to cut stone.  Cut lines straight, true, and at right angles to finished surfaces unless beveling is required for clearance.  Ease edges slightly to prevent snipping.

E. Set stone to comply with requirements indicated on Drawings and Shop Drawings.  Shim and adjust stone to locations indicated, with uniform joints of widths indicated and with edges and faces aligned according to established relationships and indicated tolerances.[  Install anchors and other attachments indicated or necessary to secure stone countertops in place.]

Retain one of two paragraphs below unless joints are not allowed.  Retain first paragraph for bonded joints and second paragraph for grout- or sealant-filled joints.  Delete both if joints are not allowed.

F. Bond joints with stone adhesive and draw tight as countertops are set.  Mask areas of countertops adjacent to joints to prevent adhesive smears.

G. Space joints with 1/16-inch (1.5-mm) gap for filling with [grout] [sealant].  Use temporary shims to ensure uniform spacing.

Consider retaining either or both subparagraphs below with either paragraph above.  Metal splines may be an unnecessary expense at typical joints but may be advantageous if narrow strips of stone are used between joints to form large openings for kitchen sinks, cooktops, etc.  See details in MIA's "Dimension Stone--Design Manual."

1. Install metal splines in kerfs in stone edges at joints[ where indicated].  Fill kerfs with [stone adhesive] [setting adhesive] [sealant] before inserting splines and remove excess immediately after adjoining units are drawn into position.

2. Clamp units to temporary bracing, supports, or each other to ensure that countertops are properly aligned and joints are of specified width.

Delete paragraph below if field cutting is not allowed.

H. Complete cutouts not finished in shop.  Mask areas of countertops adjacent to cutouts to prevent damage while cutting.  Use power saws with diamond blades to cut stone.  Make cutouts to accurately fit items to be installed, and at right angles to finished surfaces unless beveling is required for clearance.  Ease edges slightly to prevent snipping.

Retain one of three paragraphs below depending on joining methods chosen.  Usually adhere splashes to either countertop or wall, but not both, and fill remaining joint with sealant to allow some movement.  MIA recommends adhering to wall and applying sealant to joint at countertop.

I. Install backsplash and end splash by adhering to wall with water-cleanable epoxy adhesive and to countertops with stone adhesive.  Mask areas of countertops and splashes adjacent to joints to prevent adhesive smears.

J. Install backsplash and end splash by adhering to countertops with stone adhesive.  Mask areas of countertops and splashes adjacent to joints to prevent adhesive smears.  Leave 1/16-inch (1.5-mm) gap between splash and wall for filling with sealant.  Use temporary shims to ensure uniform spacing.

K. Install backsplash and end splash by adhering to wall with water-cleanable epoxy adhesive.  Leave 1/16-inch (1.5-mm) gap between countertop and splash for filling with sealant.  Use temporary shims to ensure uniform spacing.

Delete paragraph below if grouted joints are not used.

L. Grout joints to comply with ANSI A108.10.  Remove temporary shims before grouting.  Tool grout uniformly and smoothly with plastic tool.

Delete paragraph below if sealant is not used.

M. Apply sealant to [joints] [and] [gaps specified for filling with sealant]; comply with Division 07 Section "Joint Sealants." Remove temporary shims before applying sealant.

3.5 ADJUSTING AND CLEANING

A. In-Progress Cleaning:  Clean countertops as work progresses.  Remove adhesive, grout, mortar, and sealant smears immediately.

B. Remove and replace stone countertops of the following description:

1. Broken, chipped, stained, or otherwise damaged stone.  Stone may be repaired if methods and results are approved by Architect.

2. Defective countertops.

3. Defective joints, including misaligned joints.

4. Interior stone countertops and joints not matching approved Samples and mockups.

5. Interior stone countertops not complying with other requirements indicated.

C. Replace in a manner that results in stone countertops matching approved Samples and mockups, complying with other requirements, and showing no evidence of replacement.

Revise the words "six days" in paragraph below to minimum needed for curing sealants or adhesives as applicable.

D. Clean stone countertops not less than six days after completion of [sealant installation] [installation], using clean water and soft rags.  Do not use wire brushes, acid-type cleaning agents, cleaning compounds with caustic or harsh fillers, or other materials or methods that could damage stone.

Delete paragraph below if not required or recommended for stone type.

E. Sealer Application:  Apply stone sealer to comply with stone producer's and sealer manufacturer's written instructions.

END OF SECTION 123640

STONE COUNTERTOPS
123640 - 1

