Copyright 2006 AIA
MASTERSPEC Full Length
05/06

Copyright 2006 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 09720 - WALL COVERINGS
Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.2 SUMMARY

A. Section Includes:

1. Vinyl wall covering.

2. Woven glass-fiber wall covering.

3. Textile wall covering.

4. Heavy-duty synthetic textile wall covering.

5. Wood-veneer wall covering.

6. Wallpaper.

Retain first paragraph below and describe wall-covering materials to be supplied by Owner if applicable.

B. Owner-Furnished Materials:  <Insert wall-covering materials>.

C. Related Sections:

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.

Retain one or both of two subparagraphs below if coating application is specified in that Division 9 Section; revise if using another Division 9 Section.  Delete subparagraphs if specified in this Section.

1. Division 9 Section "[Interior Painting] <Insert Section title>" for [priming wall surfaces] [primers, coatings, and paint for woven glass-fiber wall coverings].

2. Division 9 Section "Wood Stains and Transparent Finishes" for field-applied finishes for wood-veneer wall coverings.

If alternates, allowances, or unit prices apply to Work of this Section, insert brief paragraphs here to alert Contractor and reference appropriate Division 1 Sections for specific details.

1.3 SUBMITTALS

First six paragraphs below are defined in Division 1 Section "Submittal Procedures" as "Action Submittals."

A. Product Data:  For each type of product indicated.  Include data on physical characteristics, durability, fade resistance, and flame-resistance characteristics.

B. LEED Submittals:

Retain first subparagraph below and "Forest Certification" Paragraph in "Quality Assurance" Article if wood-veneer wall coverings are required to be certified for LEED-NC or LEED-CI Credit MR 7, which requires that a minimum of 50 percent of wood-based materials be certified.

1. Certificates for Credit MR 7:  Chain-of-custody certificates certifying that wood-veneer wall coverings comply with forest certification requirements.  Include evidence that manufacturer is certified for chain of custody by an FSC-accredited certification body.

Retain first subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1; coordinate with requirements selected in Part 2 for adhesives.

2. Product Data for Credit EQ 4.1:  For adhesives, including printed statement of VOC content.

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.2; coordinate with requirements selected in Part 2 for paints and coatings.  Retain option for LEED-CI.

3. Product Data for Credit EQ 4.2:  For paints and coatings, including printed statement of VOC content[ and chemical components].

Retain first option in first paragraph below for patterned wall covering; retain second option for wood-veneer wall coverings.

C. Shop Drawings:  Show location and extent of each wall-covering type.  Indicate [pattern placement,] [veneer matching,] seams and termination points.

D. Samples for Initial Selection:  For each type of wall covering indicated.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled.  Retain first paragraph below with or without above.

E. Samples for Verification:  Full width by [36-inch- (914-mm-)] <Insert dimension> long section of wall covering.

Retain first subparagraph below for all types of wall coverings except wood veneer.

1. Sample from same print run or dye lot to be used for the Work, with specified [treatments] [paint] applied.[  Show complete pattern repeat.] Mark top and face of fabric.

Retain subparagraph below for wood-veneer wall coverings.

2. Sample from same flitch to be used for the Work, with specified finish applied.

F. Product Schedule:  For wall coverings.[  Use same designations indicated on Drawings.]

Remaining paragraphs are defined in Division 1 Section "Submittal Procedures" as "Informational Submittals."

Coordinate first paragraph below with qualification requirements in Division 1 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

G. Qualification Data:  For qualified testing agency.

H. Product Test Reports:  Based on evaluation of comprehensive tests performed by a qualified testing agency, for wall covering.

I. Maintenance Data:  For wall coverings to include in maintenance manuals.

1.4 QUALITY ASSURANCE

Retain first paragraph below if wood-veneer wall coverings are required to be certified for LEED-NC or LEED-CI Credit MR 7, which requires that a minimum of 50 percent of wood-based materials be certified.

A. Forest Certification:  Fabricate products with wood veneer produced from wood obtained from forests certified by an FSC-accredited certification body to comply with FSC STD-01-001, "FSC Principles and Criteria for Forest Stewardship."

B. Fire-Test-Response Characteristics:  As determined by testing identical wall coverings applied with identical adhesives to substrates according to test method indicated below by a qualified testing agency.  Identify products with appropriate markings of applicable testing agency.

1. Surface-Burning Characteristics:  As follows, per ASTM E 84:

a. Flame-Spread Index:  [25] <Insert value> or less.

b. Smoke-Developed Index:  [50] [450] <Insert value> or less.

Delete both subparagraphs below if no textile wall covering or if test in paragraph above and protection by automatic sprinkler system are acceptable alternatives that comply with requirements of authorities having jurisdiction.  First example below is relevant for textile wall covering under the 1997 Uniform Building Code.  The 2003 IBC references NFPA 265 for textiles and NFPA 286 for other than textiles, and has prescriptive testing requirements and acceptable results.  Verify and insert requirements of authorities having jurisdiction.

2. Fire-Growth Contribution:  Textile wall coverings complying with acceptance criteria of UBC Standard 8-2.

3. Fire-Growth Contribution:  Textile wall coverings tested according to [NFPA 265] [NFPA 286] and complying with test protocol and criteria in the 2003 IBC.

C. Mockups:  Build mockups to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for fabrication and installation.

1. Build mockups for each type of wall covering on each substrate required.  Comply with requirements in ASTM F 1141.

Retain subparagraph below if mockups are installed as part of building rather than erected separately and the intention is to make an exception to the default requirement in Division 1 Section "Quality Requirements" for demolishing and removing mockups when directed unless otherwise indicated.

2. Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

1.5 PROJECT CONDITIONS

A. Environmental Limitations:  Do not deliver or install wall coverings until spaces are enclosed and weathertight, wet work in spaces is complete and dry, work above ceilings is complete, and temporary HVAC system is operating and maintaining ambient temperature and humidity conditions at occupancy levels during the remainder of the construction period.

1. Wood-Veneer Wall Coverings:  Condition spaces for not less than 48 hours before installation.

B. Lighting:  Do not install wall covering until [a permanent level of lighting] <Insert requirement> is provided on the surfaces to receive wall covering.

C. Ventilation:  Provide continuous ventilation during installation and for not less than the time recommended by wall-covering manufacturer for full drying or curing.

1.6 EXTRA MATERIALS

A. Furnish extra materials that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

1. Wall-Covering Materials:  For each type, full-size units equal to [5] <Insert number> percent of amount installed.

PART 2 -  PRODUCTS

2.1 WALL COVERINGS

A. General:  Provide rolls of each type of wall covering from same print run or dye lot.

First five articles below cover five different types of wall coverings.  Refer to the table at the end of the Evaluations for a list of manufacturers' products.  Use this table in combination with manufacturers' catalogs or product data to insert series, type, model, and designations of other characteristics.

2.2 VINYL WALL COVERING <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

Both FS CCC-W-408D and ASTM F 793 include the same criteria and test for mildew resistance.

A. Vinyl Wall-Covering Standards:  Provide[ mildew-resistant] products complying with the following:

Retain one type option in first subparagraph below.  See Evaluations for descriptions of FS CCC-W-408D and CFFA-W-101-D.

1. [FS CCC-W-408D and ]CFFA-W-101-D for [Type I, Light] [Type II, Medium] [Type III, Heavy]-Duty products.

Retain one category option in first subparagraph below.  Coordinate with standards above.  See Evaluations for descriptions of categories.  Delete subparagraph if manufacturers selected do not test their products for compliance with ASTM F 793.

2. ASTM F 793 for [peelable] [strippable] wall coverings that qualify as [Category I, Decorative Only] [Category II, Decorative with Medium Serviceability] [Category III, Decorative with High Serviceability] [Category IV, Type I, Commercial Serviceability] [Category V, Type II, Commercial Serviceability] [Category VI, Type III, Commercial Serviceability] products.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Division 1 Section "Product Requirements."

3. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. <Insert manufacturer's name; product name or designation>.

Coordinate first paragraph below with CFFA-W-101-D type.

B. Total Weight Excluding Coatings:  <Insert weight>.

C. Width:  [27 inches (686 mm)] [54 inches (1372 mm)] <Insert width>.

Retain first paragraph below if vinyl wall covering selected has fabric backing; delete if paper backing.  Coordinate backing material below with CFFA-W-101-D type.  Verify, with manufacturers, availability of backing used with wall covering selected.

D. Backing:  [Scrim] [Osnaburg] [Drill] [Nonwoven] fabric.

1. Fiber Content:  [Cotton] [Polyester] [Polycotton] [Polyester cellulose] <Insert fiber content>.

E. Repeat:  [Random] <Insert horizontal and vertical dimensions of repeat>.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  First paragraph below is optional coating and may limit selection.  Verify, with manufacturer, availability of stain-resistant coating.  Other coatings may not be as effective as DuPont's Tedlar, but they can significantly improve stain resistance of a wall covering for substantially less expense.

F. Stain-Resistant Coating:  <Insert coating manufacturer's name; product name or designation>.

Retain paragraph below unless manufacturer's product name or designation indicates color, texture, and pattern.

G. Colors, Textures, and Patterns:  [Match Architect's samples] [As selected by Architect from manufacturer's full range].

2.3 WOVEN GLASS-FIBER WALL COVERING <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

A. General:

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Division 1 Section "Product Requirements."

1. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. <Insert manufacturer's name; product name or designation>.

B. Total Weight:  <Insert weight>.

1. Width:  [39 inches (991 m)] <Insert width>.

Retain paragraph below unless manufacturer's product name or designation indicates color, texture, and pattern.

C. Colors, Textures, and Patterns:  [Match Architect's samples] [As selected by Architect from manufacturer's full range].

2.4 TEXTILE WALL COVERING <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

Retain one category option in first paragraph below.  See Evaluations for descriptions of categories.  Delete paragraph if manufacturers selected do not test their products for compliance with ASTM F 793, but consider inserting test methods and requirements for critical characteristics such as stain resistance.

A. Wall-Covering Standard:  Provide [mildew-resistant] [peelable] [strippable] wall coverings that comply with ASTM F 793 for [Category I, Decorative Only] [Category II, Decorative with Medium Serviceability] [Category III, Decorative with High Serviceability] [Category IV, Type I, Commercial Serviceability] [Category V, Type II, Commercial Serviceability] [Category VI, Type III, Commercial Serviceability] products.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Division 1 Section "Product Requirements."

1. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. <Insert manufacturer's name; product name or designation>.

B. Test Responses:

Both subparagraphs below represent requirements for textile wall coverings per AATCC.  See Evaluations for additional information.

1. Colorfastness to Wet and Dry Crocking:  Passes AATCC 8, Grade 3, minimum.

2. Colorfastness to Light:  Passes AATCC 16, Option 1 or 3, Grade 4, minimum, at 40 hours.

C. Total Weight Excluding Coatings:  <Insert weight>.

D. Width:  <Insert width>.

E. Repeat:  [Random] <Insert horizontal and vertical dimensions of repeat>.

F. Applied Backing Material:  [Acrylic] [Paper].

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  First paragraph below is optional coating and may limit selection.  Verify, with manufacturer, availability of stain-resistant coating.

G. Stain-Resistant Coating:  <Insert coating manufacturer's name; product name or designation>.

Retain paragraph below unless manufacturer's product name or designation indicates color, texture, and pattern.

H. Colors, Textures, and Patterns:  [Match Architect's samples] [As selected by Architect from manufacturer's full range].

2.5 HEAVY-DUTY SYNTHETIC TEXTILE WALL COVERING <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

Retain one category option in first paragraph below.  See Evaluations for descriptions of categories.  Delete paragraph if manufacturers selected do not test their products for compliance with ASTM F 793, but consider inserting test methods and requirements for critical characteristics such as stain resistance.

A. Wall-Covering Standard:  Provide[ mildew-resistant] wall coverings that comply with ASTM F 793 for [Category IV, Type I, Commercial Serviceability] [Category V, Type II, Commercial Serviceability] [Category VI, Type III, Commercial Serviceability] products.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Division 1 Section "Product Requirements."

1. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. <Insert manufacturer's name; product name or designation>.

B. Test Responses:

Both subparagraphs below represent requirements for textile wall coverings per AATCC.  See Evaluations for additional information.

1. Colorfastness to Wet and Dry Crocking:  Passes AATCC 8, Class 3, minimum.

2. Colorfastness to Light:  Passes AATCC 16A or AATCC 16E, Class 4, minimum, at 40 hours.

C. Total Weight:  <Insert weight>.

D. Width:  [54 inches (1372 mm)] [60 inches (1524 mm)] <Insert width>.

Retain paragraph below unless manufacturer's product name or designation indicates color, texture, and pattern.

E. Colors, Textures, and Patterns:  [Match Architect's samples] [As selected by Architect from manufacturer's full range].

2.6 WOOD-VENEER WALL COVERING <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

A. General:

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Division 1 Section "Product Requirements."

1. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. <Insert manufacturer's name; product name or designation>.

B. Sheet Size:  [24 by 96 inches (610 by 2440 mm)] [48 by 96 inches (1220 by 2440 mm)] [48 by 120 inches (1220 by 3050 mm)] <Insert dimensions>.

C. Veneer Construction:  [Single ply veneer] [Two veneer plies assembled perpendicular to one another] <Insert construction>.

D. Wood Species:  [Red oak] [Maple] [Cherry] <Insert species>.

E. Cut and Figure:  <Insert cut and figure>.

F. Veneer Match:  [Book] [Slip] <Insert matching>.

G. Sheet Match:  [Running] [Balance] [Center] [Sequence, as indicated] [Blueprint, as indicated].

H. Applied Backing Material:  [Fabric] <Insert material>.

Retain paragraph below if wall-covering manufacturer's standard finish is required.  Delete if custom finish is specified in another Section.

I. Finish:  [Factory] [Field] applied using wall-covering manufacturer's standard [stain and polyurethane] <Insert type> system.

Retain subparagraph below unless manufacturer's product name or designation indicates color.

1. Colors:  [Match Architect's samples] [As selected by Architect from manufacturer's full range].

2.7 WALLPAPER <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

Retain one category option in first paragraph below.  See Evaluations for descriptions of categories.  Delete paragraph if manufacturers selected do not test their products for compliance with ASTM F 793, but consider inserting test methods and requirements for critical characteristics such as stain resistance.

A. Wall-Covering Standard:  Provide [mildew-resistant] [peelable] [strippable] wallpaper that complies with ASTM F 793 for [Category I, Decorative Only] [Category II, Decorative with Medium Serviceability] [Category III, Decorative with High Serviceability] products.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Division 1 Section "Product Requirements."

1. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. <Insert manufacturer's name; product name or designation>.

B. Total Weight:  <Insert weight>.

C. Width:  [20-1/2 inches (520.7 mm)] [28 inches (711.2 mm)] <Insert width>.

D. Repeat:  [Random] <Insert horizontal and vertical dimensions of repeat>.

Retain paragraph below unless manufacturer's product name or designation indicates color, texture, and pattern.

E. Colors, Textures, and Patterns:  [Match Architect's samples] [As selected by Architect from manufacturer's full range].

2.8 ACCESSORIES

Retain second option in first paragraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.  VOC limit is that for adhesives for porous materials other than wood.  Note that for wood-veneer wall coverings, it is the backing material rather than the wood that is being adhesively applied.

A. Adhesive:  Mildew-resistant, nonstaining[, strippable] adhesive, for use with specific wall covering and substrate application; as recommended in writing by wall-covering manufacturer and with a VOC content of [50] <Insert value> g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

Retain first paragraph below and insert primer requirements in the appropriate painting Section or revise and insert requirements here.

B. Primer/Sealer:  Mildew resistant, complying with requirements in Division 9 Section "[Interior Painting] <Insert Section title>" and recommended in writing by wall-covering manufacturer for intended substrate.

Retain paragraph above or first paragraph below, or delete both if not required to correct inadequate substrate conditions.

C. Wall Liner:  Nonwoven, synthetic underlayment and adhesive as recommended by wall-covering manufacturer.

D. Seam Tape:  As recommended in writing by wall-covering manufacturer.

Revise metal primer in paragraph below as required to suit metal surfaces over which wall coverings will be applied.

E. Metal Primer:  Interior ferrous metal primer complying with Division 9 Section "[Interior Painting] <Insert Section title>."

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine substrates and conditions, with Installer present, for compliance with requirements for levelness, wall plumbness, maximum moisture content, and other conditions affecting performance of the Work.

B. Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 PREPARATION

A. Comply with manufacturer's written instructions for surface preparation.

B. Clean substrates of substances that could impair bond of wall covering, including dirt, oil, grease, mold, mildew, and incompatible primers.

C. Prepare substrates to achieve a smooth, dry, clean, structurally sound surface free of flaking, unsound coatings, cracks, and defects.

1. Moisture Content:  Maximum of 5 percent on new plaster, concrete, and concrete masonry units when tested with an electronic moisture meter.

2. Plaster:  Allow new plaster to cure.  Neutralize areas of high alkalinity.  Prime with primer as recommended in writing by primer/sealer manufacturer and wall-covering manufacturer.

3. Metals:  If not factory primed, clean and apply metal as recommended in writing by primer/sealer manufacturer and wall-covering manufacturer.

Retain first subparagraph below if priming of gypsum-board surfaces is not performed under another Section.

4. Gypsum Board:  Prime with primer as recommended in writing by primer/sealer manufacturer and wall-covering manufacturer.

5. Painted Surfaces:  Treat areas susceptible to pigment bleeding.

D. Check painted surfaces for pigment bleeding.  Sand gloss, semigloss, and eggshell finish with fine sandpaper.

E. Remove hardware and hardware accessories, electrical plates and covers, light fixture trims, and similar items.

F. Acclimatize wall-covering materials by removing them from packaging in the installation areas not less than 24 hours before installation.

Retain paragraph below if required to correct inadequate substrate conditions.

G. Install wall liner, with no gaps or overlaps, where required by wall-covering manufacturer.  Form smooth wrinkle-free surface for finished installation.  Do not begin wall-covering installation until wall liner has dried.

3.3 INSTALLATION

A. General:  Comply with wall-covering manufacturers' written installation instructions applicable to products and applications indicated except where more stringent requirements apply.

B. Cut wall-covering strips in roll number sequence.  Change roll numbers at partition breaks and corners.

C. Install strips in same order as cut from roll.

Retain last paragraph above unless otherwise recommended by wall-covering manufacturer, and delete first paragraph below.  Method specified below may be recommended by wall-covering manufacturer for products that are solidly colored, evenly textured, or random-matched patterned to enhance color uniformity among strips.

D. Install reversing every other strip.

E. Install wall covering with no gaps or overlaps, no lifted or curling edges, and no visible shrinkage.

Retain first paragraph below for patterns that require matching; revise to suit Project.

F. Match pattern 72 inches (1830 mm) above the finish floor.

Revise first paragraph below if railroading (horizontal application) is required.

G. Install seams vertical and plumb at least 6 inches (150 mm) from outside corners and [3 inches (75 mm)] [6 inches (150 mm)] from inside corners unless a change of pattern or color exists at corner.  No horizontal seams are permitted.

H. Fully bond wall covering to substrate.  Remove air bubbles, wrinkles, blisters, and other defects.

I. Trim edges and seams for color uniformity, pattern match, and tight closure.  Butt seams without any overlay or spacing between strips.

3.4 FIELD FINISHING OF WOOD-VENEER WALL COVERINGS

Retain this article if wall-covering manufacturer's standard finish is required.  Delete if custom finish is specified in another Section.

A. Apply [wall-covering manufacturer's standard stain and polyurethane] <Insert type> system according to coating manufacturer's written instructions to produce finish that is consistent in color and gloss and matches approved Samples.

B. Apply no fewer than [two] [three] finish coats.

3.5 CLEANING

A. Remove excess adhesive at finished seams, perimeter edges, and adjacent surfaces.

B. Use cleaning methods recommended in writing by wall-covering manufacturer.

C. Replace strips that cannot be cleaned.

D. Reinstall hardware and hardware accessories, electrical plates and covers, light fixture trims, and similar items.

END OF SECTION 09720

WALL COVERINGS
09720 - 1

