Limestone Paving Specification

1. Prepare a compacted base of sandy clay, or if using native material add soil cement or lime. Geotextile fabric could be beneficial but is not necessary.

2. Install 2” 6/10 limestone.

3. Install 1” to 1 ½” #57 limestone over the 6/10.

CONSTRUCTION METHODS:

The base material shall be placed on the prepared subgrade in

uniform courses with the compacted thickness to be no more than 7 inches. Material deposited on the subgrade shall be spread and shaped the same day.

The course shall then be sprinkled as required and rolled as directed until a uniform compaction is secured.

Through this entire operation, the shape of the course shall be maintained by blading and the surface, upon

completion, shall be smooth and in conformance with the typical sections shown on the plans and to the

established lines and grades. 

All irregularities, depressions or weak spots which develop shall be corrected immediately by scarifying the area affected, adding suitable material as required, and reshaping and

recompacting by sprinkling and rolling. Material excavated in preparation of the subgrade may be utilized in the construction of adjacent shoulders and slopes or otherwise disposed of as directed, and any additional material required for the completion of the shoulders and slopes shall be secured from approved sources.

Each course of base shall be compacted to a minimum density of 100 percent (100%).

THICKNESS CONTROL:

 The thickness of the compacted flexible base may vary from a maximum of 1/2 inches less than specified to a maximum of 1 inch more than specified. Deviations not within this

tolerance shall be corrected.
