
SECTION 02510PRIVATE 


ASPHALTIC CONCRETE PAVING

1 PART 1 GENERAL


.1

SECTION INCLUDES



A.
Asphaltic concrete paving and surface sealer; wearing binder or base course.



B.
Aggregate base course.


.2

PRODUCTS INSTALLED BUT NOT FURNISHED UNDER THIS SECTION





Not Used


.3

RELATED SECTIONS




A.
Section 09900 ‑ Painting:  Pavement markings.


.4

UNIT PRICE ‑ MEASUREMENT AND PAYMENT





Not Used




.5

REFERENCES



A.
MS‑2 ‑ Mix Design Methods for Asphalt Concrete and Other Hot Mix Types ‑ The Asphalt Institute (AI).



B.
MS‑3 ‑ Asphalt Plant Manual ‑ The Asphalt Institute (AI).



C.
MS‑8 ‑ Asphalt Paving Manual ‑ The Asphalt Institute (AI).



D.
MS‑19 ‑ Basic Asphalt Emulsion Manual, The Asphalt Institute (AI).



E.
ASTM D946 ‑ Penetration‑Graded Asphalt Cement for Use in Pavement Construction.


.6

PERFORMANCE REQUIREMENTS



A.
Paving:  Designed for traffic.


.7

QUALITY ASSURANCE



A.
Perform Work in accordance with AI Manual MS‑8.



B.
Mixing Plant:  Conform to La DOTD Manual.



C.
Obtain materials from same source throughout.



D.
Maintain one copy of document on site.


.8

REGULATORY REQUIREMENTS



A.
Conform to applicable code for paving work.  


.9

ENVIRONMENTAL REQUIREMENTS



A.
Do not place asphalt when base surface temperature is less than 40 degrees F (4 degrees C), or surface is wet or frozen.

2 PART 2 PRODUCTS


.1

MATERIALS (See drainage)



A.
Asphalt Cement: In accordance with LA DOTD standards.



B.
Aggregate for Binder Course Mix:
In accordance with LA DOTD Standards.



C.
Aggregate for Wearing Course Mix:  In accordance with LA DOTD Standards.



D.
Fine Aggregate: In accordance with LA DOTD Standards.



E.
Mineral Filler: Finely ground particles of limestone, hydrated lime or other mineral dust, free of foreign matter.


.2

ACCESSORIES



A.
Primer: In accordance with LA DOTD Standards.



B.
Tack Coat: In accordance with LA DOTD Standards.



C.
Seal Coat: In accordance with LA DOTD Standards.


.3

ASPHALT PAVING MIX



A.
Use dry material to avoid foaming.
Mix uniformly.



B.
Wearing Course: In accordance with LA DOTD Standards.


.4

SOURCE QUALITY CONTROL





Not Used



3 PART 3 EXECUTION


.1

EXAMINATION



A.
Verify base conditions.



B.
Verify that compacted sub grade & Base Layer is dry and ready to support paving and imposed loads.



C. Verify that entire existing surface has been treated with 

Grass killer and that all larger vegetation has been removed.


.2

SUBBASE





Not Used


.3

PREPARATION - PRIMER





Not Used


.4

PREPARATION ‑ TACK COAT





Not Used




.5

PLACING ASPHALT PAVEMENT ‑ SINGLE COURSE



A.
Install Work in accordance with LA DOTD Standards.



B.
Develop rolling with consecutive passes to achieve even and smooth finish, without roller marks.


.6

PLACING ASPHALT PAVEMENT ‑ DOUBLE COURSE





Not Used



.7

CURBS





Not Used


.8

SEAL COAT



A.
Install work in accordance with LA DOTD standards.


.9

PAINT STRIPPING



A.
Install work in accordance with LA DOTA standards.


.10
FIELD QUALITY CONTROL





Not Used


.11
PROTECTION



A.
Immediately after placement, protect pavement from mechanical injury for 2 days.


.12

SCHEDULES





Not Used









END OF SECTION

PAGE  
Error! Main Document Only.
Section 02510 Page 3 of 3      

