
SECTION 05500PRIVATE 


METAL FABRICATIONS

Provisions of the contract including General and Supplementary General Conditions and the General Requirements apply to the work of this section.
1 PART 1   GENERAL


.1

SECTION INCLUDES



A.
Shop fabricated ferrous metal galvanized and prime painted.


.2

seq level2 \h \r0 

PRODUCTS FURNISHED BUT NOT INSTALLED UNDER THIS SECTION




Not Used


.3

seq level2 \h \r0 

RELATED SECTIONS



A.
Section 05520 ‑ Handrails and Railings.



B.
Section 09900 ‑ Painting: Paint finish.



C.
Reference of General Conditions.

.4

seq level2 \h \r0 

REFERENCES



A.
ASTM A36 ‑ Structural Steel.



B.
ASTM A53 ‑ Hot‑Dipped, Zinc‑coated Welded and Seamless Steel Pipe.



C.
ASTM A123 ‑ Zinc (Hot‑Galvanized) Coatings on Products Fabricated From Rolled, Pressed and Forged Steel Shapes, Plates, Bars, and Strip.



D.
ASTM A153 ‑ Zinc Coating Hot‑Dip on Iron and Steel Hardware.



E.
ASTM A283 ‑ Carbon Steel Plates, Shapes, and Bars.



F.
ASTM A307 ‑ Carbon Steel Externally Threaded Standard Fasteners.



G.
ASTM A325 ‑ High Strength Bolts for Structural Steel Joints.



H.
ASTM A386 ‑ Zinc‑Coating (Hot‑Dip) on Assembled Steel Products.



I.
ASTM A500 ‑ Cold‑Formed Welded and Seamless Carbon Steel Structural Tubing in Round and Shapes.



J.
ASTM A501 ‑ Hot‑Formed Welded and Seamless Carbon Steel Structural Tubing.



K.
ASTM B177 ‑ Chromium Electroplating on Steel for Engineering Use.



L.
AWS A2.0 ‑ Standard Welding Symbols.



M.
AWS D1.1 ‑ Structural Welding Code.



N.
SSPC ‑ Steel Structures Painting Council.


.5
seq level2 \h \r0 
SUBMITTALS



A.
Submit under provisions of Section 01300.



B.
Shop Drawings: Indicate profiles, sizes, connection attachments, reinforcing, anchorage, size and type of fasteners, and accessories.  Include erection drawings, elevations, and details where applicable.



C.
Indicate welded connections using standard AWS A2.0 welding symbols.  Indicate net weld lengths.


.6

seq level2 \h \r0 

QUALIFICATIONS



A.
Prepare Shop Drawings under direct supervision of a Professional Structural Engineer experienced in design of this work and licensed in the State of Louisiana.



B.
Welders' Certificates: Submit under provisions of Section 01300, certifying welders employed on the Work, verifying AWS qualification within the previous 12 months.


.7

seq level2 \h \r0 

FIELD MEASUREMENTS



A.
Verify that field measurements are as indicated on shop drawings.

2

seq level1 \h \r0 

seq level2 \h \r0  PART 2   PRODUCTS


.1

MATERIALS



A.
Steel Sections: ASTM A36.



B.
Steel Tubing: ASTM A500, Grade B.



C.
Pipe:  ASTM A53, Grade Schedule 40.



D.
Bolts, Nuts, and Washers: ASTM A325 galvanized to ASTM           

A153 for galvanized components.




E.
Welding Materials: AWS D1.1; type required for materials being welded.




seq level0 \h \r2 

seq level1 \h \r1 

seq level2 \h \r7 

seq level3 \h \r0 

seq level4 \h \r0 

seq level5 \h \r0 

seq level6 \h \r0 

seq level7 \h \r0 F.
Touch‑Up Primer for Galvanized Surfaces: Zinc rich type.


.2

seq level2 \h \r0 

FABRICATION



A.
Fit and shop assemble in largest practical sections, for delivery to site.



B.
Fabricate items with joints tightly fitted and secured.



C.
Continuously seal joined members by continuous welds.



D.
Grind exposed joints flush and smooth with adjacent finish surface.  Make exposed joints butt tight, flush, and hairline.  Ease exposed edges to small uniform radius.



E.
Exposed Mechanical Fastenings: Flush countersunk screws or bolts; unobtrusively located; consistent with design of component, except where specifically noted otherwise.



F.
Supply components required for anchorage of fabrications. Fabricate anchors and related components of same material and finish as fabrication, except where specifically noted otherwise.


.3
seq level2 \h \r0 
FINISHES



A.
Prepare surfaces to be primed in accordance with SSPC SP 2.



B.
All exposed metal surfaces shall be galvanized.

3

seq level1 \h \r0 

seq level2 \h \r0  PART 3   EXECUTION


.1

EXAMINATION



A.
Verify that field conditions are acceptable and are ready to receive work.



B.
Beginning of installation means erector accepts existing conditions.


.2

seq level2 \h \r0 

PREPARATION



A.
Clean and strip primed steel items to bare metal where site welding is required.



B.
Supply items required to be cast into concrete with setting templates, to appropriate sections.


.3

seq level2 \h \r0 

INSTALLATION



A.
Install items plumb and level, accurately fitted, free from distortion or defects.



B.
Allow for erection loads, and for sufficient temporary bracing to maintain true alignment until completion of erection and installation of permanent attachments.



C.
Field weld components indicated on drawings, shop drawings. 



D.
Perform field welding in accordance with AWS D1.1.



E.
Obtain Architect/Engineer approval prior to site cutting or making adjustments not scheduled.



F.
After erection, prime welds, abrasions, and surfaces not shop primed , except surfaces to be in contact with concrete.


.4

seq level2 \h \r0 

ERECTION TOLERANCES



A.
Maximum Variation from Plumb: 1/4 inch per story, non‑cumulative.



B.
Maximum Offset From True Alignment: 1/4 inch.


.5

seq level2 \h \r0 

SCHEDULE



A.
The Schedule is a list of principal items only.  Refer to drawing details for items not specifically scheduled.



B.
Bumper Posts and guardrails: As detailed; prime paint finish.



C.
Bollards:  Steel pipe, concrete filled, crowned cap, as detailed; galvanized finish.


END OF SECTION
PAGE  
Section 05500 Page 1 of 4

