
SECTION 06114PRIVATE 


WOOD BLOCKING AND CURBING

Provisions of the contract including General and Supplementary General Conditions and the General Requirements apply to the work of this section.
1 PART 1 GENERAL


.1

SECTION INCLUDES



A.
Wood furring and grounds.



B.
Concealed wood blocking for support of toilet and bath accessories wall cabinets wood trim.



C.
Telephone and electrical panel boards.



D.
Preservative treatment of wood.


.2

REFERENCES



A.
ALSC ‑ American Lumber Standards Committee: Softwood Lumber Standards.



B.
APA:  American Plywood Association.



C.
AWPA (American Wood Preservers Association) C1 ‑ All Timber Products Preservative Treatment by Pressure Process.



D.
AWPA (American Wood Preservers Association) C20 ‑ Structural Lumber Fire Retardant Treatment by Pressure Process.



E.
NFPA:  National Forest Products Association.



F.
RIS:  Redwood Inspection Service.



G.
SPIB:  Southern Pine Inspection Bureau.



H.
WCLIB:
West Coast Lumber Inspection Bureau.

I. WWPA:  Western Wood Products Association.

J.
Reference to General Conditions.


.3

SUBMITTALS



A.
Submit under provisions of Section 01300.



B.
Product Data:  Provide technical data on wood preservative materials and application instructions.


.4

QUALITY ASSURANCE



A.
Perform Work in accordance with the following agencies:




1.
Lumber Grading Agency:
Certified by ALSC.




2.
Plywood Grading Agency:  Certified by APA.

2 PART 2 PRODUCTS


.1

MATERIALS



A.
Lumber Grading Rules:  SPIB.



B.
Miscellaneous Framing:  S.Y.P. species, 15 percent maximum moisture content, pressure preservation treat..



C.
Plywood:  APA Rated Sheathing, Grade C‑ D Ext.


.2

ACCESSORIES



A.
Fasteners and Anchors:




1.
Fasteners:  Hot‑dipped galvanized steel for high humidity and treated wood locations, unfinished steel elsewhere.




2.
Anchors:
Toggle bolt type for anchorage to hollow masonry. Expansion shield and lag bolt type for anchorage to solid masonry or concrete. Bolt or ballistic fastener for anchorage to steel.


.3

FACTORY WOOD TREATMENT



A. 
Wood Preservative (Pressure Treatment): AWPA Treatment C1 using  water borne preservative with 0.25 percent retainage.

3 PART 3 EXECUTION


.1

FRAMING



A.
Set members level and plumb, in correct position.



B.
Place horizontal members flat, crown side up.



C.
Construct curb members of single pieces.



D.
Space framing and furring 16 inches (400 to 600 mm) o.c.



E.
Curb roof openings except where prefabricated curbs are provided.  Form corners by alternating lapping side members.


.2

SHEATHING



A.
Install telephone and electrical panel boards with plywood sheathing material where required.  Over size the panel by 12 inches (300 mm) on all sides.


END OF SECTION
4
Section 06114 Page 1 of 3
Error! Main Document Only.

