
SECTION 07212PRIVATE 


BOARD INSULATION

1 PART 1   GENERAL


.1

SECTION INCLUDES



A.
Board insulation exterior wall behind brick veneer wall finish.


B.
Board insulation between roof desk and roofing.

.2

seq level2 \h \r0 

REFERENCES


A.
ANSI/ASTM D2842 ‑ Water Absorption of Rigid Cellular Plastics.



B.
ASTM C240 ‑ Testing Cellular Glass Insulating Block.



C.
ASTM C578 ‑ Preformed Cellular Polystyrene Thermal Insulation.



D.
ASTM E96 ‑ Test Methods for Water Vapor Transmission of Materials.



E.
FS HH‑I‑530 ‑ Insulation Board, Thermal, Unfaced, Polyurethane or Polyisocyanurate.



F.
FS HH‑I‑551 ‑ Insulation Block and Boards, Thermal (Cellular Glass).



G.
FS HH‑I‑1972/GEN ‑ Insulation Board, Thermal, Faced, 




Polyurethane or Polyisocyanurate.


.3
seq level2 \h \r0 
PERFORMANCE REQUIREMENTS



A.
Materials of this Section shall provide continuity of thermal barrier at building enclosure elements.

.4
seq level2 \h \r0 
SUBMITTALS



A.
Submit under provisions of Section 01300.



B.
Product Data: Provide data on product characteristics, performance criteria, limitations.



C.
Manufacturer's Installation Instructions: Indicate special environmental conditions required for installation, installation techniques.


.5
seq level2 \h \r0 

seq level2 \h \r0 
ENVIRONMENTAL REQUIREMENTS



A.
Do not install insulation adhesives when temperature or weather conditions are detrimental to successful installation.


.6




A.
Coordinate work under provisions of Section 01039.

2

seq level1 \h \r0 

seq level2 \h \r0  PART 2   PRODUCTS


.1
seq level2 \h \r0 
INSULATION MATERIALS



A.
Polystyrene Insulation  Type B: ASTM 0578 Type VI extruded cellular type, conforming to the following:



Thermal Resistance

 R 3.0



Thickness



 ½” Thick 



Board Size



 4ft x 8ft  




Compressive Strength
 
 Minimum 30 psi
(210 KPA)





  




Water Absorption

 
 In accordance with ANSI/ASTM










 D2842 0.3 percent by volume







                  maximum




Edges




 Square edges.




Fire Rating



 Meet FS25 or Better Specs

.2
seq level2 \h \r0 
ADHESIVES



A.
Adhesive:  Type recommended by insulation manufacturer for application.

.3
seq level2 \h \r0 
ACCESSORIES



A.
Sheet Barrier:  Black polyethylene film for above grade application, 20 mil thick; Secure to wall with asphaltic wall parge adhesive. 




3

seq level1 \h \r0 

seq level2 \h \r0  PART 3   EXECUTION


.1

EXAMINATION



A.
Verify site conditions under provisions of Section 01039.


B.
Verify that substrate, adjacent materials, and insulation boards are dry and ready to receive insulation and adhesive.



C.
Verify substrate surface is flat, free of irregularities materials or substances that may impede adhesive bond.


.2

seq level2 \h \r0 

INSTALLATION ‑ CAVITY WALLS


A.
Adhere a 12-inch wide strip of polyethylene sheet over control joint with double beads of Type adhesive each side of joint between sheets.  Extend sheet full height of joint.


B.
Apply adhesive in three continuous beads per board length.  Daub adhesive tight to protrusions to ensure continuity of vapor and air barrier.


C.
Install boards horizontally.


D.
Place boards in a method to maximize contact bedding. Stagger end joints.  Butt edges and ends tight to adjacent board and no protrusions. 


E.
Place 12-inch wide polyethylene sheet at perimeter of wall openings from adhesive vapor and air barrier bed to window and door frame.  Tape seal in place to ensure continuity of vapor/air barrier.

.3

INSTALLATION – ROOF



A.
Lay directly on roof with 20-mil meruasteol over insulation.  Between runners at 4’- 0” oc.



seq level2 \h \r0 




.3
PROTECTION OF FINISHED WORK



A.
Protect finished Work under provisions of Section 01500. 



B.
Do not permit Work to be damaged prior to covering insulation.


END OF SECTION
PAGE  
Section 07212 Page 3 of 3

