

SECTION 07900PRIVATE 


JOINT SEALERS

Provisions of the contract including General and Supplementary General Conditions and the General Requirements apply to the work of this section.
PART 1

GENERAL

.1

SECTION INCLUDES


A.
Preparing substrate surfaces.


B.
Sealant and joint backing.

.2

seq level2 \h \r0 

RELATED SECTIONS


A.
Section 02520 – Concrete Paving: Sealers required in conjunction with masonry. 


B.
Section 04300 – Unit Masonry: Sealants required in conduction with masonry.


C.
Section 07465 – Preformed Metal Siding: Sealants required in conjunction with masonry.


D.
Section 07611 – Sheet Metal Roofing: Sealants required in conjunction with roofing.


E.
Section 07620 – Sheet Metal Flashing: Sealants required in conjunction with metal flashings.


F.
Section 08112 – Steel Frames: Sealants required in conjunction with doorframes.


G.
Section 08520 – Aluminum Windows: Sealants required in conjunction with aluminum.


H.
Section 08800 ‑ Glazing: Sealants required in conjunction with glazing methods.


F.
Reference to General Conditions.
.3
seq level2 \h \r0 
REFERENCES


A.
ASTM C790 ‑ Use of Latex Sealing Compounds.


B.
ASTM C804 ‑ Use of Solvent‑Release Type Sealants.


C.
ASTM C834 ‑ Latex Sealing Compounds.


D.
ASTM C919 ‑ Use of Sealants in Acoustical Applications.


E.
ASTM C920 ‑ Elastomeric Joint Sealants.


F.
ASTM D1056 ‑ Flexible Cellular Materials ‑ Sponge or Expanded Rubber.


G.
ASTM D1565 ‑ Flexible Cellular Materials ‑ Vinyl Chloride Polymers and Copolymers (Open‑Cell Foam).


H.
SWRI (Sealant, Waterproofing and Restoration Institute) ‑ Sealant and Caulking Guide Specification.

.4

seq level2 \h \r0 

SUBMITTALS


A.
Submit under provisions of Section 01300.


B.
Product Data: Provide data indicating sealant chemical characteristics, performance criteria, substrate preparation, limitations, color availability.


C.
Manufacturer's Installation Instructions: Indicate special procedures, surface preparation, perimeter conditions requiring special attention.


.5

seq level2 \h \r0 

QUALITY ASSURANCE



A.
Perform work in accordance with sealant manufacturer's requirements for preparation of surfaces and material installation instructions.

.6
seq level2 \h \r0 
ENVIRONMENTAL REQUIREMENTS


A.
Maintain temperature and humidity recommended by the sealant manufacturer during and after installation.

.7
seq level2 \h \r0 
COORDINATION


A.
Coordinate work under provisions of Section 01039.


B.
Coordinate the work with all sections referencing this section.

.8
seq level2 \h \r0 
WARRANTY


A.
Provide five-year warranty under provisions of Section 01700.


B.
Warranty:  Include coverage for installed Sealants and accessories which fail to achieve water tight seal, exhibit loss of adhesion or cohesion, or do not cure.

PART 2

seq level1 \h \r0 

seq level2 \h \r0 

PRODUCTS

.1

SEALANTS


A.
Oil Based (Type A): Single component, resinous compound, elongation capability of 0 to 2 percent of joint width; manufactured by.


B.
Bituminous Based (Type B): Single component, asphalt compound elongation capability of 0 to 2 percent of joint width.


C.
seq level3 \h \r0 Acrylic Emulsion Latex (Type C):  ASTM C834, single component; gray color.


D.
Acrylic Sealant (Type D):  single component, solvent curing, non‑staining, non‑bleeding, non‑sagging; color as selected:



1. Elongation Capability

  7.5 to 12 percent



2. Service Temperature Range
  ‑13 to 180 degrees F (‑25 to 








          82 to degrees C)



3. Shore A Hardness Range
  25 to 50


E.
seq level3 \h \r0 Butyl Sealant (Type E): single component, solvent release, non‑skinning, non‑sagging, black color.



1.
Elongation Capability

7 to 10 percent



2.
Service Temperature Range
‑13 to 180 degrees F (‑25 to 82 degrees C)



3.
Shore A Hardness Range

10 to 30


F.
seq level3 \h \r0 Polysulfide Sealant (Type F): two component, chemical curing, non‑staining, non‑bleeding, capable of continuous water immersion, non‑sagging type; color as selected.



1.
Elongation Capability

25 percent



2.
Service Temperature Range
‑40 to 180 degrees F (‑40 to 82 degrees C)



3.
Shore A Hardness Range

20 to 35


G.
seq level3 \h \r0 Polyurethane Sealant (Type G): single component, chemical curing, non‑staining, non‑bleeding, capable of continuous water immersion, non‑sagging type; color as selected.



1.
Elongation Capability

25 percent



2.
Service Temperature Range
‑40 to 180 degrees F (‑40 to 82 degrees C)



3.
Shore A Hardness Range

20 to 35


H.
seq level3 \h \r0 Polyurethane Sealant (Type H): multi‑component, chemical curing, non‑staining, non‑bleeding, capable of continuous water immersion, non‑sagging; color as selected.



1.
Elongation Capability

25 percent



2.
Service Temperature Range
‑40 to 180 degrees F (‑40 to 82 degrees C)



3.
Shore A Hardness Range

20 to 35


I.
seq level3 \h \r0 Silicone Sealant (Type I): single component, solvent curing, non‑sagging, non‑staining, fungus resistant, non‑bleeding; color as selected.



1.
Elongation Capability

25 percent



2.
Service Temperature Range
‑65 to 180 degrees F (‑54 to 82 degrees C)



3.
Shore A Hardness Range

15 to 35


J.
seq level3 \h \r0 Silicone Sealant (Type J): single component, fungus resistant, chemical curing, non‑sagging, non‑staining, non‑bleeding; color as selected.



1.
Elongation Capability

25 percent



2.
Service Temperature Range
‑65 to 180 degrees F (‑54 to 82 degrees C)



3.
Shore A Hardness Range

15 to 25


K.
seq level3 \h \r0 Silicone Sealant (Type K): single component, fungus resistant, acidic curing, non‑sagging, non‑staining, non‑bleeding; color as selected.



1.
Elongation Capability

25 percent



2.
Service Temperature Range
‑65 to 180 degrees F (‑54 to 82 degrees C)



3.
Shore A Hardness Range

15 to 25

.2
seq level2 \h \r0 

seq level3 \h \r0 
ACCESSORIES


A.
Joint Cleaner: Non‑corrosive and non‑staining type, recommended by sealant manufacturer; compatible with joint forming materials.


B.
Joint Backing: ASTM D1056; round, closed cell polyethylene  foam rod; oversized 30 to 50 percent larger than joint width.


C.
Bond Breaker: Pressure sensitive tape recommended by sealant manufacturer to suit application.

PART 3
seq level1 \h \r0 

seq level2 \h \r0 
EXECUTION

.1

EXAMINATION


A.
Verify that substrate surfaces and joint openings are ready to receive work.


B.
Verify that joint backing and release tapes are compatible with sealant.

.2
seq level2 \h \r0 
PREPARATION


A.
Remove loose materials and foreign matter, which might impair adhesion of sealant.


B.
Clean joints in accordance with manufacturer's instructions.


C.
Perform preparation in accordance with manufacturer's instructions.


D.
Protect elements surrounding the work of this section from damage or disfiguration.

.3

seq level2 \h \r0 

INSTALLATION


A.
Install sealant in accordance with manufacturer's instructions.


B.
Measure joint dimensions and size materials to achieve required width/depth ratios.


C.
Install joint backing to achieve a neck dimension no greater than 1/3 of the joint width.


D.
Install bond breaker where joint backing is not used.


E.
Install sealant free of air pockets, foreign embedded matter, ridges, and sags.


F.
Apply sealant within recommended application temperature ranges.  Consult manufacturer when sealant cannot be applied within these temperature ranges.


G.
Tool joints concave channel shaped.

.4
seq level2 \h \r0 
CLEANING


A.
Clean work under provisions of 01700.


B.
Clean adjacent soiled surfaces.

.5

seq level2 \h \r0 

PROTECTION OF FINISHED WORK


A.
Protect finished installation under provisions of Section 01500.


B.
Protect Sealants until cured.

.6
seq level2 \h \r0 
SCHEDULE


Location





Type




Color


A.
Window perimeter


G




Dark Brown


B.
Metal Siding



F




to match siding/

                                                   roofing


C.
Door Frame/Walls


C




Grey


D.
Under Thresholds


E




Black


E.
Bathtub/Ceramic


I




White



Tile


F.
Paving Joints


B




Black


END OF SECTION

PAGE  
Section 07900 Page 2 of 6

