

SECTION 09311PRIVATE 


CERAMIC TILE FLOOR FINISH

Provisions of the contract including General and Supplementary General Conditions and the General Requirements apply to the work of this section.
1 PART 1   GENERAL


.1

SECTION INCLUDES



A.
Ceramic tile floor and base finish using the thinset application method.



B.
Thresholds at door openings.


.2

RELATED SECTIONS



A.
Section 09312 ‑ Ceramic Tile Wall Finish.



B.
Section 15440 - Plumbing: Floor drains.


.3

REFERENCES



A.
ANSI/TCA A108.4 ‑ Installation of Ceramic Tile with Water Resistant Organic Adhesive.



B.
ANSI/TCA A108.5 ‑ Ceramic Tile Installed with Dry‑Set Portland Cement Mortar or Latex Portland Cement Mortar.



C.
ANSI/TCA A118.1 ‑ Dry‑Set Portland Cement Mortar.



D.
ANSI/TCA A137.1 ‑ Specifications for Ceramic Tile.

E. TCA (Tile Council of America) ‑ Handbook for Ceramic Tile Installation.



F.
Reference to General Conditions.


.4

SUBMITTALS



A.
Submit shop drawings under provisions of Section 01300. 



B.
Submit product data indicating material specifications, characteristics, and instructions for using adhesives and grouts.



C.
Submit samples under provisions of Section 01300.



D.
Submit maintenance data under provisions of Section 01700.



E.  Include recommended cleaning and stain removal methods, cleaning materials.


.5

QUALITY ASSURANCE



A.
Conform to ANSI/TCA A137.1



B.
Conform to ANSI/TCA A108.4


.6

DELIVERY, STORAGE, AND HANDLING



A.
Deliver products to site under provisions of Section 01600. 01610.



B.
Store and protect products under provisions of Section 01600. 



C.
Protect adhesives from freezing or overheating in accordance with manufacturer's instructions.


.7

ENVIRONMENTAL REQUIREMENTS



A.
Do not install adhesives in a closed, unventilated environment.



B.
Maintain 50 degrees F (10 degrees C) during installation of mortar materials.

2 PART 2   PRODUCTS


.1

MANUFACTURERS ‑ TILE



A.
American Ocean



B.
Florida Tile; Natural Liberty


.2

TILE MATERIAL



A.
Ceramic Mosaic Floor Tile: ANSI/TCA A137.1, conforming to the following:




Moisture Absorption 

 0 to 0.5 percent






 




Size





 12 x 12 inch






 




Edge





 Square




Surface Finish


 Unglazed









 [Mottle glazed] [__________]




Color




 As selected









 ([___x___] mm)



B.
Base: Match mosaic floor tile for moisture absorption, surface finish, and color; 12” inch long x 12” inch high; square top edge, coved internal corner.


.3

ADHESIVE MATERIALS



A.
Organic Adhesive: ANSI/TCA A136.1, Type 1; thinset bond type.


.4

MORTAR MATERIALS



A.
Mortar Materials: ANSI/TCA A118.1; Portland cement, sand, latex additive, and water.


.5

GROUT MATERIALS



A.
 Grout: Cementitious type with latex additive.


.6

ACCESSORIES



A.
Tile Floor Edging: Ceramic, to match tile.


3 PART 3   EXECUTION


.1

EXAMINATION



A.
Verify that surfaces are ready to receive work.



B.
Beginning of installation means installer accepts condition of existing substrate.


.2

PREPARATION



A.
Protect surrounding work from damage or disfiguration.



B.
Vacuum clean existing substrate and damp clean.



C.
Seal substrate surface cracks with filler.  Level existing substrate surfaces to acceptable flatness tolerances.



D.
Apply sealer to surfaces as recommended by adhesive manufacturer.


.3

INSTALLATION ‑ THINSET METHOD



A.
Install adhesive, tile, and grout to TCA Handbook for Ceramic Tile Installation.



B.
Request tile pattern from Architect/Engineer.  Do not interrupt tile pattern through openings.



C.
Place edge strips at exposed tile edges.



D.
Cut and fit tile tight to penetrations through tile.
 Form corners and bases neatly.  Align floor, base, and wall joints.



E.
Place tile joints uniform in width, subject to variance in tolerance allowed in tile size.  Make joints watertight, without voids, cracks, excess mortar, or excess grout.



F.
Sound tile after setting.  Replace hollow sounding units.



G.
Allow tile to set for a minimum of 48 hours prior to grouting



H.
Grout tile joints.



I.
Apply sealant to junction of tile and dissimilar materials and at junction of dissimilar planes.


END OF SECTION
1
Error! Main Document Only.
Section 09311 Page 2 of 3       

