

SECTION 09900PRIVATE 


PAINTING
Provisions of the contract including General and Supplementary General Conditions and the General Requirements apply to the work of this section.
1 PART 1 GENERAL


.1

SECTION INCLUDES



A.
Surface preparation and field application of paints and coatings.


.2

seq level2 \h \r0 

RELATED SECTIONS



A.
Section 15190 ‑ Mechanical Identification.



B.
Section 16195 ‑ Electrical Identification.


.3
seq level2 \h \r0 
REFERENCES



A.
ASTM D16 ‑ Definitions of Terms Relating to Paint, Varnish, Lacquer, and Related Products.



B.
ASTM D2016 ‑ Test Method for Moisture Content of Wood.



C.
AWWA (American Water Works Association) ‑ C204 -Chlorinated Rubber‑Alkyd Paint Systems for the Exterior of Above Ground Steel Water Piping.



D.
AWWA (American Water Works Association) ‑ D102 ‑ Painting Steel Water Storage Tanks.



E.
NACE (National Association of Corrosion Engineers) -Industrial Maintenance Painting.



F.
NPCA (National Paint and Coatings Association) ‑ Guide to U.S. Government Paint Specifications.



G.
PDCA (Painting and Decorating Contractors of America) -Painting ‑ Architectural Specifications Manual.



H.
SSPC (Steel Structures Painting Council) ‑ Steel    Structures Painting Manual.


I.
Reference to General Conditions.

.4

seq level2 \h \r0 

DEFINITIONS



A.
Conform to ASTM D16 for interpretation of terms used in this Section.


.5

seq level2 \h \r0 

SUBMITTALS



A.
Submit under provisions of Section 01300.



B.
Product Data:  Provide data on all finishing products.



C.
Samples:
Submit two samples, 2 x 3 inch in size illustrating range of colors and textures available for each surface finishing product scheduled.



D.
Samples:
Submit two samples, 2 x 3 inch in size illustrating selected colors and textures for each color selected.



E.
Manufacturer's Instructions:
Indicate special surface preparation procedures, substrate conditions requiring special attention.


.6

seq level2 \h \r0 

QUALIFICATIONS



A.
Manufacturer:  Company specializing in manufacturing the Products specified in this section with minimum three years documented experience.



B.
Applicator:  Company specializing in performing the work of this section with minimum 3 years-documented experience.


.7

seq level2 \h \r0 
 
REGULATORY REQUIREMENTS



A.
Conform to applicable code for flame and smoke rating requirements for finishes.


.8

seq level2 \h \r0 

FIELD SAMPLES



A.
Accepted sample may not remain as part of the Work.


.9

seq level2 \h \r0 

DELIVERY, STORAGE, AND HANDLING





A.
Deliver products to site in sealed and labeled containers; inspect to verify acceptability.



A.
Container label to include manufacturer's name, type of paint, brand name, lot number, brand code, coverage, surface preparation, drying time, cleanup requirements, color designation, and instructions for mixing and reducing.



B.
Store paint materials at minimum ambient temperature of 45 degrees F (7 degrees C) and a maximum of 90 degrees F (32 degrees C), in ventilated area, and as required by manufacturer's instructions.


.10

seq level2 \h \r0 
ENVIRONMENTAL REQUIREMENTS



A.
Do not apply materials when surface and ambient temperatures are outside the temperature ranges required by the paint product manufacturer.



B.
Do not apply exterior coatings during rain or snow, or when relative humidity is outside the humidity ranges required by the paint product manufacturer.



C.
Minimum Application Temperatures for Latex Paints:  45 degrees F for interiors; 50 degrees F for exterior; unless required otherwise by manufacturer's instructions.



D.
Minimum Application Temperature for Varnish Finishes:  65 degrees F (18 degrees C) for interior or exterior, unless required otherwise by manufacturer's instructions.



E.
Provide lighting level of 80-ft candles measured mid‑height at substrate surface.


.11

seq level2 \h \r0 
EXTRA MATERIALS






Not Used

2

seq level1 \h \r0 

seq level2 \h \r0  PART 2 PRODUCTS


.1

MANUFACTURERS



A.
Manufacturers ‑ Paint




1.
[ Sherwin Williams] 




2
.
[ Devo            ] 




3.
[ Benjamin Moore  ] 


.2

seq level2 \h \r0 

MATERIALS



A.
Coatings:  Ready mixed, except field-catalyzed coatings. Process pigments to a soft paste consistency, capable of being readily and uniformly dispersed to a homogeneous coating; good flow and brushing properties; capable of drying or curing free of streaks or sags.



B.
Accessory Materials:
Linseed oil, shellac, turpentine, paint thinners and other materials not specifically indicated but required to achieve the finishes specified, of commercial quality.



C.
Patching Materials:  Latex filler.



D.
Fastener Head Cover Materials:
Latex filler.


.3

seq level2 \h \r0 

FINISHES



A.
Refer to schedule at end of section for surface finish and color schedule.

3

seq level1 \h \r0 

seq level2 \h \r0  PART 3 EXECUTION


.1

EXAMINATION



A.
Verify site conditions under provisions of Section 01039.



B.
Verify that surfaces are ready to receive work as instructed by the product manufacturer.



C.
Examine surfaces scheduled to be finished prior to commencement of work.  Report any condition that may potentially affect proper application.



D.
Test shop applied primer for compatibility with subsequent cover materials.



E.
Measure moisture content of surfaces using an electronic moisture meter.  Do not apply finishes unless moisture content of surfaces are below the following maximums:




4.
Plaster and Gypsum Wallboard:  12 percent.




5.
Masonry, Concrete, and Concrete Unit Masonry:  [12] percent.




6.
Interior Wood:  15 percent, measured in accordance with ASTM D2016.




7.
Exterior Wood:  15 percent, measured in accordance with ASTM D2016.




8.
Concrete Floors:  8 percent.


.2

seq level2 \h \r0 

seq level3 \h \r0 

 PREPARATION



A.
Remove or mask electrical plates, hardware, light fixture trim, escutcheons, and fittings prior to preparing surfaces or finishing.



B.
Correct defects and clean surfaces which affect work of this section.  Remove existing coatings that exhibit loose surface defects.



C.
Seal with shellac and seal marks which may bleed through surface finishes.



D.
Impervious Surfaces:
Remove mildew by scrubbing with solution of tri‑sodium phosphate and bleach.  Rinse with clean water and allow surface to dry.



E.
Aluminum Surfaces Scheduled for Paint Finish:  Remove surface contamination by steam or high pressure water.    Remove oxidation with acid etch and solvent washing.  Apply etching primer immediately following cleaning.



F.
Asphalt, Creosote, or Bituminous Surfaces Scheduled for Paint Finish:  Remove foreign particles to permit adhesion of finishing materials.  Apply compatible sealer or primer.



G.
Insulated Coverings:
Remove dirt, grease, and oil from canvas and cotton.



H.
Concrete Floors:
Remove contamination, acid etch, and rinse floors with clear water.  Verify required acid‑ 

       alkali balance is achieved.  Allow to dry.



I.
Gypsum Board Surfaces:  Fill minor defects with filler compound.  Spot prime defects after repair.



J.
Galvanized Surfaces:
Remove surface contamination and oils and wash with solvent.  Apply coat of etching primer.



K.
Concrete and Unit Masonry Surfaces Scheduled to Receive Paint Finish:  Remove dirt, loose mortar, scale, salt or alkali powder, and other foreign matter.  Remove oil and grease with a solution of tri‑sodium phosphate; rinse well and allow to dry.  Remove stains caused by weathering of corroding metals with a solution of sodium metasilicate after thoroughly wetting with water.  Allow to dry.



L.
Plaster Surfaces:  Fill hairline cracks, small holes, and imperfections with latex patching plaster.  Make smooth and flush with adjacent surfaces.  Wash and neutralize high alkali surfaces.



M.
Uncoated Steel and Iron Surfaces:  Remove grease, mill scale, weld splatter, dirt, and rust.  Where heavy coatings of scale are evident, remove by power tool wire brushing or sandblasting; clean by washing with solvent.  Apply a treatment of phosphoric acid solution, ensuring weld joints, bolts, and nuts are similarly cleaned.  Spot prime paint after repairs.



N.
Shop Primed Steel Surfaces:  Sand and scrape to remove   loose primer and rust. Feather edges to make touch‑up patches inconspicuous. Clean surfaces with solvent.  Prime bare steel surfaces. Prime metal items including shop primed items.



O.
Interior Wood Items Scheduled to Receive Paint Finish:  Wipe off dust and grit prior to priming.  Seal knots, pitch streaks, and sappy sections with sealer.  Fill nail holes and cracks after primer has dried; sand between coats.


P.
Exterior Wood Scheduled to Receive Paint Finish:
Remove dust, grit, and foreign matter.  Seal knots, pitch streaks, and sappy sections.  Fill nail holes with tinted exterior caulking compound after prime coat has been applied.



Q.
Exterior Wood Scheduled to Receive Transparent Finish:  Remove dust, grit, and foreign matter; seal knots, pitch streaks, and sappy sections with sealer.  Fill nail holes with tinted exterior caulking compound after sealer has been applied.



R.
Wood and Metal Doors Scheduled for Painting: Seal top and bottom edges with primer.


.3

seq level2 \h \r0 

APPLICATION



A.
Apply products in accordance with manufacturer's instructions.



B.
Do not apply finishes to surfaces that are not dry.



C.
Apply each coat to uniform finish.



D.
Apply each coat of paint slightly darker than preceding coat unless otherwise approved.



E.
Sand wood and metal lightly between coats to achieve required finish.



F.
Vacuum clean surfaces free of loose particles.  Use tack cloth just prior to applying next coat.



G.
Allow applied coat to dry before next coat is applied.



H.
Where clear finishes are required, tint fillers to match wood.  Work fillers into the grain before set.  Wipe excess from surface.



I.
Prime concealed surfaces of interior and exterior woodwork with primer paint.



J.
Prime concealed surfaces of interior woodwork scheduled to receive stain or varnish finish with gloss varnish reduced 25 percent with mineral spirits.


.4

seq level2 \h \r0 

FINISHING MECHANICAL AND ELECTRICAL EQUIPMENT



A.
Refer to Section 15190 and Section 16195 for color coding and identification banding of equipment, duct work, piping, and conduit.



B.
Paint shop primed equipment.
Paint shop pre-finished items occurring at [interior areas.



C.
Remove unfinished louvers, grilles, covers, and access panels on mechanical and electrical components and paint separately.



D.
Prime and paint insulated and exposed pipes, conduit, boxes, insulated and exposed ducts, hangers, brackets, collars and supports, and except where items are pre-finished.



E.
Paint interior surfaces of air ducts that are visible through grilles and louvers with one coat of flat black paint, to visible surfaces.  Paint dampers exposed behind louvers, grilles, [and convector and baseboard cabinets] to match face panels.



F.
Paint exposed conduit and electrical equipment occurring in finished areas.



G.
Paint both sides and edges of plywood backboards for electrical and telephone equipment before installing equipment.



H.
Color code equipment, piping, conduit, and exposed duct work in accordance with requirements indicated. Color band and identify with flow arrows.



I.
Reinstall electrical cover plates, hardware, light fixture trim, escutcheons, and fittings removed prior to finishing.


.5
seq level2 \h \r0 
FIELD QUALITY CONTROL



A.
Field inspection and testing will be performed under provisions of Section 01400.



B.
Test questionable coated areas.


.6

seq level2 \h \r0 

CLEANING



A.
Clean work thoroughly.



B.
Collect waste material, which may constitute a fire hazard, place in closed metal containers and remove daily from site.


.7

seq level2 \h \r0 

SCHEDULE ‑ SHOP PRIMED ITEMS FOR SITE FINISHING



A.
Metal Fabrications.



B.
Metal Stairs all existing and renovated exterior stairs.


.8

seq level2 \h \r0 

SCHEDULE ‑ EXTERIOR SURFACES



A.
Wood ‑ Painted:




1.
One coat of alkyd primer sealer.




2.  Two coats of alkyd  enamel, semi‑gloss.seq level3 \h \r0 


B.seq level3 \h \r0 
Pavement Markings & Stripping:




1.  Two coats of Marking paint, white.


.9

seq level2 \h \r0 

seq level3 \h \r0 

SCHEDULE ‑ INTERIOR SURFACES



A.
Wood ‑ Painted:




1
.
One coat of Sherman Williams or Benjamin prime sealer.




2
.
Two coats of alkyd enamel, gloss.    


.10

seq level2 \h \r0 

seq level3 \h \r0 
SCHEDULE ‑ COLORS



A.
Match existing colors for all new surfaces and with touch up.

B. Match existing colors on walls, where existing piping or 

Or heaters have been removed.  Assure that patching or existing plaster, etc. has been accomplished prior to painting.

END OF SECTION
PAGE  
Section 09900 Page 2 of 7

