STANDARD
6 May 1999
04092
UPDATES  -



SECTION  04092


EMBEDDED FLASHING
PART 1 GENERAL
 1.1
SUMMARY
A.
Products Supplied But Not Installed Under This Section

1.
Flexible flashing for bottom of brick veneer

2.
Flexible flashing for brick sills

Paragraph ‘3' applies only on the Heritage 98 TRADITIONAL Style Option.

3.
Copper flashing at pilaster columns 

B.
Related Sections

1.
Sections under 04800 heading  -  Installation
04813 04814
 1.2
REFERENCES
Delete or add references based on editing of other parts of this Section.

A.
American Society For Testing And Materials
ASTM
1.
ASTM B 101-96, 'Standard Specification for Lead-Coated Copper Sheet and Strips for Building Construction'

PART 2 PRODUCTS
 2.1
MATERIALS
A.
Flexible Flashing

1.
Five ounces copper per sq ft of material with two layers of kraft paper.

2.
Acceptable Products And Manufacturers  -
Approved Products
a.
Cop-R-Kraft Duplex by Advanced Building Products Inc, Springvale, ME  (800) 252-2306  www.advancedbldgproducts.com
b.
Cop-A-Bond Duplex by AFCO Products Inc, Sommerville, MA  (800) 397-2687  

c.
Cop-R-Tex Duplex by York Manufacturing Inc, Sanford, ME  (800) 551‑2828  www.yorkflashings.com
d.
Copper Kraft Duplex by Sandell Manufacturing Co, Schenectady, NY  (800) 283-3888 www.sandellmfg.com
e.
Equal as approved by Architect prior to installation.  See Section 01600.

The flashing specified in Paragraph ‘B’ is used at the base of the fiberglass half-columns installed at the front of the building on the Heritage 98 TRADITIONAL Style Option.

B.
Lead-Coated Copper Flashing  -  Meet requirements of ASTM B 101, Grade I or II, weighing 17 oz per sq ft minimum.

PART 3 EXECUTION  -  Not Used
Installation

END OF SECTION

20020
1
Section 04092

MeetingHouse
May 22, 2000
Embedded Flashing


