SUPPLEMENTARY
7 Mar 2000
07133sup
UPDATES  -

This Section may be necessary when there are severe below grade water problems if neither the standard Section 07111 nor Section 07140 will handle the problem.



SECTION  07133


MODIFIED BITUMINOUS SHEET WATERPROOFING
PART 1 GENERAL
 1.1
SUMMARY
A.
Includes But Not Limited To

1.
Furnish and install membrane waterproofing as described in Contract Documents.

 1.2
QUALITY ASSURANCE
A.
Pre-Installation Conference  -  Schedule pre-installation conference prior to application of system.
Pre-installation
 1.3
DELIVERY, STORAGE, AND HANDLING
Delivery
A.
Storage provisions, safety precautions, and protection from incompatible materials shall comply with Manufacturer's directions.

 1.4
PROJECT CONDITIONS
A.
Project Environmental Requirements  -  Ambient temperature shall be 25 deg F and rising at time of application.

 1.5
WARRANTY
Warranty
A.
Manufacturer's 5 year material and 2 year labor warranty on total system.

PART 2 PRODUCTS
 2.1
COMPONENTS
A.
Membrane

1.
For Application At Temperatures Above 40 deg F  -

a.
Bituthene 3000 by Grace

b.
Elasto-Ply 60 Mil Membrane by Karnak

c.
Miradri 860 by Miradri

d.
Sealtight Mel-Rol by W R Meadows

2.
For Application At Temperatures Between 25 and 40 deg F  -

a.
Bituthene 3100 by Grace

b.
Elasto-Ply 60 Mil Membrane by Karnak

c.
Miradri 861 by Miradri

d.
Sealtight Mel-Rol by W R Meadows

B.
Primers

1.
For Application At Temperatures Above 40 deg F  -

a.
P‑3000 by Grace

b.
No 2000 primer by Karnak

c.
P-804 by Miradri

d.
Sealtight Mel-Prime by W R Meadows

2.
For Application At Temperatures Between 25 and 40 deg F  -

a.
P‑3100 by Grace

b.
No 3000 primer by Karnak

c.
P-805 by Miradri

d.
Sealtight Mel-Prime by W R Meadows

C.
Elastomeric Mastic

1.
EM-3000 by Grace

2.
No 81 Rubberized Mastic by Karnak

3.
M-800 by Miradri

4.
Sealtioght Pointing Mastic by W R Meadows

D.
Liquid Membrane

1.
LM‑3000 by Grace

2.
W-1 One-Kote by Karnak

3.
LM-800 by Miradri

4.
Sealtight Liquid Membrane by W R Meadows

E.
Protection Board (1/8 inch backer board)

1.
PB-3000 by Grace

2.
As recommended by Karnak

3.
As recommended by Miradri

4.
PC-1 Protection Course by W R Meadows

F.
Protection Board Adhesive

1.
PBA-3000 by Grace

2.
As recommended by Karnak

3.
As recommended by Miradri

4.
Sealtight Pointing Mastic by W R Meadows

 2.2
APPROVED MANUFACTURERS
Approved Products
A.
Grace Construction Products, Cambridge, MA  (800) 521-2737  www.gcp-grace.com
B.
Karnak Corporation, Clark, NJ  (800) 526-4236  www.karnakcorp.com
C.
Miradri Inc, Duluth, GA  (888) 464-7234  www.miradri.com  

D.
W R Meadows, Elgin, IL  (800 342-5976  www.wrmeadows.com
PART 3 EXECUTION
 3.1
EXAMINATION
A.
Concrete surfaces shall be dry, smooth, and monolithic with no voids, spalled areas, loose aggregate, sharp protrusions, or finishes other than smooth troweled.

 3.2
INSTALLATION
Installation
A.
Do not apply until 7 days minimum after form removal.

B.
Apply primer with lambswool roller at the rate of 250 to 350 sq ft per gal.  Allow to dry until tack free, one hour minimum.  Do not prime area larger than can be covered in one working day.  Re-prime areas left overnight.

C.
Apply membrane vertically in 8 foot maximum strips with vertical and horizontal joints lapping 2‑1/2 inches minimum.  Press membrane on vertical surfaces with heavy hand pressure during application.  Press top edges with metal or wood hammer or knife handle.

D.
Seal daily and permanent terminations with thin troweled bead of specified mastic on vertical surfaces.  Do not permanently expose to sunlight.

E.
Apply specified protection board adhesive and protection board.

 3.3
FIELD QUALITY CONTROL
A.
Manufacturer's Field Service

1.
Manufacturer's Technical Representative shall inspect installed systems prior to backfilling.

2.
Notify Architect two working days prior to backfilling.


END OF SECTION

ADVANCE \d252
B L A N K   P A G E

20020
1
Section 07133

MeetingHouse
May 22, 2000
Modified Bituminous Sheet Waterproofing

