
STANDARD
19 Nov 1999
07631

UPDATES  -

19 Nov
-
Added Metal Sales Mfg Corp.

3 Mar 99
-
Moved drip edges from 07634 to this Section.  Deleted requirement for valley flashing.  Changed metal to kynar coated aluminum or steel.

This Section is intended for use with asphalt shingles specified in Section 07312.  Flashing for metal shingles specified in Section 07313 is included with the shingle system, and flashing for concrete roof tile is specified in Section 07634opt.



SECTION  07631


ROOF FLASHING
PART 1 GENERAL
Edit Article ‘1.1' as necessary to give an accurate, but brief description of the work of this Section and accurate listing of related work, especially if the scope of the work is not shown graphically on the Drawings.

 1.1
SUMMARY
A.
Products Supplied But Not Installed Under This Section

1. Gravel stops, roof edge strips, and scuppers not specified to be of other materials.  

B.
Related Sections

1.
Section 07621  -  Installation
07312


 1.2
REFERENCES
Delete or add references based on editing of other parts of this Section.

A.
American Society For Testing And Materials
ASTM
1.
ASTM A 361-94, 'Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) by the Hot-Dip Process for Roofing and Siding'

 PART 2 PRODUCTS
 2.1 MATERIALS
A. Sheet metal flashing

1. 24 ga galvanized steel.  Meet requirements of ASTM a 361, for 1.25 oz. commercial.  

2. Copings 

a. 22 ga galvanized steel 

3. Finish 

a. Metal exposed to view shall have face coating of polyvinyledene Fluoride (PVF2) resin-base finish (Kynar 500 or Hylar 5000) containing 70 percent minimum PVF2 in resin portion of formula.  Thermo-cured two coat system consisting of corrosion inhibiting epoxy or acrylic latex primer and top coat factory applied over properly pre-treated metal.  Reverse side coating shall be thermo-cured system consisting of corrosion inhibiting epoxy or acrylic latex primer applied over properly pre-treated metal.  

b. Color as selected by Architect from manufacturer’s standard colors.  

B. Sealants – rubber base type conforming to Fed Spec TC-S-00230.  

C. Nails and other fasteners – Hot-dipped galvanized of strength and type consistent with function.  

 2.2
FABRICATION
A.
Form accurately to details

B.
Profiles, bends, and intersections shall be even and true to line.

PART 3 EXECUTION – Not Used 

END OF SECTION

557-1804 (20020)
1
Section 07631

Orlando Welfare Complex
October 11, 2000
Roof Flashing

