STANDARD
3 Nov 1998
07920
UPDATES  -



SECTION  07920


JOINT SEALANTS
PART 1 GENERAL
 1.1
SUMMARY
A.
Includes But Not Limited To

1.
Quality of sealants to be used on Project not specified elsewhere, including submittal, material, and installation requirements.

B.
Related Sections

Delete paragraph ‘1' if no existing sealants are to be removed.  Specify removal of existing sealants in Section responsible for installing new sealants.

1.
Furnishing and installing of sealants is specified in Sections specifying work to receive new sealants.

Edit paragraph ‘3' to show the exact EIFS specification Section to be used.

 1.2
SUBMITTALS
A.
Product Data
Product Data
1.
Manufacturer's literature and installation recommendations for each Product.

2.
Schedule showing joints requiring sealants.  Show also backing and primer to be used.

B.
Quality Assurance / Control  -  Certificate from Manufacturer indicating date of manufacture.
Quality
 1.3
DELIVERY, STORAGE, AND HANDLING
Delivery
A.
Handle to prevent inclusion of foreign matter, damage by water, or breakage.

B.
Deliver and keep in original containers until ready for use.

C.
Do not use damaged or deteriorated materials.

D.
Store in a cool place, but never under 40 deg F.

PART 2 PRODUCTS
 2.1
MATERIALS
A.
Sealants

1.
Sealants provided shall meet Manufacturer's shelf-life requirements.

Edit paragraph ‘2' to fit locations to receive sealant.

2.
Exterior Building Elements  -

a.
Joints and cracks around windows

b.
Aluminum entrance perimeters and thresholds

c.
Door frames

d.
Columns

e.
Louvers

f.
Wall penetrations

g.
Connections

h.
Parapet caps

i.
Other joints necessary to seal off building from outside air and moisture

j.
Approved Products  -
Approved Products
1)
Dow Corning  -

a)
Primer  -  1200

b)
Sealant  -  791

2)
General Electric  -

a)
Primer  -  SCP 3154

b)
Sealant  -  Silpruf

3.
Exterior Sheet Metal And Miscellaneous  -

a.
Penetrations in soffits and fascias

b.
Roof vents and flues

c.
Flashings

d.
Approved Products  -
Approved Products
1)
791 or 790 by Dow Corning

2)
Sikaflex 15LM by Sika Corp

Delete paragraph ‘4' if no concrete retaining walls or Portland cement concrete parking areas.  Sealants are not required in expansion joints of sidewalks and curbs except as noted.

4.
Exterior Concrete  -

a.
Approved Products  -
Approved Products
1)
Joints between sidewalks and building foundations  -

a)
Dow Corning  -

(1)
Primer  -  1200

(2)
Sealant  -  790

b)
General Electric  -

(1)
Primer  -  SCP 3154

(2)
Sealant  -  Silpruf

2)
Expansion joints in retaining walls  -

a)
Dow Corning  -

(1)
Primer  -  1200

(2)
Sealant  -  790

b)
General Electric  -

(1)
Primer  -  SCP 3154

(2)
Sealant  -  Silpruf

3)
Expansion joints in Portland cement concrete parking lots  -

a)
Dow Corning  -

(1)
Primer  -  1200

(2)
Sealant  -  NS.  SL may be used on non-sloping areas.

5.
Interior  -

a.
Inside jambs and heads of exterior door frames

b.
Inside perimeters of windows

c.
Approved Manufacturers And Products  -
Approved Products
1)
Trademate Paintable by Dow Corning

2)
Acrylic Latex 834 by Tremco

6.
Interior At Exposed Masonry Walls  -

a.
Both sides of interior door frames

b.
Approved Manufacturers And Products  -
Approved Products
1)
Trademate Paintable by Dow Corning

2)
Acrylic Latex 834 by Tremco

7.
Interior Joints Formed By  -

a.
Countertops and backsplash to wall

b. Sinks and lavatories to countertops

c.
Approved Manufacturers And Products  -
Approved Products
1)
Dow Corning Trademate Tile & Ceramic Sealant


2)
General Electric Sanitary 1700

Edit or delete paragraph ‘c’ to correspond with Project requirements.

8.
Color  -  As selected by Architect from Manufacturer's standard colors.

B.
Backing  -  Flexible closed cell polyurethane or polyolefin rod or bond breaker tape as recommended by Sealant Manufacturer for joints being sealed.

 2.2
MANUFACTURERS
Approved Products
A.
Dow Corning Corp, Midland, MI  (800) 248-2481  www.dowcorning.com
B.
G E Silicone Products, Waterford, NY  (800) 255-8886 www.ge.com/silicones/sealants
C.
Sika Corporation, Lyndhurst, NJ  (201) 933-9379  www.sika.com
D.
Tremco, Beachwood, OH  (800) 321-7906  www.tremcosealants.com
PART 3 EXECUTION
 3.1
PREPARATION
Delete first sentence of Paragraph ‘A’ if no existing sealants are to be removed. 

A.
Surfaces shall be clean, dry, and free of dust, oil, grease, dew, or frost.

B.
Apply primer.

C.
Joint Backing

1.
Rod for open joints shall be at least 1-1/2 times width of open joint and of thickness to give solid backing.  Backing shall fill up joint so depth of sealant bite is no more than 3/8 inch deep.

2.
Apply bond-breaker tape in shallow joints as recommended by Sealant Manufacturer.

 3.2
APPLICATION
Installation
A.
Apply sealant with hand-calking gun with nozzle of proper size to fit joints.  Use sufficient pressure to insure full contact to both sides of joint to full depth of joint.

B.
Tool joints immediately after application of sealant if required to achieve full bedding to substrate or to achieve smooth sealant surface.

C.
Depth of sealant bite shall be 1/4 inch minimum and 1/2 inch maximum, but never more than one half or less than one fourth joint width.

D.
Do not apply calking at temperatures below 40 deg F.

E.
Calk opening perimeters unless indicated otherwise.

 3.3
CLEANING
A.
Clean adjacent materials which have been soiled immediately (before setting) as recommended by Manufacturer.


END OF SECTION

557-1804 (20020)
1
Section 07920

Orlando Welfare Complex 
October 11, 2000
Joint Sealants


