STANDARD
3 Aug 1999
09925

UPDATES  -

3 Aug 99
-
Added PPG Porter

11 Jan 99
-
Updated Benjamin Moore products.



SECTION  09925


INTERIOR PAINTED WOOD
PART 1 GENERAL
Edit Article ‘1.1' as necessary to give an accurate, but brief description of the work of this Section and accurate listing of related work, especially if the scope of the work is not shown graphically on the Drawings.

 1.1
SUMMARY
A.
Includes But Not Limited To

1.
Preparing and painting new woodwork and wood floors not requiring transparent finish, as described in Contract Documents.

On addition / remodel Projects requiring painting of existing surfaces, list or describe the existing wood surfaces to receive an opaque finish under this Section, show them graphically of the Drawings, or include them in a schedule on the Drawings.  If one of the latter two options is used, delete paragraph ‘2' and the  word ‘new’ from paragraph ‘1' above.

2.
Preparing and painting following existing woodwork surfaces not requiring transparent finish, as described in Contract Documents  -

a.


b.


c.


d.


B.
Related Sections

1.
Section 09901  -  General Painting Requirements
09901
PART 2 PRODUCTS
Delete all the sets of paint systems but one under each substrate to be painted.  Then edit the list of approved manufacturers and their systems to include only those with whom you are familiar and whose products are available in the Project area.  DO NOT ADD OR APPROVE ANY OTHER MANUFACTURERS OR SYSTEMS.

 2.1
MATERIALS
A.
Woodwork

OPTION 1  -  Include this set of paint systems if Project is located in an area where VOC compliant paints ARE required.

1.
Primer Coat  -

a.
New Surfaces  -

1)
Benjamin Moore  -  023 Fresh Start

2)
ICI Paints  -

a)
ICI Dulux  -  1020-XXXX Ultra-Hide Latex Interior Wood Undercoater

b)
ICI Devoe  -  DR51701 Wonder-Prime Primer-Sealer Interior Acrylic

c)
ICI Fuller O’Brien  -  FOB220-02 Interior Latex Enamel Undercoater

3)
PPG Paints  -

a)
PPG Pittsburgh Paints  -  Speedhide 6-855 Enamel Undercoat

b)
PPG Porter  -  1129 Blankit Interior Acrylic Primer / Sealer

4)
Pratt & Lambert  -  Suprime 11

5)
Sherwin-Williams  -  Wall & Wood Primer, B49 WZ1

If existing painted surface is sound, a primer coat may not be necessary.

b.
Existing Painted Surfaces  -

1)
Benjamin Moore  -  023 Fresh Start

2)
ICI Paints  -

a)
ICI Dulux  -  1020-XXXX Ultra-Hide Latex Interior Wood Undercoater

b)
ICI Devoe  -  DR51701 Wonder-Prime Primer-Sealer Interior Acrylic

c)
ICI Fuller O’Brien  -  FOB220-02 Interior Latex Enamel Undercoater

3)
PPG Paints  -

a)
PPG Pittsburgh Paints  -  17-21 Seal Grip Stain Blocking Primer

b)
PPG Porter  -  1129 Blankt interior Acrylic Primer / Sealer

4)
Pratt & Lambert  -  Suprime 11

5)
Sherwin-Williams  -  Wall & Wood Primer, B49 WZ1

2.
Finish Coats  -

a.
Benjamin Moore  -  Two Coats M28 Acrylic Gloss Enamel

b.
ICI Paints  -

1)
ICI Dulux  -  Two Coats 4208-XXXX Devflex Interior / Exterior Acrylic Semigloss Enamel

2)
ICI Devoe  -  DP84XX Mirrolac-WB Interior / Exterior High Gloss Enamel

3)
ICI Fuller O’Brien  -  

c.
PPG Paints  -

1)
PPG Pittsburgh Paints  -  Two Coats 51-Line Brilliant Reflections High Gloss Acrylic

2)
PPG Porter  -  Two Coats 909 Advantage 900 Gloss Interior / Exterior Acrylic Enamel

d.
Pratt & Lambert  -  Two Coats Enducryl

e.
Sherwin-Williams  -  Two Coats DTM Acrylic Gloss Coating, B66 Series

OPTION 2  -  Include this set of paint systems if Project is located in an area where VOC compliant paints ARE NOT required.

1.
Primer Coat  -

a.
New Surfaces -

1)
Benjamin Moore  -  Moore's Alkyd Enamel Underbody 217

2)
ICI Paints  -

a)
ICI Dulux  -  1120-XXXX Ultra-Hide Oil / Alkyd Interior Wood Undercoater

b)
ICI Devoe  -  DR8801 Velour Interior Alkyd Enamel Undercoater

c)
ICI Fuller O’Brien  -  FOB220-07 Interior Alkyd Enamel Undercoater

3)
Pittsburgh Paints  -  Speedhide Enamel Undercoater 6-6

4)
Pratt & Lambert  -  Suprime 11

5)
Sherwin-Williams  -  Wall & Wood Primer, B49 W1

If existing painted surface is sound, a primer coat may not be necessary.

b.
Existing Painted Surfaces  -

1)
Benjamin Moore  -  Moore's Alkyd Enamel Underbody 217

2)
ICI Paints  -

a)
ICI Dulux  -  1120-XXXX Ultra-Hide Oil / Alkyd Interior Wood Undercoater

b)
ICI Devoe  -  DR8801 Velour Interior Alkyd Enamel Undercoater

c)
ICI Fuller O’Brien  -  FOB220-07 Interior Alkyd Enamel Undercoater

3)
PPG Paints  -

a)
PPG Pittsburgh Paints  -  17-21 Seal-Grip Stain Blocking Primer

b)
PPG Porter  -  135 Glyptex Interior Alkyd Enamel

4)
Pratt & Lambert  -  Suprime 11

5)
Sherwin-Williams  -  Wall & Wood Primer, B49 W1

2.
Finish Coats  -

a.
Benjamin Moore  -  Two Coats M22 Urethane Alkyd Enamel

b.
ICI Paints  -

1)
ICI Dulux  -  Two Coats 4308-XXXX Devguard Gloss Alkyd Industrial Enamel

2)
ICI Devoe  -

3)
ICI Fuller O’Brien  -

c.
PPG Paints  -

1)
PPG Pittsburgh Paints  -  Two 51-Line Brilliant Reflections Hi Gloss Latex

2)
PPG Porter  -  Two Coats 4139 Glyptex Urethane Gloss Enamel

d.
Pratt & Lambert  -  Two Coats Effecto Enamel

e.
Sherwin-Williams  -  Two Coats Industrial Enamel

B.
Wood Floors

OPTION 1  -  Include this set of paint systems if Project is located in an area VOC compliant paints ARE required.

1.
ICI Paints  -

a.
ICI Dulux  -  Two Coats 3018-XXXX Ultra-Hide Acrylic Latex Interior / Exterior Floor Enamel

b.
ICI Devoe  -  Two Coats DR78XX Porch & Floor Satin Interior / Exterior Acrylic Latex Enamel

c.
ICI Fuller O’Brien  -  Two Coats FOB631-XX Latex Floor Enamel Satin

2.
PPG Paints  -

a.
PPG Pittsburgh Paints  -  Two Coats 98-Line Aquapon WB, Waterborne Epoxy

b.
PPG Porter  -  Two Coats 1069 Acrylic Floor Enamel

3.
Sherwin-Williams  -  Two Coats ArmaSeal Treadplex B90 Series

4.
Sonneborn  -  Two Coats Oncrete II

OPTION 2  -  Include this set paint systems if Project is located in an area where VOC compliant paints ARE NOT required.

1.
Benjamin Moore  -  Two Coats IronClad Chex-Wear Epoxy-Ester Enamel

2.
ICI Paints -

a.
ICI Dulux  -

1)
First Coat  -  3118-XXXX Ultra-Hide Urethane Interior / Exterior Floor Enamel (thinned 15 percent)

2)
Second Coat  -  3118-XXXX Ultra-Hide Urethane Interior / Exterior Floor Enamel

b.
ICI Devoe  -

1)
First Coat  -  DR77XX Porch & Floor Gloss Interior / Exterior Alkyd-Urethane Enamel (thinned 15 percent)

2)
Second Coat  -  DR77XX Porch & Floor Gloss Interior / Exterior Alkyd-Urethane Enamel

c.
ICI Fuller O’Brien  -

1)
First Coat  -  FOB630-XX Floor & Deck Alkyd Gloss Enamel (Thinned 15 percent)

2)
Second Coat  -  FOB630-XX Floor & Deck Alkyd Gloss Enamel

3.
PPG Paints  -

a.
PPG Pittsburgh Paints  -  Two Coats 97-Line Aquapon Polyamide Epoxy

b.
PPG Porter  -

1)
First Coat  -  69 Glyptex Floor & Porch Enamel thinned with one pint Manufacturer’s recommended material per gallon

2)
Second Coat  -  69 Glyptex Floor & Porch Enamel

4.
Sherwin-Williams  -  Two Coats ArmaSeal Treadplex B90 Series

5.
Sonneborn  -  Two Coats Oncrete II

Edit the list of approved manufacturers to include only those with whom you are familiar and whose products are available in the Project area.  Edit the product listing in each paint Section to correspond with this list as edited for this Project.  DO NOT ADD OR APPROVE ANY OTHER MANUFACTURERS OR SYSTEMS.  NO OTHER MANUFACTURERS OR PRODUCTS ARE ACCEPTABLE FOR THIS PAINT.

 2.2
APPROVED MANUFACTURERS
Approved Products
A.
Benjamin Moore, Montvale, NJ  (888) 236-6667  www.benjaminmoore.com
B.
ICI Paints

1.
ICI Dulux Paints, Cleveland, OH  (800) 984-5444  www.icidulux.com
2.
ICI Devoe,  www.devoepaint.com
3.
ICI Fuller O’Brien,  www.fullerpaint.com
C.
PPG Paints

1.
PPG Pittsburgh Paints, Pittsburgh, PA  (800) 441-9695 www.ppgaf.com
2.
PPG Porter, Louisville, KY  (800) 322-6370  www.porterpaints.com
D.
Pratt & Lambert, Cleveland, OH  (800) 289-7728  

E.
Sherwin-Williams, Cleveland, OH  (800) 321-8194  www.sherwin-williams.com
F.
Sonneborn, Shakopee, MN  (800) 496-6067  www.chemrex.com
PART 3 EXECUTION
 3.1
APPLICATION
Installation
A.
General  -  See appropriate paragraphs of Section 09901.
09901
B.
Interface With Other Work

1.
Properly clean and paint light cove interiors before installation of light fixtures.

2.
Where back-priming is required, apply one coat of first coat material.

C.
New Surfaces

1.
Spot prime nail holes, cracks, and blemishes before and after puttying.

2.
Apply stain blocker or other product recommended by Paint Manufacturer to knots before applying primer coat.

After examination of the existing surfaces to be repainted, specify the procedure to be followed in preparing those surfaces for repainting.  Some editing of the standard procedure may be required.

Delete Paragraph ‘D’ if no existing exterior wood is to be painted.

D.
Existing Painted Surfaces

1.
Remove deteriorated existing paint down to sound substrate by scraping and sanding.  Feather edges of existing paint by sanding to be smooth with adjacent surfaces.  Spot prime bare wood areas on woodwork.

2.
Wash surfaces that have been defaced with marking pens, crayons, lipstick, etc, with solvent recommended by Paint Manufacturer.  Spot prime such surfaces.

3.
Apply finish coats.


END OF SECTION

ADVANCE \d252
B L A N K   P A G E

20020
4
Section 09925

MeetingHouse
May 22, 2000
Interior Painted Wood

