Orleans Parish Administration Buildings
07551

3510 DeGaulle
APP-MODIFIED BITUMINOUS MEMBRANE ROOFING

New Orleans, LA
Page 4

SECTION 07551 - APP-MODIFIED BITUMINOUS MEMBRANE ROOFING

PART 1 - GENERAL

RELATED DOCUMENTS:
Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

SUMMARY:
This Section includes the following:


Two-ply, APP modified bituminous membrane roofing.

Related Sections include the following:


Division 6 Section “Miscellaneous Carpentry” for wood blocking, curbs, cants, and nailers; and wood-based, structural-use roof deck panels.


Division 7 Section “Sheet Metal Flashing and Trim” for metal roof penetration flashings, flashings, and counterflashings.

Unit Prices:  Refer to Division 1 Section “Unit Prices” for description of Work in this Section that is affected by unit prices.

DEFINITIONS:
Roofing Terminology:  Refer to ASTM D 1079 for definitions of terms related to roofing work not otherwise defined in this Section.

PERFORMANCE REQUIREMENTS:
General:  Install a watertight, modified bituminous membrane roofing and base flashing system with compatible components that will not permit the passage of liquid water and will withstand wind loads, thermally induced movement, and exposure to weather without failure.

FM Listing:  Provide modified bituminous membrane, base flashings, and component materials that meet requirements of FM 4450 and FM 4470 as part of a roofing system and that are listed in FM’s “Approval Guide” for Class 1 or noncombustible construction, as applicable.  Identify materials with FM markings.


Roofing system shall comply with the following:



Fire/Windstorm Classification:  Class 1A-240.

ISO Certification:   Manufacturer of roofing materials must be ISO 9001 Certified for the “Design and manufacture of modified bitumen roofing and water barrier systems.”  Manufacturer of roofing materials must provide a copy of their Certificate of Registration.

Roofing System Design:  Provide a roofing system that complies with roofing system manufacturer’s written design instructions and with the following:


SPRI’s “Wind Design Guide for Adhered Roofing Systems.”

SUBMITTALS:
Product Data:  For each type of roofing product specified.  Include data substantiating that materials comply with requirements.

Shop Drawings:  Include plans, sections, details, and attachments to other work, for the following:


Base flashings, cants, and membrane terminations.


Tapered insulation, including slopes.


Crickets, saddles, and tapered edge strips, including slopes.

Samples for Verification:  Of the following products:


12-by-12-inch (300-by-300-mm) square of modified bituminous, granule-surfaced cap sheets, of color specified.


12-by-12-inch (300-by-300-mm) square of roofing insulation.

Installer Certificates:  Signed by roofing system manufacturer certifying that Installer is approved, authorized, or licensed by manufacturer to install specified roofing system and is eligible to receive the standard roofing manufacturer’s warranty.

Manufacturer Certificates:  Signed by roofing system manufacturer certifying that the roofing system complies with requirements specified in the “Performance Requirements” Article.  Upon request, submit evidence of complying with requirements.

Qualification Data:  For firms and persons specified in the “Quality Assurance” Article to demonstrate their capabilities and experience.  Include lists of completed projects with project names and addresses, names and addresses of architects and owners, and other information specified.

Certificates of Analysis:  Based on evaluation of tests performed by manufacturer, indicate compliance of components of roofing system with requirements based on comprehensive testing of current product compositions.

Research/Evaluation Reports:  Evidence of roofing system’s compliance with building code in effect for Project from a model code organization acceptable to authorities having jurisdiction.

Maintenance Data:  For roofing system to include in the maintenance manuals specified in Division 1.

Warranty:  Sample copy of standard roofing manufacturer’s warranty stating obligations, remedies, limitations, and exclusions of warranty.

Inspection Report:  Copy of roofing system manufacturer’s inspection report of completed roof installation.

QUALITY ASSURANCE:
Installer Qualifications:  Engage an experienced installer to perform Work of this Section who has specialized in installing roofing similar to that required for this Project; who is approved, authorized, or licensed by the roofing system manufacturer to install manufacturer’s product; and who is eligible to receive the standard roofing manufacturer’s warranty.

Fire-Test-Response Characteristics:  Provide roofing materials with the fire-test-response characteristics indicated as determined by testing identical products per test method indicated below by UL, FM, or another testing and inspecting agency acceptable to authorities having jurisdiction.  Identify materials with appropriate markings of applicable testing and inspecting agency.


Exterior Fire-Test Exposure:  Class A; complying with ASTM E 108, for application and slopes indicated.

Preliminary Roofing Conference:  Before starting roof deck construction, conduct conference at Project site.  Meet with the same participants and review the same items listed for the preinstallation conference.  In addition, review status of submittals and coordination of work related to roof construction.  Notify participants at least 5 working days before conference.

Preinstallation Conference:  Before installing roofing system, conduct conference at Project site to comply with requirements of Division 1 Section “Project Meetings.”  Notify participants at least 5 working days before conference.


Meet with Owner; Architect; Owner’s insurer, if applicable; testing and inspecting agency representative; roofing Installer; roofing system manufacturer’s representative; deck Installer; and installers whose work interfaces with or affects roofing, including installers of roof accessories and roof-mounted equipment.


Review methods and procedures related to roofing installation, including manufacturer’s written instructions.


Examine deck substrate conditions and finishes for compliance with requirements, including flatness and attachment to structural members.


Review loading limitations of deck during and after roofing.


Review flashings, special roofing details, roof drainage, roof penetrations, equipment curbs, and condition of other construction that will affect roofing.


Review governing regulations and requirements for insurance, certifications, and inspection and testing, if applicable.


Review temporary protection requirements for roofing system during and after installation.


Review roof observation and repair procedures after roofing installation.


Document proceedings, including corrective measures or actions required, and furnish copy of record to each participant.

DELIVERY, STORAGE, AND HANDLING:
Store roofing materials in a dry, well-ventilated, weathertight location to ensure no significant moisture pickup and maintain at a temperature exceeding roofing system manufacturer’s written instructions.  Store rolls of felt and other sheet materials on end on pallets or other raised surfaces.  Do not double-stack rolls.


Handle and store roofing materials and place equipment in a manner to avoid significant or permanent damage to deck or structural supporting members.

Do not leave unused felts and other sheet materials on the roof overnight or when roofing work is not in progress unless protected from weather and moisture and unless maintained at a temperature exceeding 50 deg F (10 deg C).

Deliver and store liquid materials in their original undamaged containers in a clean, dry, protected location and within the temperature range required by roofing system manufacturer.

Protect roofing insulation materials from physical damage and from deterioration by sunlight, moisture, soiling, and other sources.  Store in a dry location.  Comply with insulation manufacturer’s written instructions for handling, storing, and protecting during installation.

PROJECT CONDITIONS:
Weather Limitations:  Proceed with roofing work only when existing and forecasted weather conditions permit roofing to be installed according to manufacturers’ written instructions and warranty requirements.

WARRANTY:
General Warranty:  The warranties specified in this Article shall not deprive the Owner of other rights the Owner may have under other provisions of the Contract Documents and shall be in addition to, and run concurrent with, other warranties made by the Contractor under requirements of the Contract Documents.

Standard Roofing Manufacturer’s Warranty:  Submit a written warranty, without monetary limitation, signed by roofing system manufacturer agreeing to promptly repair leaks in the roof membrane and base flashings resulting from defects in materials or workmanship for the following warranty period:


Warranty Period:  20 years

Special Project Warranty:  Submit roofing Installer’s warranty, on warranty form at end of this Section, signed by Installer, covering Work of this Section, including membrane roofing, base flashing, roofing insulation, fasteners, and vapor retarders, if any, for the following warranty period:


Warranty Period:  2 years from date of Substantial Completion.

PART 2 - PRODUCTS

MANUFACTURERS:
Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

Manufacturers:  Subject to compliance with requirements, provide products by one of the following:


APP-Modified Bituminous Sheet:



Performance Roof Systems, Inc.


Polyisocyanurate Board Insulation:



1.5” Insulation supplied by System Manufacturer to meet warranty requirements.

APP-MODIFIED BITUMINOUS SHEET:
APP-Modified Bituminous Sheet, Smooth Surfaced:  Atactic-polypropylene-modified asphalt sheet meeting ASTM D-6223-98, smooth surfaced; suitable for application method specified; manufacturer’s standard thickness and weight; for use and of reinforcing type as follows: 


Use:  Base flashing.  


Use:  Base ply of 2-ply, modified bituminous membrane roofing.


Reinforcing:  Composite fiberglass and polyester mat.


Product:  
Derbigum® GP as manufactured by Performance Roof Systems, Inc.

APP-Modified Bituminous Sheet, Mineral-Granule Surfaced:  Fire-Rated Atactic-polypropylene-modified asphalt sheet meeting ASTM D-6223-98, reinforced, with continuous layer of mineral granules factory applied to top exposed surface and a sanded surface on bottom surface; suitable for application method specified; manufacturer’s standard thickness and weight; for use and of reinforcing type and granule color as follows:


Use:  Finish ply of 2-ply, modified bituminous membrane roofing and base flashing.


Reinforcing:  Composite fiberglass and polyester mat.


Product:  
Derbicolor® GP-FR as manufactured by Performance Roof Systems, Inc.

Granule Color:  White.

Physical Properties:  Provide APP-modified bituminous membrane materials with the following properties when tested according to ASTM D 5147:


Thickness:    180 mils (4.5 mm) – Cap Membrane.



160 mils (4.0 mm) – Base Ply Membrane



Tensile Strength:  90 lbf/in. (15.75 kN/m) at 0 deg F (minus 18 deg C) in each direction.


Elongation at Maximum Load:  20 percent minimum at 0 deg F (minus 18 deg C) in each direction.


Tear Strength:  85 lbf (378 N) minimum.


Low-Temperature Flexibility:  Pass at minus 13 deg F (minus 25 deg C).

AUXILIARY MEMBRANE MATERIALS:
General:  Furnish auxiliary materials recommended by roofing system manufacturer for intended use and compatible with APP-modified bituminous roofing.


Furnish liquid-type auxiliary materials that meet VOC limits of authorities having jurisdiction.

Asphalt Primer:  ASTM D 41.

Cold-Applied Adhesive:  Roofing system manufacturer’s standard asphalt-based, 1-part, asbestos-free, cold-applied adhesive specially formulated for compatibility and use with modified bituminous membrane roofing and flashings.


Product:  
Permastic® as manufactured by Performance Roof Systems, Inc.

Asphalt Roofing Cement:  ASTM D 4586, asbestos free, of consistency required by roofing system manufacturer for application.

Mastic Sealant:  Polyisobutylene, plain or modified bituminous, nonhardening, nonmigrating, nonskinning, and nondrying.

Metal Flashing Sheet:  Metal flashing sheet is specified in Division 7 Section “Sheet Metal Flashing and Trim.”

Wood Nailer Strips:  Furnish wood nailer strips complying with requirements of Division 6 Section “Miscellaneous Carpentry.”

Cants:  Wood cants are specified in Division 6 Section “Miscellaneous Carpentry.”

Miscellaneous Accessories:  Provide miscellaneous accessories recommended by roofing system manufacturer for intended use.

INSULATION MATERIALS
General:  Provide preformed, roofing insulation boards that comply with requirements, selected from manufacturer’s standard sizes and of thicknesses indicated.


Provide preformed, tapered insulation boards where indicated for sloping to drain.  Fabricate with the following taper:



1/4 inch per 12 inches (1:48), unless otherwise indicated.


Provide preformed saddles, crickets, tapered edge strips, and other insulation shapes where indicated for sloping to drain.  Fabricate to slopes indicated.

Polyisocyanurate Board Insulation:  Rigid, cellular polyisocyanurate thermal insulation with core formed by using HCFCs as blowing agents, complying with ASTM C 1289, classified by facer type as follows:


Facer Type:  Type II, felt or glass-fiber mat on both major surfaces.

INSULATION ACCESSORIES:
General:  Furnish roofing insulation accessories recommended by insulation manufacturer for intended use and compatible with sheet roofing material.

Tapered Edge Strips:  Rigid, perlite insulation board, complying with ASTM C 728.

Protection Mat:  Woven or nonwoven polypropylene, polyolefin, or polyester fabric mat, water permeable and resistant to UV degradation, type and weight as recommended by roofing system manufacturer for application.

PART 3 - EXECUTION

EXAMINATION:
Examine substrates, areas, and conditions under which roofing will be applied, with Installer present, for compliance with requirements.

Verify that roof openings and penetrations are in place and set and braced and that roof drains are properly clamped into position.

Verify that wood blocking, curbs, and nailers are securely anchored to roof deck at roof penetrations and terminations and match the thicknesses of insulation required.


Verify that wood nailer strips are located perpendicular to roof slope and are spaced according to requirements of roofing system manufacturer.

Do not proceed with installation until unsatisfactory conditions have been corrected.

PREPARATION:
Clean substrate of dust, debris, and other substances detrimental to roofing installation according to roofing system manufacturer’s written instructions.  Remove sharp projections.

Prevent materials from entering and clogging roof drains and conductors and from spilling or migrating onto surfaces of other construction.  Remove roof-drain plugs when no work is taking place or when rain is forecast.

GENERAL INSTALLATION REQUIREMENTS:
Install modified bituminous membrane roofing system according to roofing system manufacturer’s written instructions and applicable recommendations of NRCA/ARMA’s “Quality Control Recommendations for Polymer Modified Bitumen Roofing.”


Install roofing system according to applicable specification plates of NRCA’s “The NRCA Roofing and Waterproofing Manual.”

Start installation of modified bituminous membrane roofing in presence of roofing system manufacturer’s technical personnel.

Shingling Plies:  Install modified bituminous membrane roofing system with ply sheets shingled uniformly to achieve required number of membrane plies throughout.  Shingle in direction to shed water.


Where roof slope exceeds 2 inch per 12 inches (2:12), run sheets of modified bituminous membrane roofing parallel with slope.  Backnail top ends of sheets to nailer strips.

Cant Strips:  Install and secure preformed 45-degree cant strips at junctures of modified bituminous membrane roofing system with vertical surfaces or angle changes greater than 45 degrees.

Cooperate with inspecting and testing agencies engaged or required to perform services for installing modified bituminous membrane roofing system.

Coordinate installing roofing system components so insulation and roofing plies are not exposed to precipitation or left exposed at the end of the workday or when rain is forecast.


Provide cutoffs at end of each day’s work to cover exposed ply sheets and insulation with a course of coated felt with joints and edges sealed.


Complete terminations and base flashings and provide temporary seals to prevent water from entering completed sections of roofing system.


Remove and discard temporary seals before beginning work on adjoining roofing.

INSULATION INSTALLATION:
Coordinate installing roofing system components so insulation is not exposed to precipitation or left exposed at the end of the workday.

Comply with roofing system manufacturer’s written instructions for installing roofing insulation.

Install tapered insulation under area of roofing to conform to slopes indicated and to Shop Drawings.

Install tapered edge strips at perimeter edges of roof that do not terminate at vertical surfaces.

Install one or more layers of insulation under area of roofing to achieve required thickness.  Where overall insulation thickness is 2 ½ inches (62.5 mm) or greater, install required thickness in 2 or more layers with joints of each succeeding layer staggered from joints of previous layer a minimum of 6 inches (150 mm) in each direction.

Trim surface of insulation where necessary at roof drains so completed surface is flush with ring of drain.

Nailer Strips:  Where roof slopes are greater than 2 inch per 12 inches (2:12), mechanically fasten to deck 4-inch nominal- (89-mm actual-) wide, wood nailer strips of same thickness as insulation, spaced not more than 20 to 21 feet (6.0 to 6.4 m) apart.  Run nailers perpendicular to slope of roof.

Install insulation with long joints of insulation in continuous straight lines with end joints staggered between rows, abutting edges and ends between boards.  Fill gaps exceeding 1/4 inch (6 mm) with insulation.


Cut and fit insulation within 1/4 inch (6 mm) of nailers, projections, and penetrations.

Attached Insulation:  Prime surface of concrete deck with asphalt primer at a rate of 3/4 gal./100 sq. ft. (0.3 L/sq. m), unless a greater weight is required by roofing system manufacturer, and allow primer to dry.  Set each layer of insulation in a solid mopping of hot roofing asphalt.

Attached Insulation:  Secure first layer of insulation to deck using a benign mineral spirit/asphalt based cold adhesive specifically designed for adhering specified board-type roofing insulation to deck type indicated.  Install subsequent layers of insulation in the same insulation cold-applied adhesive.


Fasten insulation according to requirements of FM’s “Approval Guide” for specified Windstorm Resistance Classification and the insulation and roofing system manufacturers’ written instructions.


Fasten insulation according to the insulation and roofing system manufacturers’ written instructions.

ROOF MEMBRANE INSTALLATION:
General:  Install modified bituminous membrane over area to receive roofing, according to manufacturer’s written instructions.  Extend modified bituminous membrane over and terminate beyond cants.


Unroll sheet and allow it to relax for the minimum time period required by manufacturer.

Two-Ply, Modified Bituminous Membrane:  Install 2 plies of modified bituminous membrane, consisting of a base ply and a finish ply, starting at low point of roofing system.


Base- and Finish-Ply Application:  Adhere each ply to substrate in cold adhesive, applied within 
temperature range and at rate required by roofing system manufacturer.

Laps:  Accurately align sheets, without stretching, and maintain uniform side and end laps.  Stagger end laps.  Heat-weld side and end laps and completely seal by rolling, leaving no voids.


Repair tears and voids in laps and lapped seams not completely sealed.


Apply granules, while asphalt is hot, to cover asphalt bead extruded at laps.

Install modified bituminous membranes with side laps shingled with slope of roof deck where possible.

Membrane Walkways:  Install another ply of modified bituminous membrane, approximately 36 inches (900 mm) wide and in lengths not exceeding 10 feet (3 m), leaving a space of 6 inches (150 mm) between strips.  Adhere walkways by same method used to adhere roof membrane.

FLASHING AND STRIPPING INSTALLATION:
Install modified bituminous membrane base flashing over cant strips and other sloping and vertical surfaces, at roof edges, and at penetrations through roof, and secure to substrates according to roofing system manufacturer’s written instructions and as follows:


Prime substrates with asphalt primer if required by roofing system manufacturer.


Base Flashing Application:  Torch apply modified bituminous membrane base flashing to substrate.


Or


Base Flashing Application:  Adhere modified bituminous membrane base flashing to substrate in cold adhesive, applied within temperature range and at rate required by roofing system manufacturer.

Extend base flashing up the wall a minimum of 8 inches (200 mm) above roof membrane and 4 inches (100 mm) onto field of roof membrane.

Mechanically fasten top of modified bituminous membrane base flashing securely at terminations and perimeter of roofing.


Seal top termination of base flashing.


Seal top termination of base flashing with a strip of glass-fiber fabric set in asphalt roofing cement.

Install modified bituminous stripping where metal flanges and edgings are set on membrane roofing, according to roofing system manufacturer’s written instructions.

Roof Drains:  Set 30-by-30-inch (760-by-760-mm) metal flashing in bed of asphalt roofing cement on completed modified bituminous membrane roofing.  Cover metal flashing with modified bituminous stripping extending a minimum of 4 inches (100 mm) beyond edge of metal flashing onto field of roof membrane.  Clamp roof membrane, metal flashing, and stripping into roof-drain clamping ring.

FIELD QUALITY CONTROL:
Final Roof Inspection:  Arrange for roofing system manufacturer’s technical personnel to inspect roofing installation on completion and submit report to Architect/Roofing Consultant.

Notify Architect/Roofing Consultant and Owner 48 hours in advance of the date and time of inspection.

PROTECTING AND CLEANING:
Protect modified bituminous membrane roofing from damage and wear during remainder of construction period.  When remaining construction will not affect or endanger roofing, inspect roofing for deterioration and damage, describing its nature and extent in a written report, with copies to Architect/Roofing Consultant and Owner.

Correct deficiencies in or remove modified bituminous roofing that does not comply with requirements, repair substrates, reinstall roofing, and repair base flashings to a condition free of damage and deterioration at the time of Substantial Completion and according to warranty requirements.

Clean overspray and spillage from adjacent construction using cleaning agents and procedures recommended by manufacturer of affected construction.

ROOFING INSTALLER’S WARRANTY:
WHEREAS <NAME> of <ADDRESS>, herein called the “Roofing Installer,” has performed roofing and associated work (“work”) on the following project:


Owner:


Address:


Building Name/Type:


Address:


Area of Work:


Acceptance Date:


Warranty Period:


Expiration Date:

AND WHEREAS Roofing Installer has contracted (either directly with Owner or indirectly as a subcontractor) to warrant said work against leaks and faulty or defective materials and workmanship for designated Warranty Period,

NOW THEREFORE Roofing Installer hereby warrants, subject to terms and conditions herein set forth, that during Warranty Period he will, at his own cost and expense, make or cause to be made such repairs to or replacements of said work as are necessary to correct faulty and defective work and as are necessary to maintain said work in a watertight condition.

This Warranty is made subject to the following terms and conditions:


Specifically excluded from this Warranty are damages to work and other parts of the building, and to building contents, caused by:



lightning;



fire;



failure of roofing system substrate, including cracking, settlement, excessive deflection, deterioration, and decomposition;



faulty construction of parapet walls, copings, chimneys, skylights, vents, equipment supports, and other edge conditions and penetrations of the work;



vapor condensation on bottom of roofing; and



activity on roofing by others, including construction contractors, maintenance personnel, other persons, and animals, whether authorized or unauthorized by Owner.


When work has been damaged by any of foregoing causes, Warranty shall be null and void until such damage has been repaired by Roofing Installer and until cost and expense thereof has been paid by Owner or by another responsible party so designated.


The Roofing Installer is responsible for damage to work covered by this Warranty but is not liable for consequential damages to building or building contents, resulting from leaks or faults or defects of work.


During Warranty Period, if Owner allows alteration of work by anyone other than Roofing Installer, including cutting, patching, and maintenance in connection with penetrations, attachment of other work, and positioning of anything on roof, this Warranty shall become null and void on date of said alterations, but only to the extent said alterations affect work covered by this Warranty.  If Owner engages Roofing Installer to perform said alterations, Warranty shall not become null and void, unless Roofing Installer, before starting said work, shall have notified Owner in writing, showing reasonable cause for claim, that said alterations would likely damage or deteriorate work, thereby reasonably justifying a limitation or termination of this Warranty.


During Warranty Period, if original use of roof is changed and it becomes used for, but was not originally specified for, a promenade, work deck, spray-cooled surface, flooded basin, or other use or service more severe than originally specified, this Warranty shall become null and void on date of said change, but only to the extent said change affects work covered by this Warranty.


The Owner shall promptly notify Roofing Installer of observed, known, or suspected leaks, defects, or deterioration and shall afford reasonable opportunity for Roofing Installer to inspect work and to examine evidence of such leaks, defects, or deterioration.


This Warranty is recognized to be the only warranty of Roofing Installer on said work and shall not operate to restrict or cut off Owner from other remedies and resources lawfully available to Owner in cases of roofing failure.  Specifically, this Warranty shall not operate to relieve Roofing Installer of responsibility for performance of original work according to requirements of the Contract Documents, regardless of whether Contract was a contract directly with Owner or a subcontract with Owner’s General Contractor.

IN WITNESS THEREOF, this instrument has been duly executed this <DAY> day of <MONTH>, 20<YEAR>.


Authorized Signature:


Name:


Title:

END OF SECTION 07551 - 2/96

