554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

dammonengineering.com

info@dammonengineering.com

# Structural Inspection

February 13, 2025

Anthony Herbert

6160 2nd Street

Bay St. Louis, Ms. 39520

Construction:

Raised one-story wood frame home, on wood columns with a metal roof.

Scope:

This inspection is limited to a visual inspection of the 21 wood columns supporting the home; No Inspection of the mechanical, plumbing or electrical systems was performed.  This report is as outlined by the National Academy of Building Inspection Engineers and is not an explanation of cause, effect, or engineering.

History:

Dammon Engineering was contacted to perform a structural inspection of the referenced home due to the concerns of damaged wood columns supporting the home.

Findings:

An overall visual inspection was conducted of the 21 8”x 8” wood columns.  All of the wood columns have rotten basses at the bottom near the concrete foundation.  Some have more damage than others.  The signs of damage are noted by the color of the wood. A hammer was used to tap on the columns and listen for the sound of solidness and hollowness. All of these columns have a hollowness sound near the bottom of the column.

Conclusion:

It is our opinion that all of the wood columns should be replaced or repaired with the same size wood column.

Sincerely,

Brian Mistich, P.E.

See attached Photos