STRUCTURAL INSPECTION

Date:
June 17, 2003

Type:
Residential

For:
Joni Howard/Century 21

Slidell, La 

Re:
Keith Laborde

135 Trafalgar

Slidell, La. 70461 

History:

The home is approximately 25+ years old with a square footage of 1,500.  It is wood frame construction on a concrete foundation with brick veneer and vinyl siding. Joni Howard W/Century 21 Realtors contacted us to perform a structural inspection due to cracks in the concrete foundation.

Findings:

The carpet has been removed in all the rooms except were they have vinyl flooring. If the vinyl flooring is removed I am sure it will also have cracks in the concrete. Upon inspection, it was noted that there were several cracks in the foundation, ranging from 1/16” to ¼” wide. Some were noted all the way from the front of the home to the rear. Viewing it from the exterior, some of these cracks go all the way through to the footings. And in some instances the exterior brick walls have cracks. There are no visibly signs of cracks in the walls or ceilings.

Analysis:

This house, being the age it is, has gone through many years of contraction & expansion. There are two remedies for this problem. Step 1, Hire a foundation expert to check the tension of the post tension foundation to see if it can be tightened to close up the cracks prior to it being closed up it must be treated for termites. Step 2, fill in the cracks of the foundation and brick walls with an epoxy filler after the foundation and the cracks have been treated for termites.

Conclusion:

It is my professional opinion that after the house has been repaired with one of the above that it would be structurally sound.
Sincerely,

Emmett G. (Pete) Dammon, P.E.

Louisiana License No. 8796
This inspection is limited to the apparent visual conditions of the structural components of this building.  It does not cover, nor attempts to cover, any components, items, and/or conditions which, by their nature or location, are concealed or are difficult or hazardous to inspect, or which require the moving of furniture, flooring materials, rugs, fixtures, appliances, or any component-part nailed, bolted, or screwed down or shut.  No opinions are expressed regarding conditions which could be discovered only by the disassembly of any component parts, special testing, or removal of any concealing objects.

Inspections are made under normal weather conditions, and are not opinions of the conditions of the property and/or structure which may exist under unusual weather conditions, such as, but not limited to floods, heavy rains or snows, high winds, temperature extremes, or any act of God.  Specific hazardous wastes, toxic substances, toxic mold, air and water quality, communicable diseases, asbestos, soil, environmental, radon, carbon monoxide, formaldehyde, building code and termite conditions are not included in this report unless otherwise stipulated.

This report is not a warranty or guarantee of the property inspected, but it is our opinion of its condition at the time inspected.  Our liability shall be limited to reimbursement of the total cost of inspection.


