ST. TAMMANY FIRE PROTECTION DISTRICT NO. 1

NEW TRAINING FACILITY

34780 S. RANGE ROAD 

SLIDELL LA  70460


Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 081416
FLUSH WOOD DOORS
Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Solid-core doors with wood-veneer faces.

2. Factory finishing flush wood doors.

3. Factory fitting flush wood doors to frames and factory machining for hardware.

1.2 ACTION SUBMITTALS

A. Product Data: For each type of door. Include factory-finishing specifications.

B. Shop Drawings: Indicate location, size, and hand of each door; elevation of each kind of door; construction details not covered in Product Data; and the following:

1. Dimensions and locations of blocking.

2. Dimensions and locations of mortises and holes for hardware.

3. Dimensions and locations of cutouts.

4. Undercuts.

5. Requirements for veneer matching.

6. Doors to be factory finished and finish requirements.

7. Fire-protection ratings for fire-rated doors.

C. Samples: For factory-finished doors.
1.  
Provide factory finishes applied to actual door face materials for each material and finish.  For each wood species and transparent finish, produce set of three samples showing typical examples of color and grain to be expected in finished work.

2.
Louver blade and frame section minimum 6 inches long for each material and finish specified.
1.3 INFORMATIONAL SUBMITTALS

A. Quality Standard Compliance Certificates: AWI Quality Certification Program certificates.

1.4 QUALITY ASSURANCE

Retain "Manufacturer Qualifications" and "Vendor Qualifications" paragraphs below if required for LEED.

A. Manufacturer Qualifications: A qualified manufacturer that is a certified participant in AWI's Quality Certification Program.

Chain-of-custody certification is not required for subcontractors (entities that install products) but is required for vendors unless they are simply acting as an agent of manufacturer and the sale is actually between manufacturer and Contractor or subcontractor.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 MANUFACTURERS

Retain "Manufacturers" Paragraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

A. Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Manufacturers listed are representative only; many others make flush wood doors. See WDMA's and AWI's Web sites for listings of door manufacturers. Retain only manufacturers offering doors complying with requirements selected for each type used, and insert other manufacturers offering suitable products. See Evaluations and manufacturers' catalogs.

1. Algoma Hardwoods, Inc.

2. Ampco.

3. Chappell Door Co.

4. Eggers Industries.

5. General Veneer Manufacturing Co.

6. Graham Wood Doors; an Assa Abloy Group company.

7. Haley Brothers, Inc.

8. Ipik Door Company.

9. Lambton Doors.

10. Marlite.

11. Marshfield Door Systems, Inc.

12. Mohawk Doors; a Masonite company.

13. Oshkosh Door Company.

14. Poncraft Door Company.

15. Vancouver Door Company.

16. VT Industries, Inc.

2.2 FLUSH WOOD DOORS, GENERAL

Retain one standard in "Quality Standard" Paragraph below. Review retained standard and coordinate its requirements with retained options. See Evaluations.

A. Quality Standard: In addition to requirements specified, comply with AWI's, AWMAC's, and WI's "Architectural Woodwork Standards, WDMA I.S.1-A, "Architectural Wood Flush Doors."

If retaining subparagraph below, verify applicability of certification for Project's geographic location. Certification programs of both organizations are available to member and nonmember firms.

1. Provide AWI Quality Certification Labels indicating that doors comply with requirements of grades specified.

Retain first "Regional Materials" Paragraph below for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5 and LEED-CI Credit MR 5, Option 2; before retaining, verify availability of materials that comply. An alternative method of dealing with these credit requirements is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.16 "Sustainable Design Requirements - LEED for Commercial Interiors," or Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development" that gives Contractor the option and responsibility to determine how these credit requirements will be met.

Retain "WDMA I.S.1-A Performance Grade" Paragraph below to specify performance grade if referencing WDMA I.S.1-A. See Evaluations.

B. WDMA I.S.1-A Performance Grade:

1. Heavy Duty unless otherwise indicated.

Retain "Fire-Rated Wood Doors" Paragraph below if applicable.

C. Fire-Rated Wood Doors: Doors complying with NFPA 80 that are listed and labeled by a qualified testing agency, for fire-protection ratings indicated, based on testing at positive pressure according to UL 10C.

1. Cores: Provide core specified or mineral core as needed to provide fire-protection rating indicated.

Retain "Edge Construction" Subparagraph below unless using surface-applied intumescent seals.

2. Edge Construction: Provide edge construction with intumescent seals concealed by outer stile. Comply with specified requirements for exposed edges.

Retain "Pairs" Subparagraph below if steel edges and astragals are unacceptable. Coordinate availability and ratings with manufacturers.

3. Pairs: Provide fire-retardant stiles that are listed and labeled for applications indicated without formed-steel edges and astragals. Provide stiles with concealed intumescent seals. Comply with specified requirements for exposed edges.

Retain "Smoke- and Draft-Control Door Assemblies" Paragraph below if required. The IBC requires fire door assemblies to comply with smoke- and draft-control requirements in corridors, smoke barriers, and smoke partitions.

D. Smoke- and Draft-Control Door Assemblies: Listed and labeled for smoke and draft control, based on testing according to UL 1784.

Retain "Particleboard-Core Doors" Paragraph below if doors have particleboard cores.

E. Particleboard-Core Doors:

Retain one or more of four options in "Particleboard" Subparagraph below. Grade LD-2 makes a stronger door, has higher screw-holding capacity, and is standard with some manufacturers and optional with others. Before retaining last option, verify availability with door manufacturers.

1. Particleboard: ANSI A208.1, Grade LD-1 or Grade LD-2, made with binder containing no urea-formaldehyde.

2. Blocking: Provide wood blocking in particleboard-core doors as needed to eliminate through-bolting hardware.

3. Provide doors with glued-wood-stave or structural-composite-lumber cores instead of particleboard cores for doors indicated to receive exit devices.

F. Structural-Composite-Lumber-Core Doors:

1. Structural Composite Lumber: WDMA I.S.10.

a. Screw Withdrawal, Face: 700 lbf (3100 N).

b. Screw Withdrawal, Edge: 400 lbf (1780 N).

G. Mineral-Core Doors:

1. Core: Noncombustible mineral product complying with requirements of referenced quality standard and testing and inspecting agency for fire-protection rating indicated.

2. Blocking: Provide composite blocking with improved screw-holding capability approved for use in doors of fire-protection ratings indicated as needed to eliminate through-bolting hardware.

3. Edge Construction: At hinge stiles, provide laminated-edge construction with improved screw-holding capability and split resistance. Comply with specified requirements for exposed edges.

2.3 VENEER-FACED DOORS FOR TRANSPARENT FINISH

See the tables at the end of the Evaluations for a list of manufacturers' products. Use these tables in combination with manufacturers' catalogs or product data to insert series, type, model, and designations of other characteristics.

Copy appropriate paragraphs below and re-edit for each product.

Insert drawing designation for each product required. Use these designations on Drawings to identify each product.

A. Interior Solid-Core Doors <Insert drawing designation>:

AWI's, AWMAC's, and WI's "Architectural Woodwork Standards" requires Grade AA faces for Premium-grade doors; WDMA I.S.1-A requires Grade A faces for Premium-grade doors. Both standards require Grade A faces for Custom-grade doors unless Grade B is specified. See Evaluations.

1. Grade: Premium, with Grade AA faces.

Options in "Species" Subparagraph below are examples only; revise or insert another species.

2. Species: Select white birch.

"Rift cut" option in "Cut" Subparagraph below applies only to oak.

3. Cut: Quarter sliced.

"Pleasing" option in "Match between Veneer Leaves" Subparagraph below is available only with Grade B veneers.

4. Match between Veneer Leaves: Pleasing match.

"Center-balance" option in "Assembly of Veneer Leaves on Door Faces" Subparagraph below is expensive. AWI's, AWMAC's, and WI's "Architectural Woodwork Standards" requires center-balance match for Premium-grade doors. "Running" option is standard for Custom-grade and WDMA Premium-grade doors. See Evaluations.

5. Assembly of Veneer Leaves on Door Faces: Balance match.

6. Pair and Set Match: Provide for doors hung in same opening.

Retain one of five options in "Core" Subparagraph below.

7. Core: Particleboard Glued wood stave Either glued wood stave or structural composite lumber.

8. Construction: Seven plies. Stiles and rails are bonded to core, then entire unit is abrasive planed before veneering. Faces are bonded to core using a hot press.

Retain one of first two options in "Construction" Subparagraph above or retain "Construction" Subparagraph below. Third option above applies to some five-ply doors. Glued-wood-stave core is available only with bonded construction and nonglued-wood-stave core is available only with nonbonded construction.

9. Construction: Seven plies, either bonded or nonbonded construction.

2.4 LIGHT FRAMES AND LOUVERS

Retain "Wood-Veneered Beads for Light Openings in Fire-Rated Doors" or "Metal Frames for Light Openings in Fire-Rated Doors" Paragraph below if required for doors with fire-protection rating exceeding 20 minutes.

A. Metal Louvers:

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following:

a. Air Louvers, Inc.

b. Anemostat; a Mestek company.

c. L & L Louvers, Inc.

d. Louvers & Dampers, Inc.; a division of Mestek, Inc.

e. McGill Architectural Products.

Retain one of three "Metal and Finish" subparagraphs below.

2. Metal and Finish: Hot-dip galvanized steel, 0.040 inch (1.0 mm) thick, with baked-enamel- or powder-coated finish.

3. Metal and Finish: Extruded aluminum with Class II, clear anodic finish, AA-M12C22A31.

2.5 FABRICATION

Delete first paragraph below if no doors are required to be factory fitted. Retain paragraph and revise to indicate exceptions if only some doors are required to be factory fitted. Plastic-laminate-edged and factory-finished doors must be factory fitted and machined. Fire-rated and plastic-laminate-faced doors with wood edges should also be factory fitted and machined. Factory fitting and machining for other doors are optional. See Evaluations.

A. Factory fit doors to suit frame-opening sizes indicated. Comply with clearance requirements of referenced quality standard for fitting unless otherwise indicated.

1. Comply with NFPA 80 requirements for fire-rated doors.

Delete first paragraph below if no doors are required to be factory machined. Retain paragraph and revise to indicate exceptions if only some doors are required to be factory machined. See Evaluations.

B. Factory machine doors for hardware that is not surface applied.

C. Openings: Factory cut and trim openings through doors.

1. Light Openings: Trim openings with moldings of material and profile indicated.

"Glazing" Subparagraph below is unnecessary if using only metal light frames.

2. Glazing: Factory install glazing in doors indicated to be factory finished. Comply with applicable requirements in Section 08800 "Glazing."

3. Louvers: Factory install louvers in prepared openings.

2.6 SHOP PRIMING

Retain this article if field-finished doors are required to be shop primed. Factory fitting is recommended to minimize damage to shop-primed doors.

A. Doors for Opaque Finish: Shop prime faces, all four edges, edges of cutouts, and mortises with one coat of wood primer specified in Section “Interior Painting."

2.7 FACTORY FINISHING

Retain this article if factory finishing is required. Factory finishing can be used to help comply with LEED-NC, LEED-CS, or LEED-CI Credit IEQ 4.2, which limits VOC content of paints and coatings used within buildings. Factory finishing also has other advantages. See Evaluations.

A. General: Comply with referenced quality standard for factory finishing. Complete fabrication, including fitting doors for openings and machining for hardware that is not surface applied, before finishing.

1. Finish faces, all four edges, edges of cutouts, and mortises. Stains and fillers may be omitted on top and bottom edges, edges of cutouts, and mortises.

B. Factory finish doors that are indicated to receive transparent finish.

Retain first paragraph below if required for LEED for Schools Credit IEQ 4.

C. Use only paints and coatings that comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

D. Transparent Finish:

In "Grade" Subparagraph below, usually retain same grade for finish as specified for doors.

1. Grade: Premium.

Retain one of two "Finish" subparagraphs below and one or more options in subparagraph retained, or insert another option. Before specifying, verify availability of finishes with manufacturers. Caution: Finish systems vary among manufacturers. Require Samples for verification.

2. Finish: AWI's, AWMAC's, and WI's "Architectural Woodwork Standards" System 5, conversion varnish or System 9, UV curable, acrylated epoxy, polyester, or urethane or System 10, UV curable, water based or System 11, catalyzed polyurethane.

3. Finish: WDMA TR-4 conversion varnish or WDMA TR-6 catalyzed polyurethane.

4. Staining: As selected by Architect from manufacturer's full range.

Retain one of three options in "Staining" Subparagraph above and usually one of three options in "Effect" Subparagraph below. Some door manufacturers will not provide filled finish because filling is best done by hand, which cannot be done on a finishing line; instead, some will offer semifilled finish as described below. Delete subparagraph below if using only closed-grain wood species.

5. Effect: Open-grain finish.

Retain one of two options in "Sheen" Subparagraph below or revise to suit Project.

6. Sheen: Satin.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. Hardware: For installation, see Section "Door Hardware."

B. Installation Instructions: Install doors to comply with manufacturer's written instructions and referenced quality standard, and as indicated.

Retain first subparagraph below for fire-rated doors.

1. Install fire-rated doors according to NFPA 80.

Retain subparagraph below for smoke- and draft-control doors. The IBC requires fire door assemblies to comply with smoke- and draft-control requirements in corridors, smoke barriers, and smoke partitions.

2. Install smoke- and draft-control doors according to NFPA 105.

Retain "Job-Fitted Doors" Paragraph below if all doors are not factory fitted. Factory fitting of fire-rated doors is preferred to job fitting because of limitations on trimming narrower stiles and rails.

C. Job-Fitted Doors: Align and fit doors in frames with uniform clearances and bevels as indicated below; do not trim stiles and rails in excess of limits set by manufacturer or permitted for fire-rated doors. Machine doors for hardware. Seal edges of doors, edges of cutouts, and mortises after fitting and machining.

1. Clearances: Provide 1/8 inch (3.2 mm) at heads, jambs, and between pairs of doors. Provide 1/8 inch (3.2 mm) from bottom of door to top of decorative floor finish or covering unless otherwise indicated. Where threshold is shown or scheduled, provide 1/4 inch (6.4 mm) from bottom of door to top of threshold unless otherwise indicated.

Retain subparagraph below for fire-rated doors or if doors are not factory fitted.

a. Comply with NFPA 80 for fire-rated doors.

D. Factory-Fitted Doors: Align in frames for uniform clearance at each edge.

E. Factory-Finished Doors: Restore finish before installation if fitting or machining is required at Project site.

END OF SECTION 081416
	FLUSH WOOD DOORS
	081416 - 1



