ST. TAMMANY FIRE PROTECTION DISTRICT NO. 1

NEW TRAINING FACILITY

34780 S. RANGE ROAD 

SLIDELL LA  70460


Copyright 2002 and 2005, The American Institute of Architects (AIA)

SECTION 093013 - CERAMIC TILING
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

A. This Section includes the following:

Adjust list below to suit Project.

1. Ceramic mosaic tile. 

2. Quarry tile. 

3. Pressed floor tile. 

4. Porcelain tile. 

5. Glazed wall tile. 

6. Glass Tile. 

7. Stone thresholds. 

8. Tile backing panels. 

9. Waterproof membrane for thinset applications. 

If allowances, unit prices, or alternates apply to Work of this Section, insert brief paragraphs here to alert Contractor and reference appropriate Division 01 Sections for specific details.  Coordinate description with applicable paragraphs in Parts 2 and 3.

1.3 DEFINITIONS

Retain terms that remain after this Section has been edited.

First definition below is based on definitions in ASTM C 119 and in MIA's "Dimension Stone Design Manual."

A. General: Definitions in the ANSI A108 series of tile installation standards and in ANSI A137.1 apply to Work of this Section unless otherwise specified.

B. ANSI A108 Series: ANSI A108.01, ANSI A108.02, ANSI A108.1A, ANSI A108.1B, ANSI A108.1C, ANSI A108.4, ANSI A108.5, ANSI A108.6, ANSI A108.8, ANSI A108.9, ANSI A108.10, ANSI A108.11, ANSI A108.12, ANSI A108.13, ANSI A108.14, ANSI A108.15, ANSI A108.16, and ANSI A108.17, which are contained in its "Specifications for Installation of Ceramic Tile.".

Delete finish paragraphs below not required.  Not all finishes below are available for all stone varieties.

Visual test for polished finish in first paragraph below requires surface flatness that cannot be measured with a straightedge.

C. Module Size: Actual tile size plus joint width indicated.

D. Face Size: Actual tile size, excluding spacer lugs.

1.4 SUBMITTALS

A. Product Data:  For each type of product indicated.

Delete first paragraph below if tile installations are not complex enough to justify Shop Drawings.

B. Shop Drawings:  Show locations of each type of tile and tile pattern.  Show widths, details, and locations of expansion, contraction, control, and isolation joints in substrates and finished ceramic tile surfaces.

C. Samples for Initial Selection:  For each type of grout indicated and accessories involving color selection.

Delete paragraph above if colors and other characteristics are preselected and specified or scheduled.  Retain paragraph and subparagraphs below with or without above.  Revise list of Samples to correspond with products specified.

D. Samples for Verification:

Retain one or more of first three subparagraphs below.

1. Full-size units of each type and composition of tile and for each color and finish required. For ceramic mosaic tile in color blend patterns, provide full sheets of each color blend.

Samples in subparagraph below may be a good alternative to mockups.  Samples below will generally be smaller than most mockups but have the advantage that they can be submitted before Project is ready for constructing a mockup.

2. Full-size units of each type of trim and accessory for each color and finish required.

Division 01 Section "Submittal Procedures" requires that Samples for verification "show the full range of color and texture variations expected," but this requirement may not be adequate for stone varieties that exhibit wide variations in color and veining.  First subparagraph below should provide better control.

3. Ceramic thresholds in 6-inch lengths.

Retain paragraph and subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1; coordinate with requirements selected in Part 2 for adhesives and sealants.

Coordinate first paragraph below with qualification requirements in Division 01 Section "Quality Requirements."

1.5 QUALITY ASSURANCE

Delete first paragraph below if not required by size of Project.

A. Supplier Qualifications:  A firm experienced in supplying products similar to those indicated for the Project and with a record of successful in-service performance.

B. Source Limitations for Ceramic Tile. Obtain each type of ceramic product through one source from a single producer.

Subparagraph below may help provide consistent appearance for each stone variety among tiles with different finishes and thresholds but may not always be practical or necessary.  Unless large quantities of a variety of stone are used, tiles and possibly thresholds may be stock items, in which case the supplier will have no control over which quarry location and possibly even quarry the material comes from.  For varieties that exhibit a high degree of consistency, below may not be necessary.

1. Obtain each variety of ceramic, regardless of product, size, and finish, from same location in a single quarry with resources to provide materials of consistent quality in appearance and physical properties.

C. Source Limitations for Setting and Grouting Materials:  Obtain each type of manufactured product through one source from a single manufacturer.

Delete subparagraph below if no aggregates are added at Project site.

1. For aggregates added at Project site, obtain from one source or producer.

D. Source Limitations for Other Products:  Obtain each of the following products specified in this Section through one source from a single manufacturer:

Delete products below not retained in Part 2 and insert those that are added.

1. Joint sealants.

2. Cementitious backer units.

3. Metal edge strips.

Delete paragraph and subparagraphs below if not required.  If retaining, indicate location, size, and other details of mockups on Drawings or by inserts.  Revise wording if only one mockup is required.

E. Mockups:  Build mockups to verify selections made under sample submittals and to demonstrate aesthetic effects.

Division 01 Section "Quality Requirements" states "build mockups in location and of size indicated or, if not indicated, as directed." Consider inserting size and location requirements in two subparagraphs below or showing on Drawings.

1. Build mockup of[ each type of floor tile installation.

2. Build mockup of[ each type of wall tile installation.

Retain subparagraph below if mockups are erected as part of building rather than separately and the intention is to make an exception to the default requirement in Division 01 Section "Quality Requirements" for demolishing and removing mockups when directed, unless otherwise indicated.

3. Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Delete paragraph below if Work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 01.

1.6 DELIVERY, STORAGE, AND HANDLING

A. Deliver materials to Project site in factory wrappings, clearly labeled with identification of manufacturer and lot number.

B. Store tile and cementitious materials on elevated platforms, under cover, and in a dry location.

C. Store aggregates where grading and other required characteristics can be maintained and contamination avoided.

D. Store liquid latexes and emulsion adhesives in unopened containers and protected from freezing.

1.7 PROJECT CONDITIONS

A. Environmental Limitations:  Do not install ceramic tile until construction in spaces is complete and ambient temperature and humidity conditions are maintained at the levels indicated in referenced standards and manufacturer's written instructions.

1.8 SEQUENCING AND SCHEDULING

A. Sequence ceramic tile installation with other work to minimize possibility of damage and soiling during remainder of construction period.

B. Install ceramic tile and accessories only after other finishing operations, including painting, have been completed.

PART 2 -  PRODUCTS

2.1 MANUFACTURERS
Retain one of three paragraphs and associated subparagraphs below.  Retain first for nonproprietary specification, second for semiproprietary specification, or third for proprietary specification.  Refer to Division 01 Section "Product Requirements."

A. Source Limitations for Tile: Obtain tile of each type from single source or producer.
1. Obtain tile of each type and color or finish from same production run and of consistent quality in appearance and physical properties for each contiguous area. 

B. Source Limitations for Setting and Grouting Materials: Obtain ingredients of a uniform quality for each mortar, adhesive, and grout component from single manufacturer and each aggregate from single source or producer. 

1. Obtain setting and grouting materials, except for unmodified Portland cement and aggregate, from single manufacturer. 

2. Obtain waterproof membrane and crack isolation membrane, except for sheet products, from manufacturer of setting and grouting materials. 

C. Source Limitations for Other Products: Obtain each of the following products specified in this Section from a single manufacturer: 

1. Stone thresholds. 

2. Waterproof membrane. 

3. Crack isolation membrane. 

4. Cementitious backer units.Copy and re-edit paragraph and subparagraphs below for each stone tile type required.  Delete inapplicable subparagraphs.  Insert number to complete designation for each stone tile type retained below.  Use this designation on Drawings to show where each stone tile type is required.

D. Ceramic Threshold Installation[ STHI-<#>]:  Interior installation on cementitious backer units over wood; thin-set mortar; TCA F144 and ANSI A108.5.

1. Ceramic Threshold Type:  <Insert ceramic threshold type designation.>

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

2.2  PRODUCTS, GENERAL

A. ANSI Ceramic Tile Standard: Provide tile that complies with ANSI A137.1 for types, compositions, and other characteristics indicated. 

B. ANSI Standards for Tile Installation Materials: Provide materials complying with ANSI A108.02, ANSI standards referenced in other Part 2 articles, ANSI standards referenced by TCNA installation methods specified in tile installation schedules, and other requirements specified. 

C. Factory Blending: For tile exhibiting color variations within ranges, blend tile in factory and package so tile units taken from one package show same range in colors as those taken from other packages and match approved Samples. 

D. Mounting: For factory-mounted tile, provide back- or edge-mounted tile assemblies as standard with manufacturer unless otherwise indicated. 

1. Where tile is indicated for installation on exteriors or in wet areas, do not use back- or edge-mounted tile assemblies unless tile manufacturer specifies in writing that this type of mounting is suitable for installation indicated and has a record of successful in-service performance. 

2.3 TILE PRODUCTS 

A.  Ceramic Tile Type: Factory-mounted glazed ceramic mosaic tile. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. American Olean; a division of Dal-Tile Corporation. 

b. Crossville, Inc. 

c. Daltile. 

2. Composition: [Porcelain] [Impervious natural clay or porcelain] [Vitreous or impervious natural clay or porcelain]. 

3. Certification: Porcelain tile certified by the Porcelain Tile Certification Agency. 

4. Module Size: <Insert dimensions>. 

5. Thickness: 1/4 inch (6.4 mm). 

6. Face: [Plain] [Pattern of design indicated,] with cushion edges. 

7. Surface: [Smooth, without] [Slip resistant, with] abrasive admixture. 

8. Dynamic Coefficient of Friction: Not less than 0.42. 

9. Finish: <Insert description> glaze. 

10. Tile Color and Pattern: <Insert color and pattern>. 

11. Grout Color: <Insert color>. 

12. Trim Units: Coordinated with sizes and coursing of adjoining flat tile where applicable and matching characteristics of adjoining flat tile. Provide shapes as follows, selected from manufacturer's standard shapes: 

a. Base Cove: Cove, module size <Insert dimensions>. 

b. Base Cap for Portland Cement Mortar Installations: Bead (bullnose), module size <Insert dimensions>. 

c. Base Cap for Thinset Mortar Installations: Surface bullnose, module size Insert dimensions.
d. Wainscot Cap for Portland Cement Mortar Installations: Bead (bullnose), module size <Insert dimensions>. 

e. Wainscot Cap for Thinset Mortar Installations: Surface bullnose, module size <Insert dimensions>. 

f. Wainscot Cap for Flush Conditions: Regular flat tile for conditions where tile wainscot is shown flush with wall surface above it, same size as adjoining flat tile. 

g. External Corners for Portland Cement Mortar Installations: Bead (bullnose), module size <Insert dimensions>. 

h. External Corners for Thinset Mortar Installations: Surface bullnose, module size <Insert dimensions>. 

i. Internal Corners: Cove, module size <Insert dimensions>. 

j. Internal Corners: Field-butted square corners. For coved base and cap, use angle pieces designed to fit with stretcher shapes. 

B. Ceramic Tile Type: Glazed square-edged quarry tile. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. American Olean; a division of Dal-Tile Corporation. 

b. Daltile. 

c. Florida Brick & Clay Company Inc. 

d. Quarry Tile Co. 

e. Summitville Tiles, Inc. 

2. Face Size: <Insert dimensions>. 

3. Thickness: [3/8 inch (9.5 mm)] [1/2 inch (12.7 mm)] [3/4 inch (19 mm)]. 

4. Wearing Surface: [Nonabrasive, smooth] [Abrasive aggregate embedded in surface]. 

5. Dynamic Coefficient of Friction: Not less than 0.42. 

6. Finish: <Insert description> glaze. 

7. Tile Color and Pattern: <Insert color and pattern>. 

8. Grout Color: <Insert color>. 

9. Trim Units: Coordinated with sizes and coursing of adjoining flat tile where applicable and matching characteristics of adjoining flat tile. Provide shapes as follows, selected from manufacturer's standard shapes: 

a. Base: Coved with surface bullnose top edge, face size <Insert dimensions>. 

b. Wainscot Cap: Surface bullnose, face size <Insert dimensions>. 

c. Wainscot Cap for Flush Conditions: Regular flat tile for conditions where tile wainscot is shown flush with wall surface above it, same size as adjoining flat tile. 

C. Ceramic Tile Type: Glazed matte porcelain tile. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. Florim USA
b. American Olean; a division of Dal-Tile Corporation. 

c. Crossville, Inc. 

d. Daltile. 

2. Certification: Tile certified by the Porcelain Tile Certification Agency. 

3. Face Size: 6” (152 mm) x 36” (914 mm). 

4. Face Size Variation: Rectified.

5. Thickness: 5/16” (8 mm). 

6. Dynamic Coefficient of Friction: Not less than 0.42. 

8. Tile Color, Glaze, and Pattern: Cocoa/Monica, matte glaze. 

9. Grout Color: Selected by owner, see submittals.
D. Ceramic Tile Type: Glazed wall tile. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. American Marazzi Tile, Inc. 

b. American Olean; a division of Dal-Tile Corporation. 

c. Daltile. 
d. Florim USA

2. Module Size: <Insert dimensions>. 

3. Face Size Variation: Rectified. 

4. Thickness: 5/16 inch (8 mm). 

5. Finish: [Bright, opaque] [Bright, clear] [Mat, opaque] [Mat, clear] [Semimat, opaque] [Semimat, clear] [Vellum, opaque] [Vellum, clear] [Crystalline] <Insert description> glaze. 

7. Tile Color and Pattern: <Insert color and pattern>. 

8. Grout Color: Selected by owner, see submittals.
9. Mounting: Factory, back mounted. 

10. Trim Units: Coordinated with sizes and coursing of adjoining flat tile where applicable and matching characteristics of adjoining flat tile. Provide shapes as follows, selected from manufacturer's standard shapes: 

a. Base for Portland Cement Mortar Installations: Coved, module size <Insert dimensions>. 

b. Base for Thinset Mortar Installations: Straight, module size <Insert dimensions>. 

c. Wainscot Cap for Portland Cement Mortar Installations: Bullnose cap, module size <Insert dimensions>. 

d. Wainscot Cap for Thinset Mortar Installations: Surface bullnose, module size <Insert dimensions>. 

e. Wainscot Cap for Flush Conditions: Regular flat tile for conditions where tile wainscot is shown flush with wall surface above it, same size as adjoining flat tile. 

f. External Corners for Portland Cement Mortar Installations: Bullnose shape with radius of at least 3/4 inch (19 mm) unless otherwise indicated.

g. External Corners for Thinset Mortar Installations: Surface bullnose, same size as adjoining flat tile. 

h. Internal Corners: Field-butted square corners. For coved base and cap use angle pieces designed to fit with stretcher shapes. 

2.4 THRESHOLDS 

A. General: Fabricate to sizes and profiles indicated or required to provide transition between adjacent floor finishes. 

1. Bevel edges at 1:2 slope, with lower edge of bevel aligned with or up to 1/16 inch (1.5 mm) above adjacent floor surface. Finish bevel to match top surface of threshold. Limit height of threshold to 1/2 inch (12.7 mm) or less above adjacent floor surface. 

B. Granite Thresholds: ASTM C 615/C 615M, with [polished] [honed] finish. 

1. Description: Uniform, [fine] [medium]-grained, <Insert color> stone without veining. 

2. Description: Match Architect's sample. 

C. Marble Thresholds: ASTM C 503/C 503M, with a minimum abrasion resistance of [10] [12] according to ASTM C 1353 or ASTM C 241/C 241M and with honed finish. 

1. Description: Uniform, fine- to medium-grained white stone with gray veining. 

2. Description: Match Architect's sample. 

2.6 TILE BACKING PANELS 

A. Cementitious Backer Units: ANSI A118.9 or ASTM C 1325, Type A, in maximum lengths available to minimize end-to-end butt joints. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. C-Cure. 

b. Custom Building Products. 

c. Georgia-Pacific Building Products. 

2. Thickness: 5/8 inch (15.9 mm). 

2.7 WATERPROOF MEMBRANE 

A. General: Manufacturer's standard product that complies with ANSI A118.10 and is recommended by the manufacturer for the application indicated. Include reinforcement and accessories recommended by manufacturer.

B. Fabric-Reinforced, Modified-Bituminous Sheet: Self-adhering, SBS-modified-bituminous sheet with fabric reinforcement facing; 0.040-inch (1 -mm) nominal thickness. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. Boiardi Products Corporation; a QEP company. 

2.8 CRACK ISOLATION MEMBRANE 

A. General: Manufacturer's standard product that complies with ANSI A118.12 for high performance and is recommended by the manufacturer for the application indicated. Include reinforcement and accessories recommended by manufacturer. 

B. Latex-Portland Cement Crack-Resistant Mortar: Flexible mortar consisting of cement-based mix and latex additive. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. ARDEX Americas. 

b. Boiardi Products Corporation; a QEP company. 

c. C-Cure. 

d. MAPEI Corporation. 

2.9 SETTING MATERIALS 

A. Portland Cement Mortar (Thickset) Installation Materials: ANSI A108.02. 

1. Cleavage Membrane: Asphalt felt, ASTM D 226/D 226M, Type I (No. 15); or polyethylene sheeting, ASTM D 4397, 4.0 mils (0.1 mm) thick. 

2. Reinforcing Wire Fabric: Galvanized, welded-wire fabric, 2 by 2 inches (50.8 by 50.8 mm) by 0.062-inch (1.57-mm) diameter; comply with ASTM A 185/A 185M and ASTM A 82/A 82M, except for minimum wire size. 

3. Expanded Metal Lath: Diamond-mesh lath complying with ASTM C 847. 

a. Base Metal and Finish for Interior Applications: Uncoated or zinc-coated (galvanized) steel sheet, with uncoated steel sheet painted after fabrication into lath. 

b. Base Metal and Finish for Exterior Applications: Zinc-coated (galvanized) steel sheet. 

c. Configuration over Studs and Furring: Flat. 

d. Configuration over Solid Surfaces: Self-furring. 

e. Weight: 2.5 lb/sq. yd. (1.4 kg/sq. m). 

B. Dry-Set Portland Cement Mortar (Thinset): ANSI A118.1. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. Boiardi Products Corporation; a QEP company. 

b. Bonsal American, an Oldcastle company. 

c. Bostik, Inc.

d. Laticrete International, Inc. 

e. MAPEI Corporation. 

2. For wall applications, provide mortar that complies with requirements for nonsagging mortar in addition to the other requirements in ANSI A118.1. 

C. Latex-Portland Cement Mortar (Thinset): ANSI A118.4. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. Bostik, Inc. 

b. Custom Building Products. 

c. Laticrete International, Inc. 

d. MAPEI Corporation. 

2. Provide prepackaged, dry-mortar mix containing dry, redispersible, vinyl acetate or acrylic additive to which only water must be added at Project site. 

3. For wall applications, provide mortar that complies with requirements for nonsagging mortar in addition to the other requirements in ANSI A118.4. 

2.10 GROUT MATERIALS 

A. Sand-Portland Cement Grout: ANSI A108.10, consisting of white or gray cement and white or colored aggregate as required to produce color indicated. 

B. Standard Cement Grout: ANSI A118.6. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. Bostik, Inc. 

b. Laticrete International, Inc. 

c. MAPEI Corporation. 

C. High-Performance Tile Grout: ANSI A118.7. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. Bostik, Inc. 

b. Laticrete International, Inc. 

c. MAPEI Corporation. 

2. Polymer Type: Ethylene vinyl acetate or acrylic additive, in dry, redispersible form, prepackaged with other dry ingredients. 

D. Water-Cleanable Epoxy Grout: ANSI A118.3, with a VOC content of 65 g/L or less. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. Boiardi Products Corporation; a QEP company.

b. Bostik, Inc. 

c. Laticrete International, Inc. 

d. MAPEI Corporation. 

2.11 MISCELLANEOUS MATERIALS 

A. Trowelable Underlayments and Patching Compounds: Latex-modified, portland cement-based formulation provided or approved by manufacturer of tile-setting materials for installations indicated. 

B. Vapor-Retarder Membrane: Polyethylene sheeting, ASTM D 4397, 4.0 mils (0.1 mm) thick. 

C. Tile Cleaner: A neutral cleaner capable of removing soil and residue without harming tile and grout surfaces, specifically approved for materials and installations indicated by tile and grout manufacturers. 

D. Grout Sealer: Manufacturer's standard product for sealing grout joints and that does not change color or appearance of grout. 

1. Manufacturers: Subject to compliance with requirements, provide products by one of the following: 

a. Bonsal American, an Oldcastle company. 

b. Custom Building Products. 

c. Southern Grouts & Mortars, Inc. 

2. Grout sealers shall comply with requirements of FloorScore certification. 

2.12 MIXING MORTARS AND GROUT 

A. Mix mortars and grouts to comply with referenced standards and mortar and grout manufacturers' written instructions. 

B. Add materials, water, and additives in accurate proportions. 

C. Obtain and use type of mixing equipment, mixer speeds, mixing containers, mixing time, and other procedures to produce mortars and grouts of uniform quality with optimum performance characteristics for installations indicated. 

PART 3 - EXECUTION 

3.1 EXAMINATION 

A. Examine substrates, areas, and conditions where tile will be installed, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of the Work. 

1. Verify that substrates for setting tile are firm; dry; clean; free of coatings that are incompatible with tile-setting materials, including curing compounds and other substances that contain soap, wax, oil, or silicone; and comply with flatness tolerances required by ANSI A108.01 for installations indicated.

2. Verify that concrete substrates for tile floors installed with bonded mortar bed or thin set mortar comply with surface finish requirements in ANSI A108.01 for installations indicated. 

a. Verify that surfaces that received a steel trowel finish have been mechanically scarified. 

b. Verify that protrusions, bumps, and ridges have been removed by sanding or grinding. 

3. Verify that installation of grounds, anchors, recessed frames, electrical and mechanical units of work, and similar items located in or behind tile has been completed. 

4. Verify that joints and cracks in tile substrates are coordinated with tile joint locations; if not coordinated, adjust joint locations in consultation with Architect. 

B. Proceed with installation only after unsatisfactory conditions have been corrected. 

3.2 PREPARATION 

A. Fill cracks, holes, and depressions in concrete substrates for tile floors installed with thin set mortar with trowelable leveling and patching compound specifically recommended by tile-setting material manufacturer. 

B. Where indicated, prepare substrates to receive waterproofing by applying a reinforced mortar bed that complies with ANSI A108.1A and is sloped 1/4 inch per foot (1:50) toward drains. 

C. Blending: For tile exhibiting color variations, verify that tile has been factory blended and packaged so tile units taken from one package show same range of colors as those taken from other packages and match approved Samples. If not factory blended, either return to manufacturer or blend tiles at Project site before installing. 

3.3 CERAMIC TILE INSTALLATION 

A. Comply with TCNA's "Handbook for Ceramic, Glass, and Stone Tile Installation" for TCNA installation methods specified in tile installation schedules. Comply with parts of the ANSI A108 series "Specifications for Installation of Ceramic Tile" that are referenced in TCNA installation methods, specified in tile installation schedules, and apply to types of setting and grouting materials used. 

1. For the following installations, follow procedures in the ANSI A108 series of tile installation standards for providing 95 percent mortar coverage: 

a. Exterior tile floors. 

b. Tile floors in wet areas. 

c. Tile swimming pool decks. 

d. Tile floors in laundries. 

e. Tile floors consisting of tiles 8 by 8 inches (200 by 200 mm) or larger. 

f. Tile floors consisting of rib-backed tiles. 

B. Extend tile work into recesses and under or behind equipment and fixtures to form complete covering without interruptions unless otherwise indicated. Terminate work neatly at obstructions, edges, and corners without disrupting pattern or joint alignments.

C. Accurately form intersections and returns. Perform cutting and drilling of tile without marring visible surfaces. Carefully grind cut edges of tile abutting trim, finish, or built-in items for straight aligned joints. Fit tile closely to electrical outlets, piping, fixtures, and other penetrations so plates, collars, or covers overlap tile. 

D. Provide manufacturer's standard trim shapes where necessary to eliminate exposed tile edges. 

E. Where accent tile differs in thickness from field tile, vary setting-bed thickness so that tiles are flush. 

F. Jointing Pattern: Lay tile in grid pattern unless otherwise indicated. Lay out tile work and center tile fields in both directions in each space or on each wall area. Lay out tile work to minimize the use of pieces that are less than half of a tile. Provide uniform joint widths unless otherwise indicated. 

1. For tile mounted in sheets, make joints between tile sheets same width as joints within tile sheets so joints between sheets are not apparent in finished work. 

2. Where adjoining tiles on floor, base, walls, or trim are specified or indicated to be same size, align joints. 

3. Where tiles are specified or indicated to be whole integer multiples of adjoining tiles on floor, base, walls, or trim, align joints unless otherwise indicated. 

G. Joint Widths: Unless otherwise indicated, install tile with the following joint widths: 

1. Ceramic Mosaic Tile: [1/16 inch (1.6 mm)] [1/8 inch (3.2 mm)]. 

2. Quarry Tile: [1/4 inch (6.4 mm)] [3/8 inch (9.5 mm)]. 

3. Pressed Floor Tile: [1/4 inch (6.4 mm)] [3/8 inch (9.5 mm)]. 

4. Glazed Wall Tile: [1/16 inch (1.6 mm)] [1/8 inch (3.2 mm)]. 

5. Porcelain Tile: [1/4 inch (6.4 mm)] [3/8 inch (9.5 mm)]. 

H. Lay out tile wainscots to dimensions indicated or to next full tile beyond dimensions indicated. 

I. Expansion Joints: Provide expansion joints and other sealant-filled joints, including control, contraction, and isolation joints, where indicated. Form joints during installation of setting materials, mortar beds, and tile. Do not saw-cut joints after installing tiles. 

1. Where joints occur in concrete substrates, locate joints in tile surfaces directly above them. 

J. Stone Thresholds: Install stone thresholds in same type of setting bed as adjacent floor unless otherwise indicated. 

1. At locations where mortar bed (thickset) would otherwise be exposed above adjacent floor finishes, set thresholds in latex-Portland cement mortar (thin set). 

2. Do not extend cleavage membrane waterproofing or crack isolation membrane under thresholds set in dry-set Portland cement or latex-Portland cement mortar. Fill joints between such thresholds and adjoining tile set on cleavage membrane waterproofing or crack isolation membrane with elastomeric sealant. 

K. Grout Sealer: Apply grout sealer to cementitious grout joints in tile floors according to grout-sealer manufacturer's written instructions. As soon as grout sealer has penetrated grout joints, remove excess sealer and sealer from tile faces by wiping with soft cloth.

3.4 GLASS TILE INSTALLATION 

A. Comply with TCNA's "Handbook for Ceramic, Glass, and Stone Tile Installation" for TCNA installation methods specified in tile installation schedules. Comply with parts of the ANSI A108 series "Specifications for Installation of Ceramic Tile" that are referenced in TCNA installation methods, specified in tile installation schedules, and apply to types of setting and grouting materials used. 

B. Extend tile work into recesses and under or behind equipment and fixtures to form complete covering without interruptions unless otherwise indicated. Terminate work neatly at obstructions, edges, and corners without disrupting pattern or joint alignments. 

C. Accurately form intersections and returns. Perform cutting and drilling of tile without marring visible surfaces. Carefully grind cut edges of tile abutting trim, finish, or built-in items for straight aligned joints. Fit tile closely to electrical outlets, piping, fixtures, and other penetrations so plates, collars, or covers overlap tile. 

D. Where accent tile differs in thickness from field tile, vary setting-bed thickness so that tiles are flush. 

E. Jointing Pattern: Lay tile in grid pattern unless otherwise indicated. Lay out tile work and center tile fields in both directions in each space or on each wall area. Lay out tile work to minimize the use of pieces that are less than half of a tile. Provide uniform joint widths unless otherwise indicated. 

1. For tile mounted in sheets, make joints between tile sheets same width as joints within tile sheets so joints between sheets are not apparent in finished work. 

F. Joint Widths: Unless otherwise indicated, install tile with the following joint widths: 

1. Large Format Glass Tile: [1/16 inch (1.6 mm)] [1/8 inch (3.2 mm)]. 

2. Mosaic Glass Tile: [1/16 inch (1.6 mm)] [1/8 inch (3.2 mm)]. 

3. Miniature Mosaic Glass Tile: [1/16 inch (1.6 mm)] [1/8 inch (3.2 mm)]. 

G. Lay out tile wainscots to dimensions indicated or to next full tile beyond dimensions indicated. 

H. Expansion Joints: Provide expansion joints and other sealant-filled joints, including control, contraction, and isolation joints, where indicated. Form joints during installation of setting materials, mortar beds, and tile. Do not saw-cut joints after installing tiles. 

1. Where joints occur in concrete substrates, locate joints in tile surfaces directly above them. 

I. Metal Edge Strips: Install at locations indicated. 

J. Grout Sealer: Apply grout sealer to grout joints according to grout-sealer manufacturer's written instructions. As soon as grout sealer has penetrated grout joints, remove excess sealer and sealer from tile faces by wiping with soft cloth. 

3.5 TILE BACKING PANEL INSTALLATION 

A. Install panels and treat joints according to ANSI A108.11 and manufacturer's written instructions for type of application indicated.

3.6 WATERPROOFING INSTALLATION 

A. Install waterproofing to comply with ANSI A108.13 and manufacturer's written instructions to produce waterproof membrane of uniform thickness that is bonded securely to substrate. 

B. Allow waterproofing to cure and verify by testing that it is watertight before installing tile or setting materials over it. 

1. Testing Agency: Engage a qualified testing agency to inspect substrate conditions, surface preparation, and membrane application, and furnish reports to Architect. 

2. Flood Testing: Flood test each waterproofed area for leaks, according to recommendations in ASTM D 5957, after completing waterproofing installation but before overlying construction is placed. Install temporary containment assemblies, plug or dam drains, and flood with potable water. 

a. Flood to an average depth of 2-1/2 inches (65 mm) with a minimum depth of 1 inch (25 mm) and not exceeding a depth of 4 inches (100 mm). 

b. Flood each area for 48 hours. 

c. After flood testing, repair leaks, repeat flood tests, and make further repairs until installations are watertight. 

3.7 CRACK ISOLATION MEMBRANE INSTALLATION 

A. Install crack isolation membrane to comply with ANSI A108.17 and manufacturer's written instructions to produce membrane of uniform thickness that is bonded securely to substrate. 

B. Allow crack isolation membrane to cure before installing tile or setting materials over it. 

3.8 ADJUSTING AND CLEANING 

A. Remove and replace tile that is damaged or that does not match adjoining tile. Provide new matching units, installed as specified and in a manner to eliminate evidence of replacement. 

B. Cleaning: On completion of placement and grouting, clean all ceramic tile surfaces so they are free of foreign matter. 

1. Remove grout residue from tile as soon as possible. 

2. Clean grout smears and haze from tile according to tile and grout manufacturer's written instructions but no sooner than 10 days after installation. Use only cleaners recommended by tile and grout manufacturers and only after determining that cleaners are safe to use by testing on samples of tile and other surfaces to be cleaned. Protect metal surfaces and plumbing fixtures from effects of cleaning. Flush surfaces with clean water before and after cleaning. 

3.9 PROTECTION 

A. Protect installed tile work with kraft paper or other heavy covering during construction period to prevent staining, damage, and wear. If recommended by tile manufacturer, apply coat of neutral protective cleaner to completed tile walls and floors. 

B. Prohibit foot and wheel traffic from tiled floors for at least seven days after grouting is completed.

C. Before final inspection, remove protective coverings and rinse neutral protective cleaner from tile surfaces.

END OF SECTION 093013

CERAMIC TILING
093013 - 1

