ASTM E 1300 GLASS LOAD RESISTANCE REPORT

JOB DETAILS:

Project Name:		RIVER CHASE - SHEET 4 - GL2 - 50.5 x 23 (Inner & Outer)

)WINDOW GLASS DETAILS:           1-”  Insulated Window

Lite Support                                    4 Edges

Rectangular Dimensions:	Long:    50.5”            : Short:   23”

Window Construction:     	 Insulated   -   ¼” Glass / 1/2” Gas/ 1/4 ” Glass

Window Orientation:		Sloped at 0° from Vertical

Outer Lite

Product                                          SNX  on CrystalGray #2

Glass Type:		             Tempered

Construction:		             Monolithic

Nominal Thickness:	             Plate thicknesses   --  0.250”

InnerLite

____________________________________________________________________________

Product:                                          Clear: Medium Gray Frit #4

Glass Type:		             Tempered

Construction:		  	Monolithic

Nominal Thickness:	 	Plate thicknesses   --  0.250”

SHORT DURATION LOAD, RESISTANCE AND DEFLECTION DATA:

Load (<=60 sec.)    		                                            :       45 psf

Load Deflection (Inner  Lite):				:       0.063     in

Load Deflection (Outer  Lite):				:       0.063     in

Maximum Allowable Glass Deflection:	:        L/175

CONCLUSION:

This glass configuration is below the maximum L/175 deflection for the specified loading.

STATEMENT OF COMPLIANCE:

Procedures followed in determining the resistance of this window glass configuration are in accordance with ASTM E 1300-97.

Disclaimer:

The load resistance of specified glass types exposed to uniform lateral loads of short or long duration subject to the following conditions:

- The glass is free of edge and surface damage and has been properly glazed in the opening in conformance with the manufacturers recommendations.

- The glass is supported on all sides by a framing system sufficiently stiff to limit lateral deflection of the glass edge (not center-of-glass) less than to 1/175 of the glass edge length; Center of glass deflection in excess of 19-mm (0.75-in.) is a design issue and does not affect glass strength;

- The laminated glass factors for short term loads are representative of roof temperature data to which the glass is exposed.

For other limiting conditions that may apply, refer to Section 5 of ASTM E1300 and local building codes.

Prepared by : 	__________________________	Date:___ 1/9/2017_