ASTM E 1300 GLASS LOAD RESISTANCE REPORT

3/8/2017

JOB DETAILS:

Project Name:		Laurel School Renovation

WINDOW GLASS DETAILS:           1/2 “ Laminated Windows

Lite Support                                    4 Edges

Rectangular Dimensions:	Various

Window Construction:     	 Laminated   -         1/4" CL TP 090 PVB 1/4" CL TP

Window Orientation:		Sloped at 0° from Vertical

G1 Designated Panes from Plans Sheet Numbers 104, 105, 106 107, and 108

WINDOW SIZE                                                                                             DEFLECTION

Sheet 104 - Laurel School  G1 - 32.5 x 32.1675                                                           < 0.006 “

Sheet 104 - Laurel School  G1 - 55.625 x 32.1675                                                         0.003”

Sheet 104 - Laurel School  G1 - 56 x 32.1675                                                                 0.003”

Sheet 105 - Laurel School  G1 - 32.5 x 31                                                                     < 0.006 “

Sheet 105 - Laurel School  G1 - 54.875 x 31                                                                    0.002”

Sheet 105 - Laurel School  G1 - 56 x 31                                                                            0.002”

Sheet 106 - Laurel School  G1 - 32.5 x 34.75                                                                < 0.006 “

Sheet 106 - Laurel School  G1 - 37.5 x 34.75                                                                < 0.006 “

Sheet 106 - Laurel School  G1 - 55.25 x 34.75                                                                 0.006”

Sheet 106 - Laurel School  G1 - 67 x 34.75                                                                       0.015”

Sheet 107 - Laurel School  G1 - 76.625 x 52.625                                                             0.141”

Sheet 108 - Laurel School Door  G1 - 28.5 x 19                                                            < 0.006“

Sheet 108 - Laurel School Door  G1 - 29.75 x 24.5                                                        < 0.006“

Sheet 108 - Laurel School Door  G1 - 40 x 24.5                                                             < 0.006“

Sheet 108 - Laurel School Door  G1 - 59.5 x 19                                                             < 0.006“

Sheet 108 - Laurel School Door  G1 - 63.5 x 29.75	                                               0.004”

Sheet 108 - Laurel School Door  G1 - 63.5 x 40                                                                0.030”

Sheet 108 - Laurel School Door  G1 - 77.8 x 27.9                                                             0.010”

Sheet 108 - Laurel School Door  G1 - 77.63 x 27                                                              0.010”

Sheet 108 - Laurel School Door  G1 - 79.58 x 27.78                                                         0.011”

----------------------------------------------------------------------------------------------------------------------------------

SHORT DURATION LOAD, RESISTANCE AND DEFLECTION DATA:

Load (<=60 sec.)    		                                            :       45 psf

Maximum Allowable Glass Deflection:	:        L/175

CONCLUSION:

The G1 glass configurations are below the maximum L/175 deflection for the specified loading.

STATEMENT OF COMPLIANCE:

Procedures followed in determining the resistance of this window glass configuration are in accordance with ASTM E 1300-97.

Disclaimer:

The load resistance of specified glass types exposed to uniform lateral loads of short or long duration subject to the following conditions:

- The glass is free of edge and surface damage and has been properly glazed in the opening in conformance with the manufacturers recommendations.

- The glass is supported on all sides by a framing system sufficiently stiff to limit lateral deflection of the glass edge (not center-of-glass) less than to 1/175 of the glass edge length; Center of glass deflection in excess of 19-mm (0.75-in.) is a design issue and does not affect glass strength;

- The laminated glass factors for short term loads are representative of roof temperature data to which the glass is exposed.

For other limiting conditions that may apply, refer to Section 5 of ASTM E1300 and local building codes.

Prepared by : 	__________________________	Date:____3/16/2017_________________