554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

dammonengineering.com

info@dammonengineering.com

# Structural Inspection

11-14-2023

Nigel Reynolds

Facilities Coordinator

Exchange Right

1055 E. Colorado Blvd.

Suite 310

Pasadena Ca. 91106

Ref: NLP 25 Tractor Supply

2083 Gause Blvd.

Slidell, La. 70460

Construction:

One-story, corrugated metal roof, pre engineered metal frame building on a spread footing foundation with a floating slab.

Scope:

This inspection is limited to a visual inspection of the interior and exterior of the building; No Inspection of the mechanical or electrical systems was performed.  This report is as outlined by the National Academy of Building Inspection Engineers and is not an explanation of cause, effect, or engineering.

History:

Dammon Engineering was contacted to perform a structural inspection of the referenced building due to a concern about the cracks found in the exterior CMU block walls. This site was previously a vehicle junk yard prior to the new construction of a pre engineered metal building for the use of a retail business.

Findings:

An overall visual inspection of the interior and exterior of the building walls was conducted and several vertical cracks are noted in the CMU block walls everywhere there is a metal column including the southwest corner of the building near the women’s bathroom. Some of these cracks go all the way down to the last visible block but it couldn’t be verified if these cracks go into the concrete spread footings due to the design of the foundation is twelve inches below grade.

The slab/floor was also noted to have some small hairline cracks in the front left and right rear of the bldg including the area of the rear help desk.

The exterior walls are made up of CMU blocks with vertical rebar @ 4’ O.C. When the CMU blocks abut an exterior column, the CMU blocks are cut thin to enclose the exterior column with no rebar. When expansion and contraction occurs, these thin cut blocks are coming apart. There are some areas that the thin cut CMU blocks around the columns are falling out.

The majority of the eastside of the building has gutters with downspouts and are directed over the planters onto the parking pavement into the drainage system. There is one down spout in the rear that empties onto the parking paving but the down spout elbow is not connected and allowing rain water under the foundation.

The Westside of the building has gutters and down spouts that empty onto the side yard paving. These are in good physical condition but are really close to the edge of the building and allowing some splash back towards the building foundation.

Conclusion:

It’s important to recognize that South Louisiana has been in a severe drought this year and discussing with the employees these findings were noticed within the last few months.

It is important to note that all foundations settle.  Usually, everything settles together and the fastest rate of settlement occurs in the first year after construction.  By the fifth or sixth year the settlement has exponentially slowed to where there is little danger that something will happen unless caused by weather, expansion & contraction, tree roots, improper drainage, etc.

Recommendation:

The cracks in the CMU block walls and foundation do not appear to have compromised the structural integrity of the building.  It is my opinion that the structural integrity of this building is currently sound, but the foundation will expand and contract with the ground movement.

Items to be addressed are as follows:

- Remove and replace busted CMU blocks with more than 1/4" gap.

- Verify bolts are tight where beams are attached to the columns.

- Seal the cracks in the CMU block walls and floor with an elastic sealant for concrete to prevent insects from entering the Building.

- Fix the one downspout that the elbow is off.

- As an option, construct expansion joints @ each column.

See attached pictures

Sincerely,

Brian Mistich, P.E.